## Slide 1
courtesy of T. DebRoy

## Slide 2
image courtesy of
Parker Beatty
Creative Commons Attribution-Share Alike 4.0 International

## Slide 4
There are many industrial processes where we mix powders rather than atoms.
Ball milling is used to make strange alloys where powders really don’t want to mix, but we force them to do so and form an atomic solution.
The purpose is to achieve properties never before achieved.
an application of thermodynamics

## Slide 5
extrusion of canned powder
image courtesy of Jan-Olof Nilsson
Sandvik Materials Technology.
Extrusion of stainless steel.

## Slide 6
an application of thermodynamics
Suppose that instead of atoms, we mix particles of A and B, each containing many atoms
What is the configurational entropy of mixing?

## Slide 7
For a random mixture of particles, number of configurations given by:

## Slide 9
Solution-like behaviour when particles about 1000 atoms in size
Free energy of mixing due to configurational entropy alone

## Slide 10: How do we know that an atomic solution has formed?

## Slide 11
Chou & Bhadeshia

## Slide 13
Probability of pairwise bonds in random solution

## Slide 15
displacive transformation products are stopped at parent grain boundaries

## Slide 19: Phase transitions equilibrium state
photograph courtesy of Sunita Hansraj from her Antarctica expedition
“nothing changes, no matter how long it is observed”
stable to infinitesimal perturbation

## Slide 21: transformation without composition change

## Slide 22
pure iron

## Slide 23
Solutions

## Slide 25: chemical potential

## Slide 26
ice: pure
ocean: salty water
photograph courtesy of Sunita Hansraj from her Antarctica expedition
two solutions in contact
compositions different, yet in equilibrium

## Slide 28
International molybdenum association
1100-1200 °C
Mo-0.5Ti wt%

## Slide 30: proportions of phases: lever rule

## Slide 31: Liquid can decompose simultaneously into two solids

## Slide 32
Simulation, Britta Nestler, RWTH Aachen

## Slide 33: eutectic
Edo Museum in Tokyo. Shogun era, about 130 years ago.
Melting temperatures
Lead 328°C
Tin 232°C
Pb-62Sn wt% 183°C

## Slide 35
eutectic
hypereutectic
hypoeutectic

## Slide 36: Why eutectic?

## Slide 44
images courtesy of
Jane Weston

## Slide 45
constant temperature section
ternary phase diagram

## Slide 46
quaternary
system

## Slide 47: What do we need from phase diagrams?
stable phases
fractions of phases
compositions of phases
as a function of temperature, pressure etc.
consider 7 components (Fe, C, Si, Mn, Ni, Mo, Cr)
three phases BCC, Fe3C, M23C6

## Slide 50
Condition for equilibrium is simple:
uniform chemical potential defines equilibrium

## Slide 53
Praseodymium-neodymium solid solutions
Lundin, Pool: J. Less Common Metals 9 (1965) 48-53

## Slide 54
configurational entropy maximum at equiatomic concentration
free energy minimum at equiatomic concentration, assuming only the entropy contributes to free energy
1000 K

## Slide 55: “regular” solution
change in bond energy when AA and BB bonds replaced in part by AB and BA bonds

## Slide 59: Create solution by mixing in proportion
A
B
solution
number of A atoms
number of B atoms
total number of A+B atoms

## Slide 60
A
B
solution
number
A-A bonds?
number
B-B bonds?

## Slide 64
Parlier M, Valle R, Perrière L, Lartigue-Korinek S, Mazerolles L. Potential of directionally solidified eutectic ceramics for high temperature applications. Aerospace Lab. 2011 Nov 1(3):p-1.