Application of Bayesian Neural Network for modeling and prediction of ferrite number in austenitic stainless steel welds

M. Vasudevan, M. Murugananth*, and A.K. Bhaduri

Materials Joining Section

Metallury and Materials Group

Indira Gandhi Centre for Atomic Research

Kalpakkam

*Department of Metallurgy and Materials Science

Cambridge University, UK

Abstract

As neural networks are extremely useful in recognizing patterns in complex data, Bayesian neural network analysis has been followed in the present work to reveal the influence of compositional variations on ferrite content for the austenitic stainless steel base compositions from the available database and to study the significance of individual elements on ferrite content in austenitic stainless steel welds based on the optimized neural network model. Bayesian neural network’s predictions are accompanied by error bars  and the significance of each input variable is automatically quantified in this type of analysis. Neural network model based on Bayesian framework for ferrite prediction in austenitic stainless steel welds has been developed using the database which was used for generating the WRC - 92 diagram. The Bayesian framework uses a committee of models for generalization rather than a single model. The  best model was chosen based on minimum in the test error and maximum in the logarithmic predictive error.  The optimized model can be used for predicting the ferrite number in austenitic stainless steel welds with a better accuracy than the constitution diagrams. Using this model,  the influence of variations in the individual elements such as carbon, manganese, silicon, chromium, nickel, molybdenum, nitrogen, niobium, titanium, copper, vanadium, and cobalt on the ferrite number in austenitic stainless steel welds has been determined. It was found that the change in ferrite number is a non-linear function of the variation in the concentration of the elements. Elements such as silicon, chromium, nickel, molybdenum, nitrogen, titanium, and vanadium were found to influence the ferrite number more significantly than the rest of the elements in austenitic stainless steel welds. Manganese was found to have less influence on the ferrite number. Titanium was found to influence the ferrite number more significantly than niobium. This observation is new as WRC - 92 diagram only considered the niobium content in calculating the chromium equivalent.

1. 0 Introduction

The ferrite content in stainless steel welds play an important role in determining the fabrication and service performance of welded structures. The ability to estimate the ferrite content accurately has proven very useful in predicting the various properties of stainless steel welds. A minimum ferrite content is necessary to ensure hot cracking resistance in these welds1-5, while an upper limit on the delta-ferrite content determines the propensity to embrittlement due to secondary phases6 (e.g., sigma phase) formed during elevated temperature service. At cryogenic temperatures, the toughness of the stainless steel weld is  strongly influenced by the ferrite content7 . In duplex austenitic-ferritic stainless steel weld metals, a lower ferrite limit is specified for stress corrosion cracking resistance while the upper limit is specified to ensure adequate ductility and toughness4 . Hence, depending on the service requirement a lower limit and/or an upper limit on ferrite content is generally specified. During the selection of filler metals the ferrite content is normally estimated from the constitution diagrams such as the Schaeffler8, DeLong9 and WRC–92 diagrams10. These constitution diagrams are based on different Creq and Nieq formulae as given in the Table 1. The coefficients for C and Nb have been increased from 30 and 0.5 in the Schaeffler and DeLong diagrams to 35 and 0.7, respectively, in the WRC–92 diagram, whereas for N it has been lowered to 20 from 30 in the DeLong diagram. The WRC – 92 diagram estimates the ferrite content to reasonably good accuracy and also provides additional information about the mode of solidification. In these diagrams, the ferrite contents of various welds had been measured experimentally by either metallography (Schaeffler) or magnetic methods (DeLong and WRC–92 ) and are presented as iso-ferrite content maps.

| Constitution Diagram | Creq and Nieq |
| --- | --- |
| Schaeffler Diagram (1949) | Creq = Cr + Mo + 1.5 Si + 0.5 Nb Nieq = Ni + 30C + 0.5 Mn |
| DeLong Diagram (1973) | Creq = Cr + Mo + 1.5 Si + 0.5 Nb Nieq = Ni + 30C + 30 N + 0.5 Mn |
| WRC–92 Diagram (1992) | Creq = Cr + Mo + 0.7 Nb Nieq = Ni + 35C + 20N + 0.25 Cu |

Table1:	Creq and Nieq formulae used for estimating the delta-ferrite content from constitution diagrams

The ferrite content in stainless steel weldments is controlled by several factors and is the result of the series of microstructural changes that take place during the welding process11. Thus, the relationship between the alloy composition and the ferrite content can be quite complex. Linear expression such as given in the above equations can not be expected to take into account all the crucial factors. The relative influence of each alloying addition given by that elements coefficients in the Creq or Ni eq expression is likely to change when there is a change in the base composition.  In addition, constitution diagrams that rely on simple linear expressions for the Creq and Nieq  ignore the interactions between the elements.  Hence, the ferrite content estimated using the constitution diagrams will always be less accurate and will never be closer to the measured values.

Kotechi 3 has pointed out that there are number of alloying elements that have not been considered in the most accurate diagram to date, the WRC – 92 diagram. Elements like silicon, titanium, tungsten are not given due considerations though they are known to influence the ferrite content. He also stressed the point that cooling rate effects need to be considered more thoroughly in these constitution diagrams.

Recent research activities have been focused on studying the effect of various alloying elements on the ferrite content  and controlling ferrite content by modifying the weld metal compositions. In another approach for estimating ferrite content (Function Fit model), the difference in free energy between the ferrite and the austenite was calculated as a function of composition and this was related to ferrite number. The advantages of this semi-empirical model12 over the WRC 1992 diagram was that the model considers the effect of other alloying elements and the ease of extrapolation of the model to higher Creq and Nieq values. The major limitation of the constitution diagrams in not acounting for the elemental interactions was overcome by the use of neural networks in predicting ferrite content in stainless steel welds by Vitek et al13-14. The improvement of accuracy in predicting the ferrite content by the use of neural networks (feed-forward network  with a back-propagation optimization scheme) has been clearly brought by their study. The effect of various element additions on the ferrite content for few base compositions was examined by simply calculating the ferrite number as a function of composition. However, it was not possible in their analysis for direct interpretation of the elemental contributions to the final ferrite number.

Other methods and constitution diagrams are continuously being put forward to predict the ferrite content for a wider range of stainless steel  types. Thus, Prediction and measurement of ferrite in stainless steel welds remains of scientific interest due to inaccuracies involved in all the current methods.  In this context, the development of a more accurate predictive tools for estimating the effect of various alloying elements on the ferrite content for different stainless steel welds assumes importance.

The neural network analysis can capture interactions between the inputs because the hidden units are nonlinear. The training process involves a search for the optimum non-linear relationship between the inputs and the outputs, and is computer intensive. The outcome of the training is a set of coefficients (called weights) and a specification of the functions which in combination with the weights relate the input to the output. Once the network is trained, estimation of the outputs for any given inputs is very rapid15.

A potential risk associated with neural network analysis is overfitting of the training data. To avoid overfitting, Mackay16 has developed a Bayesian framework to control the complexity of the neural network. Main advantages of this method are that it provides meaningful error bars for the model predictions and also it is possible to identify automatically the input variables which are important in the non-linear regression. This methodology has proved to be  extremely useful in materials science where properties need to be estimated as a function of  a vast array of inputs.  In the present study, Bayesian neural network analysis has been applied to develop a generalized model for predicting ferrite number using data that were used to generate the WRC – 1992 diagram. Using the generalized model, the effect of individual elements on the ferrite number for two different base compositions has also been quantified.   The accuracy of the model has also been compared with the other ferrite number (FN) prediction methods.

2. 0 Database

The data that was used for generating the WRC –1992 diagram have been used in the present analysis. This database consists of stainless steel SMA (submerged metal arc) weld compositions and ferrite contents. The data well represented the common 300 -series stainless steel weld compositions such as 308, 308 L, 309, 309 L, 316, 316 L types. This database was collected from the literature4. The aim of the analysis was to model the ferrite number as a function of chemical composition. The database consists of 924 data lines. For the cases where the composition values were not available for elements such as Nb, Ti, V, Cu and Co the values were assumed zero. Table 2 gives the range, mean and standard deviation of the each composition variable and the output. This simply gives the idea of the range covered and can not be used to define the range of applicability of the neural network model as the input variables are expected to interact in neural network analysis. In Bayesian neural network analysis, size of the error bars define the range of useful applicability of the trained network. Scatter in the data for each input variable is shown in fig. 1.

Table 2 Range, Mean, standard deviation of the each input variable and the output.

| Elements | Minimum | Maximum | Mean | Std. Deviation |
| --- | --- | --- | --- | --- |
| C Mn Si Cr Ni Mo N Nb Ti Cu V Co Fe FN | 0 0.35 0.03 1.05 4.61 0.01 0.01 0 0 0 0 0 45.59 0 | 0.2 12.67 6.46 32 33.5 10.7 2.13 0.88 0.33 6.18 0.23 0.69 72.51 98 | 0.04 1.88 0.53 20.51 11.31 1.42 0.09 0.03 0.02 0.14 0.04 0.03 63.94 12.04 | 0.0219 1.79 0.35 2.76 2.56 1.64 0.14 0.098 0.028 0.437 0.04 0.046 4.33 17.31 |

3. 0 Bayesian Neural Network Analysis

The Bayesian neural network analysis has been extensively used for modeling and prediction of mechanical properties in welds17-20 and alloys21.  The complete description of the method is described elsewhere16. The aim of the analysis is to model the ferrite number in stainless steel welds as a function of composition. The networks employed consists of thirteen input nodes, xi, representing the thirteen composition variables, a number of hidden nodes, hI, and one output y. The schematic structure of the network is shown in fig. 2. The single output represents the ferrite number. Both the input and output variables were normalized within the range  0.5 as follows

xN=x−xminxmax−xmin−0.5

where xN  is the normalized value of x, which has maximum and minimum values given by xmax and xmin. Eighty neural network models were created using the data. All the models were trained on a training dataset which consisted of a random selection of half of the data (462) from the whole dataset. The remaining (462) formed the test dataset which was used to see how the model generalizes on unseen data. The models differed in terms of the number of the hidden units and random seeds used to initiate the network. For a given number of hidden units, five different sets of random seeds were used. The number of hidden units varied from 1 to 16 for the 80 different models.

The outputs are calculated from the inputs as follows: linear functions of the inputs, xj multiplied by the weights wij  are operated on by a hyperbolic tangent transfer function

hi=tanhjNwij(1)xj+θi(1)

so that each input contributes to every hidden unit where N is the number of input variables. The bias is designated  and is analogous to the constant that appears in linear regression. The transfer from the hidden units to the output is linear, and is given by

y=iwi(2)hi+θ(2)

the output y is therefore a non-linear function of xj, the function usually selected being the hyperbolic tangent because of its flexibility.

The network is completely described if the number of input nodes, output nodes and the hidden units are known along with all the weights wij and biases i. These weights are determined by training the network which involves the minimization of an objective function.

Bayesian neural network analysis developed by Mackay16  allows the calculation of error bars representing the uncertainty in the fitting parameters. It is possible to make predictions which have two components in the error bars – one representing the perceived level of noise in the output and the second indicating the uncertainty in fitting the data. This second component which comes from a Bayesian frame work allows the relative probabilities of models of different complexity to be assessed.  Further it allows us to obtain quantitative error bars which vary with the position in the input space depending on the uncertainty of fitting the function in that region of space. Instead of calculating a unique set of weights, a probability distribution of weights is used to define the fitting uncertainty.  The error bars therefore become large when data are sparse or locally noisy. In this context, a very useful measure is the log predictive error (LPE), because the penalty for making a wild prediction is reduced if that wild prediction is accompanied by appropriately large error bars

LPE=n12[t(n)−y(n)2σy(n)2+log2πσyn12]

Note that larger value of the log predictive error implies a better model. In this method it is also possible to identify automatically the input variables which are in fact significant in influencing the output variable. The input variables which are less significant are down-weighted in the regression analysis.

3. 1 Characteristics of Bayesian Neural Network Model on Ferrite Number

Characteristics of the model could be seen from the plots shown in fig. 3.  The perceived level of noise decreases with the increasing complexity i.e the increase in the hidden units (fig. 3a). The test error goes through a minimum at five units (fig. 3b) and the log predictive error reaches the maximum at fifteen hidden units (fig. 3c). The error bars throughout the present work represent the fitting uncertainty estimated from the Bayesian framework.  It is evident from the plot that there are few outliers in the predicted versus measured ferrite number for the test dataset (fig. 3f). Each of these outliers was found to represent unique data not represented in the training dataset. It is possible that a committee of models can make a more reliable prediction than an individual model. The best models are ranked using the values of the log predictive errors. Committees are then formed by combining the predictions of the best L models, where L = 1,2,3…; the size of the  committee is therefore given by the value of L. A plot of the test error of the committee versus its size gives a minimum which defines the optimum size of the committee as shown in the (fig. 3d). As seen in the figure the test error associated with the best single model is clearly greater than that of any of the committees.  The committee with 38 models was found to have an optimum membership with the smallest error. The committee was therefore retrained on the entire dataset and used for predictions. The final comparison between the predicted and measured ferrite number values for the committee of 38 is shown in fig. 4.  Details of the 38 members of the optimum committee are given in table. 3.

Model Hidden units 

1 15 0.01942 2 14 0.01594 3 7 0.02572 4 12 0.01406 5 7 0.0249 6 5 0.02847 7 11 0.02038 8 7 0.02305 9 16 0.01859 10 3 0.03037 11 10 0.02542 12 8 0.02445 13 6 0.02685 14 9 0.02083 15 6 0.02542 16 8 0.02517 17 10 0.01971 18 15 0.01831 19 13 0.02106 20 10 0.01967 21 14 0.02354 22 4 0.03123 23 8 0.02424 24 4 0.03127 25 11 0.02151 26 12 0.01855 27 11 0.01777 28 13 0.02039 29 1 0.0411 30 1 0.0411 31 1 0.0411 32 1 0.04109 33 1 0.04106 34 5 0.028 35 9 0.01875 36 9 0.02363 37 4 0.0301 38 8 0.01845

Table  3  Hidden units and   in optimum Ferrite Number committee model

4.0 Results and Discussions

The comparison between the predicted and measured FN values for the committee of models is shown in fig. 4a for the complete dataset.  There was excellent agreement between the measured and the predicted FN values. The correlation coefficient was determined to be 0.98025.  Fig. 4b shows the comparison between the measured and predicted FN values of 316 LN austenitic stainless steel (our lab data),  which was not used in training during model creation. The absolute error between the measured and predicted FN for entire dataset (25 nos) was less than 2. This error value is better than the error values reported by other methods for unseen data. The size of the error bars in fig. 4b are large for few of the data indicating compositions similar to that have not been used in the training. Figure 5 indicates the significance w  of each of the input variable as perceived by the first five best models in committee. The w  value represents the extent to which a particular input explains the variation in the output, rather like a partial correlation coefficient in linear regression analysis.  The elements Mn and Nb are not significant in influencing the ferrite number.Influence of Mn on the ferrite number is insignificant for 300 series stainless steels and this is in agreement with the results reported in the literature 22 which says that variation in Mn concentration (in the range from 1 to 12%) has almost no effect on the deposited ferrite number.  Though Nb which is found to be insignificant in the present study finds a place in the term for calculating the Creq   for the WRC – 1992 diagram. Cr and Ni were found to be the main elements in influencing the ferrite number.  This is in agreement with the published literature on ferrite number in stainless steel welds. The other elements to follow are Mo, N, V, Ti, Cu, Co, Si, C and Fe in that order. As per our model, these elements influence the ferrite number significantly. However, some of these elements like V, Ti, Co and Si have not been included in the terms for calculating Nieq and Creq in the WRC – 1992 diagram.

4.1 Comparison of the accuracy of the present model with existing methods

The error distribution (measured FN – Predicted FN) for the Bayesian neural network model is shown in fig. 6. It can be seen that the absolute error lies within 2.5 for most of the dataset used in the training while in the case of FNN-1999 model it was less than 3 for around 80% of the dataset used in training14.  The error distributions for our model is symmetrical about zero implying that model fits the data well.   Also the tail of the error distributions are less compared to the other methods12,14.  The error distributions are quantified and compared with that of the FNN-1999 model in table 4. For all the cases, Bayesian neural network model is better compared to that of the FNN – 1999 model. Vitek et al 14 have reported that FNN – 1999 model is more accurate compared to WRC – 1992 and the Function fit model. Root mean square error between the measured and the predicted FN values for all the four methods (Bayesian neural network model, FNN – 1999 model, Function Fit model and WRC – 1992 diagram) are compared in the table 5. These error values represent the quantitative measure of the degree to which the various models fit the complete dataset on which they were trained. Bayesian neural network analysis has the lowest error of all the four methods. This model has an improvement of 43% over the FNN-1999 model and 65% over the WRC – 1992 diagram. From the comparisons of the accuracies of the predictions by different methods, it is very clear that Bayesian neural network model presented in this work is the most accurate model for prediction of ferrite number in stainless steel welds.

| Bayesian Neural Network model | FNN – 1999 model |
| --- | --- |
| Absolute Number % of Total Error of points | Number % of Total Of points |
|  1.5 684 74.0% | 621 64.6% |
|  2.5 820 88.7% | 764 79.5% |
|  3.5 864 93.5% | 826 86.0% |
|  4.5 888 96.1% | - - |
|  5.5 900 97.4% | - - |
|  5.5 20 2.16% | - - |
|  9.5 4 0.4% | 32 3.3% |

Table 4 Comparison of the Errors (experimental – Predicted FN) for the Bayesian Neural network model and the FNN – 1999 model14 (training database)

| Prediction Method | RMS Error |
| --- | --- |
| Bayesian Neural Network Model | 1.99 |
| FNN – 1999 Back Propagation Neural Network Model14 | 3.5 |
| WRC – 199210 | 5.8 |
| Function Fit Model12 | 5.6 |

Table 5 Comparison of the Root Mean Square Errors for complete Training database for different FN prediction methods

4.2 Composition dependent behaviour

The severe limitation of the WRC – 92 diagram is that the coefficients in the terms for Creq and Nieq formulae are constant and hence the influence of an individual element on FN is same irrespective of the change in the base composition. As neural networks can take into account the interaction between the input variables and their influence over the output variable, it would be interesting to study how the change is base compositions affect FN.  This was done with two starting base compositions and then allowing each element to vary over a limited range adjusting Fe concentration accordingly but holding all other element concentrations constant. Table 6 gives the base compositions of the two materials for which the effect of concentration of various elements on the ferrite number has been studied.

| Material | C | Mn | Si | Cr | Ni | Mo | N | Nb | Ti | Cu | V | Co | Fe |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 308 L | 0.035 | 0.8 | 0.4 | 20.4 | 10 | 0.05 | 0.06 | 0.07 | 0.08 | 0.14 | 0.09 | 0.07 | 67.805 |
| 316 L | 0.035 | 0.8 | 0.9 | 19.4 | 11 | 2.5 | 0.06 | 0.07 | 0.08 | 0.24 | 0.09 | 0.1 | 64.725 |

Table 6 : Chemical composition of the two base materials

4.2.1 Application of the generalized model to 308 L austenitic stainless steel weld

The predicted ferrite number vs the variation in the concentration of the individual elements for 308 L austenitic stainless steel are given in the fig. 7.  The variation was found to be non-linear. Some of the elements like C, N and Ni are found to decrease the ferrite number with increasing concentration indicating that they are strong austenite stabilizers. The elements like Cr, Si and V are found increase the ferrite number with increasing concentration indicating that they are strong ferrite stabilizers. The variation in the elements like Mn, Mo, Nb, Cu and Co are found not to influence the ferrite number for this base composition. The surprising effect is found for Ti which shows a varying effect on ferrite number. This observation contradicts the observation by Vitek14 who reported the role of Ti as a strong ferrite stabilizer but for a different base composition. For the present base composition effect of Ti can be explained as follows: Titanium is expected to tie up with carbon and nitrogen very effectively in forming carbides or carbonitrides only at stoichiometric compositions23,24. Other than stoichiometric compositions, titanium is less effective  in forming the carbides or carbonitrides. So, the strong austenite stablilizers carbon and nitrogen remain in solid solution reducing the ferrite number of the stainless steel. However, this should be verified experimentally.

4.2.2 Application of the model to 316 L austenitic stainless steel weld

The predicted ferrite number vs the variation in the concentration for the individual elements for 316 L austenitic stainless steel are given in the fig. 8. Variation of ferrite number due to change in concentration of elements was found to be non-linear.  In the case of 316 L stainless steel, the elements C, Mn, Ni and N are found to decrease the ferrite number with increasing concentration indicating that they are strong austenite stabilizers. The elements Cr, Si and Mo are found to increase the ferrite number with increasing concentration indicating that they are strong ferrite stabilizers. The elements V, Cu and Co are found to increase the ferrite number slightly and hence they are weak ferrite stabilizers. There is a change in the contribution of the individual elements to FN when the base composition is changed. Thus, the severe limitation of the WRC – 1992 diagram that the Creq and Nieq coefficients do not change as a function of the alloy composition has been overcome by using neural network analysis. The role of Cu in its contribution to ferrite number for this base composition is opposite to its role as projected in the WRC – 1992 diagram.  The variation in the concentration of the element Nb was found not to influence the ferrite number. Titanium is agin found to show a varying effect on its influence over the FN.  The effect of Ti on FN is stronger compared to that of the 308 L stainless steel weld.

5.0 Conclusions

The generalized model for predicting the ferrite number in stainless steel welds using Bayesian neural network analysis has been developed. The accuracy of the Bayesian neural network model in predicting ferrite number is better compared to the existing FN prediction methods. Significance of the individual elements on FN has been quantified. Elements like manganese and niobium are insignificant in influencing the ferrite number. The study has clearly brought out the fact that individual element contributions to FN vary depending on the base composition and hold a non-linear relationship.  The variations in the concentrations of  silicon, vanadium and titanium is found to significantly influence the ferrite number for the two base compositions studied.  Titanium shows a varying effect for both the base compositions considered in the present study.  Based on the present study, it is suggested that Creq and Nieq formulas used in the WRC – 92 diagram has to be analyzed further in terms of the elements considered in order to improve the accuracy of prediction of ferrite number for stainless steel welds.

6.0 Acknowledgements

The authors would like to acknowledge Prof. H.K.D.H Bhadeshia for providing us the software. The authors would also like to acknowledge Dr. Baldev Raj, Director, metallurgy and Materials Group, Indira Gandhi Centre for Atomic Research, Kalpakkam for permitting us to publish this work.

7.0 References

- C.D. LUNDIN and C.P.D. CHOU, Hot Cracking Susceptibility of Austenitic Stainless Steel Weld Metals, 1983, WRC Bulletin 289, 1-80.

- C.D. LUNDIN, W.T. DELONG and D.F. SPOND, Ferrite-Fissuring Relationships in Austenitic Stainless Steel Weld Metals, (1975), 54 (8), 241s-246s.

3.	D.J. KOTECHI, Ferrite Determination in Stainless Steel Welds – Advances Since 1974, 1997, Welding Journal 76 (1), 24s-37s.

4.	C.N. McCOWAN, T.A. SIEWERT and D.L. OLSON, Stainless Steel Weld Metal: Prediction of Ferrite Content, 1989, WRC Bulletin 342, 1-36.

5.	D.L. OLSON, Prediction of Austenite Weld Metal Microstructure and Properties, 1985, Welding Journal 64 (10), 281s-295s.

- J.M. VITEK and S.A. DAVID, 1986, welding Journal, 65 (4), 106s-111s.

- E.R. SZUMACHOWSKI and H.F. REID, Cryogenic Toughness of SMA Austenitic Stainless Steel Weld Metals, 1978, Welding Journal, 57 (11), 325s-333s.

8.	A. SCHAEFFLER, Constitution Diagram for Stainless Steel Weld Metal, 1949, Metal Progress 56, 680-680B.

9.	W.T. DELONG, Ferrite in Austenitic Weld Metal, Welding Journal, 1974, 53, 273s-286s.

10.	D.J. KOTECHI and D T.A. SIEWERT, WRC – 92 Constitution Diagram for Stainless Steel Weld Metals: a Modification of the WRC – 1988 Diagram, 1992,Welding Journal 71 (5),  171s – 178s.

11. J.M. VITEK and S.A. DAVID, The Effect of Cooling Rate on Ferrite in Type 308 Stainless Steel Weld Metal, 1988, Welding Journal,  67 (5), 95s-102s.

12. S.S. BABU, J.M. VITEK, Y.S.ISKANDER and S.A.DAVID, New Model for Prediction of Ferrite Number in Stainless Steel Welds, Science and Technology of Welding, 1997, 2 (6), 279 – 285.

- J.M. VITEK, Y.S. ISKANDER and E.M. OBLOW, Improved Ferrite Number Prediction in Stainless Steel Arc Welds using Artificial Neural Networks – Part 1: Neural Network Developemnt, Welding Journal, 2000, 79 (2), 33 – 40.

- J.M. VITEK, Y.S. ISKANDER and E.M. OBLOW, Improved Ferrite Number Prediction in Stainless Steel Arc Welds using Artificial Neural Networks – Part 2: Neural Network Developemnt, Welding Journal, 2000, 79 (2), 41 – 50.

15. H.K.D.H. BHADESHIA, Neural Networks in Materials Science, ISIJ International, 1999, 39 (10), 966-979.

- D.J.C. MACKAY: ‘Mathematical modeling of weld phenomena 3’,  H. Cerjack ed., The Institute of Materials, London, 359-389, 1997.

17. S.H. LALAM, H.K.D.H. BHADESHIA and D.J.C. MACKAY, Estimation of Mechanical Properties of Steel Welds Part 1: Yield and Tensile Strength, Science and Technology of Welding, 2000, 5 (3), 135 – 147.

- S.H. LALAM, H.K.D.H. BHADESHIA and D.J.C. MACKAY, Estimation of Mechanical Properties of Steel Welds Part 2: Elongation and Charpy toughness, Science and Technology of Welding, 2000, 5 (3), 149 – 160.

- H.K.D.H. BHADESHIA, D.J.C. MACKAY and L.E. SVENSSON, Imapct Toughness of C-Mn Steel Arc Welds – Bayesian Neural Network Analysis, Materials Science and Technology, 1995, 11 (10), 1046 –1051.

- E.A. METZBOWER, J.J.DELOACH, S.H.LALAM and H.K.D.H. BHADESHIA, Neural Network Analysis of Strength and Ductility of Welding Alloys for High Strength Low Alloy Ship building Steels, Science and Technology of Welding, 2001, 6 (2), 116 – 124.

- R.J. GRYLLS, Mechanical Properties of a High-Strength Cupronickel Alloy- Bayesian Neural Network Analysis, Materials Science and Engineering 1997, A234-236, 267-270.

- E.R. SZUMACHOWSKI and D.J. KOTECHI, Effect of Manganese on Stainless Steel Weld Metal Ferrite, Welding Journal, 1984, 63 (5), 156s-161s.

- J. WADSWORTH, J.H. WOODHEAD and SR.KEOWN, The Influence of Stoichiometry Upon Carbide Precipitation,  1976, Metal Science, 10(1), 342.

- M. VASUDEVAN, S. VENKADESAN and P.V. SIVAPRASAD, Influence of Ti/(C+6/7N) ratio on the Recrystallization Behaviour of a Cold Worked 15CR-15Ni-2.2Mo-Ti Modified Austenitic Stainless Steel, 1996, 231 (3), 231-241.

8.0 Figure Captions

Fig. 1.  Database values of each input variable vs Ferrite Number

Fig. 2. Schematic diagram of the network structure Showing the input nodes, hidden units and the output node

Fig. 3.  Characteristics of Ferrite Number model

Fig. 4. Comparison of predicted and measured ferrite number for (a) WRC – 92  database (924)  which was used in the training   (b)  our lab data (25) not used in the training,  using optimum committee models

Fig. 5.  Perceived significance w values of the first five ferrite number models for each input

Fig. 6  Error distributions(experimental FN – Predicted FN) for the complete database (924) used in the training

Fig. 7. Predicted FN vs concentration of the elements for 308 L austenitic stainless steels weld. The plot shows the variation in the ferrite number when one of the element is varied and all other concentration are held constant at the 308 L composition except Fe, which is adjusted to compensate for the varying element concentration

Fig. 8. Predicted FN vs concentration of the elements for 316 L austenitic stainless steels weld. The plot shows the variation in the ferrite number when one of the element is varied and all other concentration are held constant at the 316 L composition except Fe, which is adjusted to compensate for the varying element concentration

Figures

a C; b Mn; c Si; d Cr; e Ni; f Mo; g N; h Nb; i Ti; j Cu; k V; l Co

Fig. 1 Database values of each input variable vs Ferrite Number

Fig. 2 Schematic diagram of the network structure Showing the input nodes, hidden units and the output node

(a) noise vs hidden units ; (b) test error vs hidden units; (c) log predictive error vs hidden units; (d) test error vs models in committee; (e) predicted vs measured FN (training dataset) (f) predicted vs measured FN (test dataset)

Fig.  3 Characteristics of Ferrite Number model

Fig.  4 Comparison of predicted and measured ferrite number for (a) WRC – 92 data  base (924)  which was used in the training   (b)  our lab data (25) not used in the training,  using optimum committee models

Fig. 5 Perceived significance w values of the first five ferrite number models       for each input

Fig.6 Error distributions(experimental FN – Predicted FN) for the complete database (924) used in the training

a C; b Mn; c Si; d Cr; e Ni; f Mo; g N; h Nb; i Ti; j Cu; k V; l Co

Fig. 7 Predicted FN vs concentration of the elements for 308 L austenitic stainless steels weld. The plot shows the variation in the ferrite number when one of the elements is varied keeping all other concentrations constant for a base composition of 308 L.

a C; b Mn; c Si; d Cr; e Ni; f Mo; g N; h Nb; i Ti; j Cu; k V; l Co

Fig. 8 Predicted FN vs concentration of the elements for 316 L austenitic stainless steel welds. The plot shows the variation in the ferrite number when one of the elements is varied keeping all other concentrations constant for a base composition of 316 L.