Volume fraction & lattice constant

XRD

|  | V | Error | V | a (RT) | a (RT) | Error |
| --- | --- | --- | --- | --- | --- | --- |
| S2_HR_No4_part5 | 0.16202 |  | 0.83798 | 2.86792 | 3.61802 |  |
| S2_HR_No4_part5-r | 0.1711 |  | 0.8289 | 2.86643 | 3.61699 |  |
| ------------------------- | -------------- | -------- | --------- |  |  |  |
| S2_HR_No4_part5 | 0.1666 | 0.0064 | 0.8334 | 2.86718 | 3.61750 | 0.00072 |
| S2_HR_No4_part1 | 0.1032 | 0.0039 | 0.8968 | 2.87088 | 3.61963 | 0.00089 |

V =  0.1666  0.0064    Undeformed

V =  0.1032  0.0039    Deformed

From dilatometric :     a = 3.65118 A     at  350 °C

a  (RT) = 3.65118 [1+(25-350) exp-coeff)]

= 3.65118 [1+(25-350) 0.23251E-04]

a  (RT)   = 3.61934 A

a  (RT) = 3.61750   0.00072 (std dev)

-------------------------------------------------------------------------------------------

S2_HR_No4_part5 (Undeformed)

| Phase Name | Wt% Rietveld | Use | Wt% of Spiked | Cell Mass | Cell Vol (Å^3) |
| --- | --- | --- | --- | --- | --- |
| Iron gamma Austenite | 16.202 | 0 | 0.000 | 223.387 | 47.36003 |
| Iron alpha | 83.798 | 0 | 0.000 | 111.693 | 23.58844 |

| Phase Name | SG | a (Å) | b (Å) | c (Å) | alpha(°) | beta(°) | gamma(°) |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Iron gamma Austenite | 225 | 3.6180175 |  |  |  |  |  |
| Iron alpha | 229 | 2.8679158 |  |  |  |  |  |

Lattice parameter = 3.61801 + 3.61699

Average Lattice parameter =3.6175(0.000721 (std deviation)

-----------------------------------------------

File 1 : "C:\DIFFDATA\GIFT CML\Sangeeta\S2 HR 10March\S2_HR_No4_part5-r.raw" (Undeformed)

Range Number :  1

R-Values

Rexp : 13.82   Rwp : 17.58    Rp  : 11.09  GOF : 1.27

Rexp`: 12.68   Rwp`: 16.13    Rp` : 10.27  DW  : 1.38

Quantitative Analysis - Rietveld

Phase 1  : "Iron gamma Austenite"         17.11(11) %

Phase 2  : "Iron alpha"                   82.89(11) %

Background

One on X                                 700(3500)

Chebychev polynomial, Coefficient  0      -4(58)

1      1(31)

2      1.7(83)

3      -0.5(21)

4      0.99(53)

Instrument

Primary radius (mm)                       217.5

Secondary radius (mm)                     217.5

Corrections

Specimen displacement                     0.1574(59)

LP Factor                                 0

Structure 1

Phase name                                Iron gamma Austenite

R-Bragg                                   3.692

Spacegroup                                225

Scale                                     0.0007(28)

Cell Mass                                 223.4(18)

Cell Volume (Å^3)                         47.320(10)

Wt% - Rietveld                            17.11(11)

Crystal Linear Absorption Coeff. (1/cm)   2370(20)

Crystal Density (g/cm^3)                  7.839(63)

Preferred Orientation (Dir 1 : 1 0 0)     1

Preferred Orientation Spherical Harmonics

Order                                  8

k00                                    1

k41                                    0.081(15)

k61                                    -0.462(16)

k81                                    0.253(26)

PV_MOD peak type: a + b Tan(Th) + c / Cos(Th)

FWHM a                                 0.00(92)

b                                 0.88(57)

c                                 0.0(11)

Lorentzian mix a                       0.9(13)

b                       0.3(13)

c                       0.3(13)

Lattice parameters

a (Å)                                  3.61699(26)

Site  Np    x           y           z         Atom Occ       Beq

s1    4   0.00000     0.00000     0.00000     FE   1.000(10) 0.1

C    0.000(10) 0.1

Structure 2

Phase name                                Iron alpha

R-Bragg                                   1.905

Spacegroup                                229

Scale                                     0(250)

Cell Mass                                 111.693

Cell Volume (Å^3)                         23.5518(36)

Wt% - Rietveld                            82.89(11)

Crystal Linear Absorption Coeff. (1/cm)   2381.20(36)

Crystal Density (g/cm^3)                  7.8750(12)

Preferred Orientation (Dir 1 : 1 0 -1)    1

Preferred Orientation Spherical Harmonics

Order                                  8

k00                                    1

k41                                    0.195(56)

k61                                    0.158(39)

k81                                    -0.138(40)

PV_MOD peak type: a + b Tan(Th) + c / Cos(Th)

FWHM a                                 0.00(42)

b                                 0.87(26)

c                                 0.00(48)

Lorentzian mix a                       0.46(92)

b                       0.00(60)

c                       0.0(11)

Lattice parameters

a (Å)                                  2.86643(15)

Site  Np    x           y           z         Atom Occ       Beq

s1    2   0.00000     0.00000     0.00000     FE   1         0.5

File 1 : "C:\DIFFDATA\GIFT CML\Sangeeta\S2 HR 10March\S2_HR_No4_part1.raw" (Deformed)

Range Number :  1

R-Values

Rexp : 9.87    Rwp : 11.56    Rp  : 8.70   GOF : 1.17

Rexp`: 13.11   Rwp`: 15.34    Rp` : 11.74  DW  : 1.48

Quantitative Analysis - Rietveld

Phase 1  : "Iron gamma Austenite"         10.32(39) %

Phase 2  : "Iron alpha"                   89.68(39) %

Background

One on X                                 2900(7900)

Chebychev polynomial, Coefficient  0      30(130)

1      -7(70)

2      1(19)

3      -0.8(49)

4      5.5(12)

Instrument

Primary radius (mm)                       217.5

Secondary radius (mm)                     217.5

Corrections

Specimen displacement                     0.0243(86)

LP Factor                                 0

Structure 1

Phase name                                Iron gamma Austenite

R-Bragg                                   0.447

Spacegroup                                225

Scale                                     0.0002(11)

Cell Mass                                 214.6(92)

Cell Volume (Å^3)                         47.423(35)

Wt% - Rietveld                            10.32(39)

Crystal Linear Absorption Coeff. (1/cm)   2250(100)

Crystal Density (g/cm^3)                  7.51(32)

Preferred Orientation (Dir 1 : 1 0 0)     1(530)

Preferred Orientation Spherical Harmonics

Order                                  8

k00                                    1

k41                                    -0.517(79)

k61                                    -0.116(91)

k81                                    0.24(12)

PV_MOD peak type: a + b Tan(Th) + c / Cos(Th)

FWHM a                                 0.2(58)

b                                 1.0(36)

c                                 0.0(68)

Lorentzian mix a                       0.9(12)

b                       0.3(12)

c                       0.3(12)

Lattice parameters

a (Å)                                  3.61963(89)

Site  Np    x           y           z         Atom Occ       Beq

s1    4   0.00000     0.00000     0.00000     FE   0.950(52) 0.1

C    0.050(52) 0.1

Structure 2

Phase name                                Iron alpha

R-Bragg                                   1.116

Spacegroup                                229

Scale                                     0.007517(47)

Cell Mass                                 111.693

Cell Volume (Å^3)                         23.6616(56)

Wt% - Rietveld                            89.68(39)

Crystallite Size

Cry Size Lorentzian (nm)               280(620)

Crystal Linear Absorption Coeff. (1/cm)   2370.15(56)

Crystal Density (g/cm^3)                  7.8385(18)

Preferred Orientation (Dir 1 : 1 0 -1)    1(10000000)

Preferred Orientation Spherical Harmonics

Order                                  8

k00                                    1

k41                                    -1.22(11)

k61                                    0.819(80)

k81                                    0.717(81)

PV_MOD peak type: a + b Tan(Th) + c / Cos(Th)

FWHM a                                 0.0(10)

b                                 0.72(64)

c                                 0.0(12)

Lorentzian mix a                       0.8(22)

b                       0.0(15)

c                       0.0(26)

Lattice parameters

a (Å)                                  2.87088(22)

Site  Np    x           y           z         Atom Occ       Beq

s1    2   0.00000     0.00000     0.00000     FE   1         0.5