## Slide 1: Assignment deadline Monday
Explain in a one page essay, how an iron alloy can be designed to emulate the nickel based superalloy, containing ordered precipitates which are coherent with the matrix.
For information on nickel based alloy see:
http://www.msm.cam.ac.uk/phase-trans/2003/Superalloys/superalloys.html

## Slide 2: Interstices in Cubic-I, Cubic-F and HCP Structures
Crystallography
H. K. D. H. Bhadeshia

## Slide 4
C 62 pm Ni 126 pm Fe 124 pm Cr 130 pm
(Andrew Fairbank)

## Slide 5
silicon in iron
carbon in iron

## Slide 6
Insterstitial solid solution strengthening
(Ghosh & Olson)

## Slide 7: Cubic-I
Close-packed direction?
(Andrew Fairbank)
Ferrite

## Slide 8
radius of iron atom in ferrite

## Slide 9
octahedral interstice in ferrite
point group symmetry?
Carbon does not fit. Therefore, placing in octahedral site reduces the tetragonality of the site.

## Slide 10
Largest atom that can fit in octahedral site

## Slide 11
tertrahedral interstice in ferrite
Vector joining centres of iron and carbon?

## Slide 12: Structure projection of 4 unit cells of ferrite
What it the vector joining iron and carbon atom neighbours?
x
y

## Slide 13
structure projection

## Slide 15
3 octahedral sites per Fe
6 tetrahedral sites per Fe

## Slide 16
austenite
cubic-F

## Slide 18
octahedral interstice in austenite
point group symmetry?
Carbon does not fit. It causes uniform expansion.

## Slide 19
Largest atom that can fit in octahedral site

## Slide 20
tertrahedral interstice in austenite
Vector joining centres of iron and carbon?

## Slide 22
Insterstitial solid solution strengthening
(Ghosh & Olson)

## Slide 23
ferrite
austenite

## Slide 24: Ferrite
Carbon in “smaller” anisotropic octahedral interstices
Resulting strain is anisotropic
Strong interaction with deviatoric and dilatational strain fields of dislocations
Intense strengthening
3 octahedral and 6 tetrahedral holes per iron

## Slide 25: Austenite
carbon in larger isotropic octahedral interstices
therefore, behaves like substitutional solute with weak interactions with dislocations
mild strengthening
1 octahedral and 2 tetrahedral holes per iron

## Slide 26
(a)
BAIN
STRAIN
(c)
Body-centered
tetragonal
austenite
(d)
Body-centered
cubic martensite
a
a
a
1
2
3
b
3
b
1
b
2
(b)

## Slide 27
tetragonal martensite?