University of Cambridge

Department of Materials Science and Metallurgy

X-ray Laboratory

Hints on Calculating Powder Data and Rietveld Refinement

for determination of cell parameters, quantitative phase analysis & checking structural models

1.Introduction

The Rietveld code in the both Panalytical programs - older X'pert Plus &/or newer Highscore Plus (HS+) - is based on Wiles and Young  J.Appl.Cryst. (1981) 14 149.

(In addition, the Bruker software TOPAS is available in the X-ray lab. It has Rietveld routines based on the work of Cheary and Coelho. It is altogether more sophisticated & has proved to be a better option for refining structures of novel materials. Currently there is only limited experience in this dept of using TOPAS for Rietveld – basic principles are the same for all software)

Many users find the older software easier to use & the output is more helpful when samples maybe oriented. However, it will not read new style CIF files & there are some errors in standardising space groups – the software is no longer supported. Some people find HS+ more complicated but it is currently supported & should be error free. (Actually it is not - recently found some errors wrt  choice of origin (1 or 2, S or Z). Be v careful if there is more than 1 setting for the space group & double check both X’pert+ (usually gives warnings) & (usually no warning) HS+.  The software wants origin 2 or Z setting. If you have 1 or S, HS+ attempts a transformation, incorrectly with no error message! (Simplest thing check special positions eg 2a, 8b etc correct & calculated data looks like data in ICDD.))

When using HS+ for this type of work set the desktop to ‘Structures’

2. Simulation

The software can be used, without any experimental data, to calculate powder data from model structures (usually loaded as CIF files) eg to see the influence of structural changes such as elemental substitution & to obtain d/I data for higher angles (beyond those in the ICDD PDF2 database). Structures can be downloaded from the databases at Daresbury (see Mary). Many are already on the PCs in the lab (look for *.CIF files). Please acknowledge use of database see http://cds.dl.ac.uk/cds/acknowledge.html.

These files can then be saved (as data (*.rd, *.udf, *.xrdml) or stick (*.di) files) & plotted together so one can see how structural changes influence X-ray data.

To save data calculated from a model so you can plot them on top of each other

2.1 Simplest method - use old Xpert+ Analysis, Rietveld, Start pattern simulation

then save as *.rd or *.udf (old format - max 8 alpha numerics as file name)

2.2 in HS+ Analysis, Rietveld, Start pattern simulation

2.2.1 Save from HS+ as a scan *.xrdml or *.rd

After Analysis, Rietveld, Start pattern simulation

Open the scan list. Right click on the (calculated) scan and select Convert  Calc Profile to obs Profile

File, save as *.XRDML or *.RD.

Sometimes just copying the peak list (deleting alpha2 peaks) & pasting it into say EXCEL is useful (but not so handy for comparisons)

2.2.2 After Analysis, Rietveld, Start pattern simulation

Save as *.di which can then be opened in HS+ (Note *.di can only be ‘opened’ not ‘inserted’ so only 1 per plot, but once opened as *.di can be saved as *.rd or *.xrdml & then several calculated data sets plotted on 1 graph)

3. Rietveld refinement (for quantitative phase analysis & cell parameters)

You must start by putting in good quality experimental data and reasonable models (see 2 for info on CIF files), ie you should have identified all the phases. (Check that there is a number for B eq. or B overall - the thermal displacement parameter. Should be ~0.5 for metals & inorganic structures with diffraction data above 100 2 & ~5.0 for organic structures where the intensity is ~0 above ~ 60 2) There are several helpful papers (see references) & the algorithms are described in the help facility.

Use

Strongly recommend that you use the software in 'semi-automatic' mode. (You will lose control of the refinement in fully automatic and manual is a lot of extra work) With HS+ suggest using the desktop ‘Structures’ – bottom of the screen in the middle.

  - Load or insert raw data *.xrdml for HS+, *.rd or *.udf for Xpert Plus, and/or insert *.cif. (With *.cif only you can calculate/simulated XRD data (sse 2), with cif & raw can do Rietveld refinement, raw data only can do some cell parameter refinement)

  - Refine ( √  tick box)1-3 background parameters (global) + the scale factor for each phase

  - Refine specimen displacement or zero point error (zero shift) or in HS+ (never both zero & displacement) and all refineable cell parameters (ie for cubic only a). It is more likely there will be a small error in sample height (~+/-0.02mm) than zero of the diffractometer. (If peaks very broad, can help to set w~0.1or 0.2 here instead of the std start  value 0.01, but do not refine (fit) profile widths until peak positions approx correct)

  - If required refine more background parameters – check to see that it looks sensible. Look at graphs, particularly difference plot and follow nos such R and GOF for problems & improvements. They should decrease as fit improves. In general once parameters refined, leave √ unless problems start to occur

3.5 Refine profile parameters - most tricky part  FWHM2   w + v tan + u tan2

First just w, then fix      (ie remove tick) w and refine u or v. Fix them and refine w again. When things look OK refine w and either u or v. It is rarely possible to refine both u and v - these parameters are highly correlated. They must not go -ve. It is nonsense.

Again if peaks are very broad the standard settings may not calculate the profile out far enough so change the profile base width from ~5 to ~20 – (refinement control, global parameters, refinement, profile base width)

3.6. Refining one (or more) peak shape parameter can sometimes improve the profile fit. It alters the ratio of Lorenztian to Gaussian in a pseudo-Voigt function (for G & L gamma = 0 & 1 respectively - do not allow >1 or <0). One parameter keeps this ratio fixed, more than one allows it to vary with 2

  - Finally check to see if sample oriented (eg 00ls all strong and hk0s all weak). Work out vector and refine orientation parameter

  - Sometimes refining Bs helps – I usually fix all similar atoms to have same B (0.1<B<10)

  - If fit poor, consider changing model, refining occupancy etc. Have you correctly identified all the phases? Could there be an over-illumination error? Check that all parameters look sensible.

Remember that some parameters are highly correlated eg background, peak widths/shapes, Bs and scale factors (ie amount of each phase). If problems continue fix some parameters to a sensible value, refine others & then refine all. That is to try and force the refinement. It is possible to exclude small regions with unidentified peaks (then you get a ratio A:B rather than wt%A & wt%B). This is not ideal just a temporary fix. Should aim to identify all crystalline phases.

  - You can end up in a situation where different models give equally good fits to the data (difference plots, Rs, GOF etc). This is then your uncertainty – the data cannot tell the difference between these different models (maybe need better quality data)

  - Refinement of atomic positions requires higher quality data & a lot of care!

Mary Vickers November 2001

Updated April 2005, Sept 07, Feb09, July09

References

R A Young et al. 'The Rietveld Method' Int.Union of Crystallography Monograph no5 (1993) OUP NbA 78

Int.Union of Crystallography reports

L McCusker et al  J. Appl. Cryst. (1999) 25 36-50 'Rietveld Refinement Guidelines'

I C Madsen, N V Y Scarlett, L M D Cranswick and T Lwin J. Appl. Cryst. (2001) 34 409-426 'Outcomes of the International Union of Crystallography Commission on Powder Diffraction Round Robin on Quantitative Phase Analysis: samples 1a to 1h'

R J Hill J Appl Cryst (1992) 27 589-610 'Rietveld Round Robin I'

R J Hill & L M D Cranswick J Appl Cryst (1994) 27 803-844 'Rietveld Round Robin II'

D Balzar, N Audebrand, M R Daymond, A Fitch, A Hewat, J I Langford, A Le Bail, D Louër, O Masson, C N McCowan, N C Popa, P W Stephens and B H Toby 'Size-strain line-broadening analysis of the ceria IUCr Round Robin sample' J Appl Cryst (2004) 37 911-924

Some of these papers are in the red file in the XRD lab.

This website/user group can be helpful

http://ccp14.sims.nrc.ca/ccp/ccp14/ftp-mirror/howardflack/pub/soft/crystal/stxnews/riet/intro.htm