Figure 1. Bright field image and associated Ni jump ratio map. Brighter areas correspond to higher Ni contents.

Figure 2. STEM annular dark-field (ADF) image with the area EDX mapped outlines (box 1). Box 2 corresponds to drift correction reference area.

Figure 3. EDX-mapped area.

Figure 4. Integrated EDX spectrum from box 1 above.

Peak       	Intensity        	Uncertainty

Cr-K         	1149.800         330.069

Cr-L          	981.207         	280.243

Fe-K         	7666.589         851.730

Fe-L         	2055.759         559.561

Co-K          	783.511         	315.703

Co-L          	640.716         	427.611

Ni-K         	1017.100        	314.981

Ni-L          	478.597         	281.476

Mo-K           	99.105          	93.204

Mo-L          	159.578         	114.375

W-L            	32.003          	66.467

W-M            	47.209          	58.020

Element	Weight %    	Atomic %    Uncertainty %    Correction    k-Factor

Cr(K)        	9.641      	10.572         0.276           0.991        1.376

Fe(K)       	69.141      	70.589         0.768           0.994        1.480

Co(K)        	7.524       	7.279         0.303           0.995        1.576

Ni(K)        	9.869       	9.586         0.305           0.996        1.592

Mo(K)        	2.766       	1.643         0.260           0.998        4.581

W(L)         	1.056       	0.327         0.219           0.752        5.419

Figure 5. EDX mapped area with analysed area outlined.

Figire 6. Integrated EDX spectrum from box 1 above.

Peak        Intensity        Uncertainty

Cr-K          683.137         256.867

Cr-L          336.325         196.511

Fe-K         4892.930         680.523

Fe-L         1407.530         382.302

Co-K          455.796         258.952

Co-L          519.723         284.426

Ni-K          671.487         231.758

Ni-L          387.844         202.497

Mo-K          110.419          78.085

Mo-L          105.783          83.351

W-L             9.534          57.540

W-M            80.405          60.233

Element    Weight %    Atomic %    Uncertainty %    Correction    k-Factor

Cr(K)        8.930       9.841         0.335           0.991        1.376

Fe(K)       68.792      70.584         0.956           0.994        1.480

Co(K)        6.824       6.635         0.387           0.995        1.576

Ni(K)       10.157       9.915         0.350           0.996        1.592

Mo(K)        4.804       2.869         0.339           0.998        4.581

W(L)         0.490       0.152         0.296           0.752        5.419

Figure 7. EDX area mapped with precipitate analysed.

Figure 8. Integrated spectrum from box 1 above.

Peak        Intensity        Uncertainty

Cr-K         1041.950         313.854

Cr-L          450.405         189.574

Fe-K         6860.620         801.821

Fe-L         1918.920         422.787

Co-K          863.499         302.670

Co-L          788.259         296.122

Ni-K          269.512         184.259

Ni-L          207.117         165.040

Mo-K         1973.790         374.692

Mo-L         2301.380         424.038

W-L          1360.650         287.345

W-M          1933.000         404.095

Element    Weight %    Atomic %    Uncertainty %    Correction    k-Factor

Cr(K)        4.813       7.370         0.145           0.991        1.376

Fe(K)       34.085      48.597         0.398           0.994        1.480

Co(K)        4.568       6.172         0.160           0.995        1.576

Ni(K)        1.440       1.954         0.098           0.996        1.592

Mo(K)       30.348      25.187         0.576           0.998        4.581

W(L)        24.743      10.716         0.522           0.752        5.419