## Slide 1: Multiple, simultaneous, martensitic transformations transformation texture intensities
www.msm.cam.ac.uk/phase-trans

## Slide 2
single start-temperature
multiple start-temperatures
Causes:
stress-affected
strain-affected
external fields

## Slide 3
Multitude of start temperatures
How does the overall volume fraction evolve?
Definition of variant: unique start temperature
How does the fraction of each variant evolve?
How does texture intensity depend on this?
Mixture of alpha and epsilon martensite?

## Slide 6
c
r
habit plane
orientation relationship
deformation

## Slide 8
random to non-random transition
random texture in austenite
random ferrite texture
non-random ferrite texture

## Slide 10
No method calculates INTENSITY, only POSITIONS of poles

## Slide 12
Kinetics of martensite
Koistinen and Marburger (1959)

## Slide 15
Each of 24 variants in a given austenite grain will have a different martensite-start temperature

## Slide 16
time = t
time = t+∆t
a

## Slide 17
time = t
time = t+∆t
a
b

## Slide 19
Distribution of volume fractions broader at large stress

## Slide 22
Estimate volume fractions of variants with different martensite-start temperatures.
Allows intensity in textures to be calculated.
Can be generalised to any scenario which introduces differences in martensite-start temperatures.
stress,
magnetic field,
non-uniform cooling,
mixed alpha and epsilon.