## Slide 1
7 and 8-03-2013
Thin foil K10
Steel (Fe-0.78C-2.02Mn-1.01Cr-1.6Si-1.37Al-3.83Co-0.25Mo) (wt.%)
Austenitized at 950°C, 30min, argon –Isothermal holding at 250°C, 16h – Homogeneization
Electropolishing
32V – 39-42mA - flow rate=16 - T=-34°C
Solution: 80% methanol+15% glycerol+5% perchloric acid
Big particles
Very magnetic sample
100 nm
300 nm
Dust?
?

## Slide 2
7 and 8-03-2013
Thin foil K10
Steel (Fe-0.78C-2.02Mn-1.01Cr-1.6Si-1.37Al-3.83Co-0.25Mo) (wt.%)
Austenitized at 950°C, 30min, argon –Isothermal holding at 250°C, 16h – Homogeneization
Electropolishing
32V – 39-42mA - flow rate=16 - T=-34°C
Solution: 80% methanol+15% glycerol+5% perchloric acid
100 nm
100 nm

## Slide 3
7 and 8-03-2013
Thin foil K10
Steel (Fe-0.78C-2.02Mn-1.01Cr-1.6Si-1.37Al-3.83Co-0.25Mo) (wt.%)
Austenitized at 950°C, 30min, argon –Isothermal holding at 250°C, 16h – Homogeneization
Electropolishing
32V – 39-42mA - flow rate=16 - T=-34°C
Solution: 80% methanol+15% glycerol+5% perchloric acid
4s
2.8s
100 nm
100 nm
100 nm

## Slide 4
100 nm
100 nm
100 nm
100 nm
Red and yellow lattices: [111] zone axis of bainitic ferrite
(same angles as theroretical ones and same ratios of distances: 1-1-1.73)
Green lattice: [110] zone axis of austenite
(same angles as theoretical ones and ratios of distances of 1.08-1.67 and 1.80 vs. 1.15-1.66 and 1.91 for theoretical ones)

## Slide 5
[1-10]
[10-1]
[01-1]
[-110]
[-101]
[0-11]
[10-1]
[1-10]
[0-11]
[-101]
[-101]
[01-1]
[00-2]
[1-1-1]
[-11-1]
[-111]
[002]
[1-11]



















## Slide 6
100 nm
300 nm
300 nm
Yellow lattice: [112] zone axis of M23C6
For Mn23C6 (same angles as theroretical ones and ratios of distances: 1.2-171-2.07 vs. 1.17-1.638-1.92 for theoretical ones)
[112] zone axis of Cr23C6 could also match.