## Slide 1
Many small precipitates (carbides?) at the interfaces of the subunits in bainitic sheaves
21-02-2013
Thin foil N9
Steel (Fe-0.78C-2.02Mn-1.01Cr-1.6Si-1.37Al-3.83Co-0.25Mo) (wt.%)
Austenitized at 950°C, 30min, argon –Isothermal holding at 250°C, 16h – Tempered at 500°C, 1 day
100 nm
200 nm
Electropolishing
22.5V - 28mA - flow rate=16 - T=-17.7°C
Solution: 80% methanol+15% glycerol+5% perchloric acid
In a normal direction to the length of the plate : LT=t/2 with LT : ’mean lineal intercept’and t: true thickness of the plate
According to
Acceleration of low temperature bainite
C. Garcia-Mateo, F.G. Caballero, H.K.D.H. Bhadeshia
ISIJ International 43(11) (2003) 1821-1825
Thickness of the plates
t  100nm
100 nm
100 nm

## Slide 2
100 nm
untempered
tempered
a
b