Table 5: Average (*Ra*) and root mean squared (*Rq*) surface roughness magnitudes and standard error based on five measurements for each RCF specimen.

|  |  |  |
| --- | --- | --- |
| Sample | *Ra* / µm | *Rq* / µm |
| Control | 0.08±0.02 | 0.13±0.04 |
| SC | 0.06±0.01 | 0.08±0.01 |
| MPC | 0.06±0.01 | 0.08±0.01 |