## Slide 1: Model Validation
<number>
Retreating side
Advancing side
Welding direction
Shoulder
Tool Pin
Joint
Nanda, Roy, Lienert and DebRoy, Acta Mat, 2007

## Slide 2: Temperature contour and velocity distribution
<number>
Temperature in K
1018 Steel
900 rpm, 0.42 mm/s
The longitudinal sections are taken just outside the pin surface

## Slide 3
<number>
Temperature in K
1018 Steel
900 rpm, 2.1 mm/s
The longitudinal sections are taken just outside the pin surface
Temperature contour and velocity distribution

## Slide 4
<number>
The transverse sections are taken just in front of the pin surface
Temperature contour and velocity distribution
1018 Steel, 900 rpm, 0.42 mm/s
Advancing Side
Retreating Side
1018 Steel, 900 rpm, 2.1 mm/s
Advancing Side
Retreating Side

## Slide 5: Steady state temperature profiles
1018 Steel, 900 rpm, 2.10 mm/s
<number>
Temperature in K
1018 Steel, 900 rpm, 0.42 mm/s

## Slide 6: Steady state temperature profiles
1018 Steel, 300 rpm, 2.10 mm/s
<number>
Temperature in K
1018 Steel, 450 rpm, 2.10 mm/s

## Slide 7: Steady state temperature profiles
1018 Steel, 600 rpm, 2.10 mm/s
<number>
Temperature in K
1018 Steel, 750 rpm, 2.10 mm/s

## Slide 8: Steady state temperature profiles
1018 Steel, 600 rpm, 1.05 mm/s
<number>
Temperature in K
1018 Steel, 450 rpm, 1.05 mm/s

## Slide 9: Steady state temperature profiles
1018 Steel, 900 rpm, 1.05 mm/s
<number>
Temperature in K
1018 Steel, 750 rpm, 1.05 mm/s

## Slide 10: Steady state temperature profiles
1018 Steel, 300 rpm, 1.05 mm/s
<number>
Temperature in K
1018 Steel, 300 rpm, 0.42 mm/s

## Slide 11: Steady state temperature profiles
1018 Steel, 450 rpm, 0.42 mm/s
<number>
Temperature in K
1018 Steel, 600 rpm, 0.42 mm/s

## Slide 12: Steady state temperature profiles
1018 Steel, 750 rpm, 0.42 mm/s
<number>
Temperature in K
1018 Steel, 900 rpm, 0.42 mm/s

## Slide 13: Computed Thermal Cycles
<number>
Thermal cycles at top, mid-plane and pin bottom in five different rotational speeds at a welding speed of 2.10 mm/s

## Slide 14: Computed Thermal Cycles
<number>
Thermal cycles at top, mid-plane and pin bottom in five different rotational speeds at a welding speed of 1.05 mm/s

## Slide 15: Computed Thermal Cycles
<number>
Thermal cycles at top, mid-plane and pin bottom in five different rotational speeds at a welding speed of 0.42 mm/s

## Slide 16: Computed Thermal Cycles
<number>
Thermal cycles at top surface in three different welding speeds at five rotational speeds.