## Slide 1
Iso-viscocity contours showing locations of thermal cycles
Workpiece: 6.35 mm thick 1018 Steel
Tool Shoulder Diameter: 15 mm
Pin Diameter: 7.90 mm (straight circular)
Pin Length: 6.22 mm
Rotational Speed: 450 rpm
Welding Speed: 0.42 mm/s
Point | Height (mm) | Transverse distance from joint interface (mm)
A | 6.35 | - 9.50 (advancing side)
B | 6.35 | - 8.00 (advancing side)
C | 6.35 | - 4.00 (advancing side)
D | 6.35 | 0 (tool center)
E | 6.35 | 4.00 (retreating side)
F | 6.35 | 8.00 (retreating side)
G | 6.35 | 9.50 (retreating side)
H | 6.35 | 12.70 (retreating side)
L | 3.78 | - 6.00 (advancing side)
M | 3.78 | - 4.25 (advancing side)
N | 3.78 | 4.25 (retreating side)
O | 3.78 | 6.00 (retreating side)
P | 0.60 | - 4.90 (advancing side)
Q | 0.60 | - 4.25 (advancing side)
R | 0.60 | 4.25 (retreating side)
S | 0.60 | 4.90 (retreating side)