## Slide 1
Introduction and point groups
Stereographic projections
Low symmetry systems
Space groups
Reciprocal Lattice & Diffraction
Deformation and texture
Interfaces, orientation relationships
Martensitic transformations
Crystallography
H. K. D. H. Bhadeshia

## Slide 2
can form at incredibly
low temperatures
can form very rapidly
no composition change
Diffusionless

## Slide 3
shape

## Slide 5
Irrational: why?

## Slide 7
Orientation relationships: irrational

## Slide 10
Glissile interface cannot contain more than one set of dislocations.
Martensitic transformation only possible if deformation which changes the parent into the product leaves one line undistorted and unrotated, i.e. an invariant-line.
Deformation is an invariant-line strain.

## Slide 16
d
s
1
s
1
d
1
uniaxial dilatation
simple shear
general invariant-plane strain
s=0.26
d=0.03

## Slide 17
c
r
d
s
1
Christian, 1957

## Slide 20
The Bain strain

## Slide 21
[100]
[001]
o
a
a'
b
b'
o
b'
b
a,a'
(a)
(b)

## Slide 23
Austenite
(a)
w
x
y
z
Twinned
Martensite
Twin
Boundary
Correct macroscopic shape, correct structure
x
w
z
y
z
Slipped
Martensite
LATTICE
-INVARIANT
DEFORMATION
x
w
y
Observed
shape,
wrong
structure
P
(b)
w
x
z
y
1
RB
(c)
x
w
z
y
P
2
Martensite
(wrong
shape)

## Slide 25
transformation twins (Wayman)