## Slide 1
Hydrogen in complex microstructures in steels
www.msm.cam.ac.uk/phase-trans

## Slide 2: Facts
Hydrogen dissolves in ferrite, austenite
Okamoto:2004

## Slide 3: Facts
Hydrogen embrittles iron
both single and polycrystalline forms
Pfeil 1926
normal
pickled
W. H. Johnson: ‘On some remarkable changes produced in iron and steel by the action of hydrogen and acids’, Proceedings of the Royal Society of London, 1875, 23, 168–179.

## Slide 4: Facts
It is diffusible hydrogen that embrittles
it is atomic hydrogen that embrittles
submerging H-containing steel causes frothing
stronger steel more susceptible
W. H. Johnson: ‘On some remarkable changes produced in iron and steel by the action of hydrogen and acids’, Proceedings of the Royal Society of London, 1875, 23, 168–179.

## Slide 5: Facts
Hobson, 1951

## Slide 6: Facts
Tendency to embrittle scales with strength
Hobson & Sykes, 1951
or does it in fact scale with ductility in the absence of hydrogen?

## Slide 7: Facts
Frohmberg, 1954

## Slide 8: Facts
hydrogen diffuses faster in ferrite, but there are complications
Coe, 1973

## Slide 9: Mechanisms
Reduction in surface energy of iron, making it easier to cleave (Oriani, 1960)
Song, Bhadeshia, Suh 2013

## Slide 10
Song, Bhadeshia, Suh 2013

## Slide 11: Mechanisms
Accumulation of internal stress due to diffusible hydrogen precipitating at defects (Zapffe, 1941)

## Slide 12: Mechanisms
Hydrogen enhanced plastic instability
increased dislocation mobility due to H segregation
microscopically ductile fracture
requires a heterogeneous distribution of hydrogen

## Slide 13: Mechanisms
Hydrogen enhances vacancy concentrations
vacancies agglomerate
enhances ductile nucleation and linking of cracks
Terasaki et al. 1998

## Slide 14: Facts: summary
All evidence points to easily diffusible or
weakly trapped hydrogen embrittles
Trapped molecular hydrogen irrelevant
Strongly trapped hydrogen irrelevant

## Slide 17
Hydrogen

## Slide 18
Yamasaki and Bhadeshia, 2006

## Slide 20
Song, Bhadeshia, Suh, 2013

## Slide 21: Composition following transformation

## Slide 23
200 Å
g
g
a
a
a
Caballero, Mateo, Bhadeshia

## Slide 25
Sherif, 2005, Ph.D. thesis, Cambridge

## Slide 26
Above percolation threshold
Below percolation threshold

## Slide 27
Geometrical percolation threshold of overlapping ellipsoids

## Slide 29
Fielding, Song, Han, Bhadeshia, Suh, unpublished

## Slide 30
Fielding, Song, Bhadeshia, Suh, unpublished

## Slide 33
Ryu, Chun, Lee, Bhadeshia, Suh, 2012

## Slide 34
Hydrogen embrittlement of austenite
B. C. De Cooman, O. Kwon and K.-G. Chin,
Materials Science & Technology, 2012

## Slide 35
Hydrogen embrittlement of austenite

## Slide 36
Hydrogen embrittlement of austenite
Fe-0.6C-18Mn wt% Fe-0.6C-18Mn-1.5Al
Ryu, Kim, Lee, Suh, Bhadeshia, 2012

## Slide 37
Hydrogen embrittlement of austenite
Ryu, Kim, Lee, Suh, Bhadeshia, 2012
Combination of inter- and trans-granular fracture

## Slide 38
Hydrogen embrittlement of austenite
Ryu, Kim, Lee, Suh, Bhadeshia, 2012

## Slide 39
Hydrogen embrittlement of austenite

## Slide 43
Methods for mitigating consequences of hydrogen
Provide traps for infused hydrogen
Retard the infusion of hydrogen
Must not compromise other properties
Ferritic
Control stacking fault energy
Control phase transformations
Austenitic

## Slide 44
Open questions:
How much hydrogen will enter steel over service life?
Any long-term ex-service samples that we can test for hydrogen content?
Can void formation at stress concentrations be observed directly using “large facilities”?
How can we suppress enhanced vacancy generation due to H?