## Slide 1: Very short and very long heat treatments in the processing of steels
www.msm.cam.ac.uk/phase-trans

## Slide 2
purpose of heat treatment is to move atoms

## Slide 6
allotriomorphic
ferrite
pearlite
Reconstructive
transformations

## Slide 7
structural scale
homogenisation

## Slide 10
Widmanstaetten ferrite
martensite
Displacive
transformations
bainite

## Slide 11
Gary Cola and the 80 ms heat treatment

## Slide 12
Image courtesy of Gary Cola

## Slide 13
Lola et al. (2009)

## Slide 15
before
after
Lolla et al. (2009)

## Slide 16
before
after

## Slide 17
Key component of car safety

## Slide 18
Key component of car safety

## Slide 20
20

## Slide 21
Notes: 21
21

## Slide 22
Yates, Jerath, Bhadeshia
Notes: 22
22

## Slide 23
Yates, Jerath
Notes: 23
23

## Slide 24
Photograph courtesy of V. Jerath
Carbide-free bainite in Eurotunnel
Notes: 24
24

## Slide 25
Custom design

## Slide 26
Continuous annealing strip production line

## Slide 27
Galvanising bath

## Slide 28
carbide-free bainitic steel

## Slide 29
carbide-free bainitic steel

## Slide 30
carbide-free bainitic steel

## Slide 31
Papadimitriou and Fourlaris, 1997

## Slide 32
…. bulk nanocrystalline steel which is very strong, tough, cheap ….

## Slide 33
Calculated data Fe-2Si-3Mn-C wt%

## Slide 34
Calculated data Fe-2Si-3Mn-C wt%

## Slide 40
Paul Davies, Tata Steel
Notes: 40

## Slide 41
“more serious battlefield threats”
Notes: 41

## Slide 42
ballistic mass efficiency
consider unit area of armour
Notes: 42

## Slide 43
Notes: 43

## Slide 45
Fang, Yang, Liu, Song, Fang, Bhadeshia, Materials and Design, 50 (2013) 38
Cannot easily be welded

## Slide 46
What next?
Steel with impossible combination of properties
>2 GPa
30% ductility at conventional strain rates
ductility at very high strain rate
toughness and Charpy impact at -40°C
weldable
cheap, large in all dimensions
mass production
high-temperature capability
www.msm.cam.ac.uk/phase-trans

## Slide 47: Composition following transformation

## Slide 48
Bhadeshia, Met. Sci. (1982)

## Slide 50
Austenite
Ferrite
Dislocation
Francisca Garcia Caballero
Caballero, Miller, Mateo, Cornide. J. Alloys & Compounds, (2012)
Large carbon concentration in solution in ferrite

## Slide 51
Caballero, Miller, Mateo, Cornide
J. Alloys & Compounds, (2012)
atom probe data for carbon in solid solution in ferrite in contact with austenite

## Slide 52
A diffusionless transformation will necessarily lead to a body-centred tetragonal ferrite.

## Slide 53
Huge increase in solubility; ferrite with tetragonal symmetry
Jang, Suh, Bhadeshia, Scr. Mat. 68 (2012) 195

## Slide 54
C. N. Hulme-Smith, I. Lonardelli,
A. C. Dippel and H. K. D. H. Bhadeshia, Scr. Mat. 69 (2013) 409.

## Slide 55
C. N. Hulme-Smith,
I. Lonardelli,
C. Dippel
H. K. D. H. Bhadeshia, Scr. Mat. 69 (2013) 409.

## Slide 56
Chatterjee & Bhadeshia, 2004
Fe-1.75C-Si-Mn wt%
2104