## Slide 1: Strength of strong materials: graphene, spider’s silk and steel
www.msm.cam.ac.uk/phase-trans

## Slide 2: Purpose
Focus on structural materials and how to assess them.
Study two incredibly successful materials
Study one new material

## Slide 3
Graphene
200 times
stronger than
steel
immensely
tough

## Slide 4
500 MPa
3000 MPa
1500 MPa

## Slide 7
Total: 1.4 billion tonnes per annum

## Slide 9
Li et al. 1993

## Slide 10: Design a new bearing steel

## Slide 11
ideal strength?

## Slide 12: BCC iron weakest along <100>
Clatterbuck et al.
Phil. Mag. Lett.
2002

## Slide 13
The Bain strain

## Slide 14: What is the maximum strength of iron when pulled along its weakest direction?
remember this number
14.5 GPa

## Slide 15
Brenner:1956
Single crystals of iron

## Slide 16
Commercial alloy made by Kobe Steel

## Slide 18
1 Denier: weight in grams, of 9 km of fibre
50-10 Denier
Scifer is 9 Denier

## Slide 19
Claimed strength of carbon nanotube is 130 GPa
Edwards, Acta Astronautica, 2000
Claimed modulus is 1.2 TPa
Terrones et al., Phil. Trans. Roy. Soc., 2004

## Slide 20: How is the strength of nanotube calculated?
By ignoring the empty space within the nanotube
Therefore strength of steel, which has 32% space unoccupied, is greater by 47% than reported since time zero
But let us ignore this

## Slide 21
36000 km
tethered space elevator

## Slide 22
strength 130 GPa
modulus 1.2 TPa
 | J g-1 | m s-1
Dynamite | 4650 | 6000
Nanotube | 5420 | 21500

## Slide 23
data from Pan et al. 1999, Yu et al. 2000

## Slide 24
An equilibrium number of defects.
Strength of a nanotube rope 2 mm long is less than 2000 MPa

## Slide 25
Strength produced by deformation limits shape: wires, sheets...
Strength in small particles relies on perfection. Doomed as size increases.
Summary

## Slide 26
Morinobu Endo, 2004

## Slide 27: What is graphene?
single-atom thick sheet (Carbon 65 [2013] 1-6)

## Slide 28
Lee et al. Science (2008)
reported breaking strength
of 130 GPa for sample
about 2 µm square of
pristine graphene

## Slide 29
Han et al.
Nanoscale
7 (2015) 15672

## Slide 30
Han et al.
Nanoscale
7 (2015) 15672
Polycrystalline graphene is brittle under homogeneous tensile stress

## Slide 31
immensely
tough

## Slide 32: Intrinsic strength of Graphene (samples 2 µm2)

## Slide 33
Graphene
200 times
stronger than
steel

## Slide 34
Stone-Wales defects
Vacancy

## Slide 35
Yazyev et al. Phys. Rev. B 81 (2010) 195420

## Slide 36
Kobayashi et al.
APL 102 (2014)
023112

## Slide 37: Graphene in composites
Zhao et al.
Macromolecules
43 (2010) 2357

## Slide 38: Spider’s silk

## Slide 39
http://creativecommons.org/licenses/by-sa/3.0

## Slide 40: Spider’s silk
Tensile strength 700 MPa
Density 1.3 g cm-3
“Specific strength 6 times greater than steel of identical tensile strength”

## Slide 41: Spider’s silk
Tensile strength 700 MPa
Density 1.3 g cm-3
Specific strength 5.38 MPa g-1 cm3
“Specific strength 6 times greater than steel of identical tensile strength”
Tensile strength of Scifer 5500 MPa
Density 7.8 g cm-3
Specific strength 7.05 MPa g-1 cm3
Steel has a greater specific strength for same diameter as the silk

## Slide 42: Spider’s silk
700 MPa, 30% elongation gives “toughness” of 105 MJ m-3
Spider’s silk is therefore “tougher than steel”
Physics Education
43 (2008) 57

## Slide 43: Twinning induced plasticity
TWIP steel on similar calculation has a toughness of 500 MJ m-3

## Slide 44: Conclusions
Graphene is at best ten times stronger than steel at the micrometre level
No evidence that the strength of graphene is sustained as the size is increased
Graphene is a brittle material

## Slide 45
With metallic bonding, the cohesion between atoms is maintained even when atoms
are translated along long distances.
Therefore, plasticity, energy absorption, safe design.
Covalent C-C bonds once broken remain broken.
Therefore, plastic deformation is absent when covalent bonds are stretched.
Therefore, limited energy absorption. Brittle.
Not safe in engineering design.

## Slide 47: Graphene is a two-dimensional material
Cannot make bicycle frame from graphene
about 3500 Pa

## Slide 48: Conclusions
Spider’s silk is excellent for webs
Spider’s silk is not stronger than steel when considering specific strength or absolute strength
Spider’s silk is not tougher than steel
Low density steels

## Slide 49
Low-density steels
lattice expansion
lower atomic mass of
substitutional atom
● Specific weight of
Fe-Al alloy
■ Specific weight of
Fe-14~28Mn-Al-C [Frommeyer]
Al : 26.98 g/mol
Fe: 55.85 g/mol
(M. Shiga et al. J. Phy. Soc. J.)

## Slide 50
Total: 1.4 billion tonnes per annum

## Slide 51
Fe-10Al-15Mn-5Ni-0.8C wt%
strengthened by fine FeAl precipitates
Density 17% lower than iron
Nature 518 (2015) 77-79, by S.-H. Kim, H. Kim and N. J. Kim,

## Slide 52
Xiong et al. Mat. Sci. Techn. (2016)

## Slide 53
An invention of a new material should not rely on just one property.
Avoid deliberate attempts to mislead the general audience.
“there is much work between measuring a single attractive property in a single alloy to demonstrating credibility for a particular application”
Dan Miracle, Materials Science and Technology (2015)