## Slide 1
Design of advanced steels
www.msm.cam.ac.uk/phase-trans

## Slide 2
electron theory
molecular dynamics
thermodynamics
kinetics
irreversible thermodynamics
finite elements
structure-properties
uncertainties

## Slide 4
Charpy
fatigue
corrosion
tensile
critical stress intensity

## Slide 6
an apple weighs
1 Newton
1 m
= 1 Pa

## Slide 7
Pure iron, Brenner (1956)

## Slide 8
Scifer, 5.5 GPa and ductile
Kobe Steel

## Slide 11
1 Denier: weight in grams, of 9 km of fibre
50-10 Denier
Scifer is 9 Denier

## Slide 12
Claimed strength of carbon nanotube is 130 GPa
Edwards, Acta Astronautica, 2000
Claimed modulus is 1.2 TPa
Terrones et al., Phil. Trans. Roy. Soc., 2004

## Slide 13
carbon nanotubes and graphene fundmentally
unsuitable for structural applications

## Slide 14
strength 130 GPa
modulus 1.2 TPa
 | J g-1 | m s-1
Dynamite | 4650 | 6000
Nanotube | 5420 | 21500

## Slide 15
Strength produced by deformation limits shape: wires, sheets...
Strength in small particles relies on perfection. Doomed as size increases.
Summary

## Slide 16
…. bulk nanocrystalline steel which is very strong, tough, cheap ….

## Slide 17
Fine crystals by transformation
Introduce work-hardening capacity
Need to store the heat of transformation
Reduce rate of transformation
Transform at low temperature

## Slide 20
Swallow and Bhadeshia, 1996

## Slide 22
22

## Slide 25
wt%
Low transformation temperature
Bainitic hardenability
Reasonable transformation time
Elimination of cementite
Austenite grain size control
Avoidance of temper embrittlement

## Slide 26
Cooking temperature?
180 to 220 °C

## Slide 28
200 Å
g
g
a
a
a
Very strong
Huge uniform ductility
No deformation
No rapid cooling
No residual stresses
Cheap
Uniform in very large sections

## Slide 29
2300-2500 MPa, up to 27% uniform elongation, about 40 MPa m1/2

## Slide 30
Above percolation threshold
Below percolation threshold

## Slide 31
Fielding, Song, Han, Bhadeshia, Suh, Proc. Roy. Soc. A, 2014

## Slide 32
ballistic mass efficiency
consider unit area of armour

## Slide 36
36

## Slide 38: Exceptional alloys of iron

## Slide 39
Notes: 39

## Slide 40: Composition following transformation

## Slide 41
Bhadeshia, Met. Sci. (1982)

## Slide 43
It was assumed therefore, that these carbon atoms are trapped at dislocations, since the original paper published in 1981.
Bhadeshia, Edmonds
Metall. Trans. (1979)

## Slide 44
Austenite
Ferrite
Dislocation
Francisca Garcia Caballero
Caballero, Miller, Mateo, Cornide. J. Alloys & Compounds, (2012)
Large carbon concentration in solution in ferrite

## Slide 45
Caballero, Miller, Mateo, Cornide
J. Alloys & Compounds, (2012)
atom probe data for carbon in solid solution in ferrite in contact with austenite

## Slide 46
A diffusionless transformation will necessarily lead to a body-centred tetragonal ferrite.

## Slide 47
Huge increase in solubility; ferrite with tetragonal symmetry
Jang, Suh, Bhadeshia, Scr. Mat. 68 (2012) 195

## Slide 48
C. N. Hulme-Smith, I. Lonardelli,
A. C. Dippel and H. K. D. H. Bhadeshia, Scr. Mat. 69 (2013) 409.

## Slide 50
Fang, Yang, Liu, Song, Fang, Bhadeshia, Materials and Design, 50 (2013) 38
Cannot easily be welded

## Slide 51
What next?
Steel with impossible combination of properties
>2 GPa
30% ductility at conventional strain rates
ductility at very high strain rate
toughness and Charpy impact at -40°C
weldable
cheap, large in all dimensions
mass production
high-temperature capability
Mathew Peet

## Slide 54
Pous et al. (2014)
Kelvin tetrakaidecahedron

## Slide 59
Two pass
12 mm
Single pass

## Slide 60: High speed video
V0 = 445 m s-1
Survival
Vickram Deshpande, Mathew Peet

## Slide 61
61

## Slide 62
Chatterjee & Bhadeshia, 2004
Fe-1.75C-Si-Mn wt%
2104