## Slide 1
Evolution of solutions
www.phase-trans.msm.cam.ac.uk

## Slide 2
mechanical alloying

## Slide 3
extrusion of canned powder

## Slide 4
200 nm
“MA956” Fe-20Cr-4.5Al-0.5Ti-0.5 yttria wt%

## Slide 5
“MA6000”
Ni-15Cr-4.5Al-2.3Ti-4W-1.1 yttria wt%
200 nm

## Slide 7
Helical grains

## Slide 9
not recrystallised

## Slide 12
MA956

## Slide 15
Probability of pairwise bonds in random solution

## Slide 16
o
o
A
B
A
B
1-x
Gibbs free energy per mole
Concentration x of B
m
m
free energy of
mechanical
mixture
G*
x
Mechanical Mixture

## Slide 17
o
o
A
B
A
B
x
Gibbs free energy per mole
Composition
m
m
G{x}
free energy of
mechanical
mixture
∆G
M
free energy
of solution
G*

## Slide 18: Entropy
P
P / 2

## Slide 19
+
=

## Slide 20
For a random mixture, number of configurations given by:

## Slide 21
Boltzmann

## Slide 23
Classical theory for entropy of mixing

## Slide 24
Solution-like behaviour when particles about 1000 atoms in size
Free energy of mixing due to configurational entropy alone

## Slide 25
Enthalpy

## Slide 27
Surface per unit volume
Sv
Particle size
Solution formation impossible!

## Slide 28
coherent
coherent
incoherent

## Slide 29
Single barrier to solution formation when components attract

## Slide 30
Double barrier to solution formation when components immiscible

## Slide 31
o
o
A
B
A
B
Gibbs free energy per mole
m
m
Concentration x of B
Paradox at concentration extremities vanishes in the discrete model of concentration