## Slide 1: Atomic mechanism of the bainite transformation
www.phase-trans.msm.cam.ac.uk

## Slide 5: Displace atomic arrangement into new pattern

## Slide 6: Reconstruct atomic arrangement into new pattern

## Slide 7
Martensitic transformation in pure iron
Zerwech & Wayman
Acta Metallurgica 13 (1965) 99

## Slide 8
Toshihiko Koseki, University of Tokyo

## Slide 9
9

## Slide 10
Displacive transformations (Widmanstaetten ferrite, bainite, martensite) cause deformation.
Reconstructive transformations (pearlite, ferrite) do not.

## Slide 12
Shipway & Bhadeshia 1995

## Slide 13: Plastic strain: stabilisation

## Slide 14
Plastic deformation cannot retard reconstructive transformation
Only displacive transformation can be mechanically stabilised.

## Slide 15
c
r
d
s
1
Christian, 1957

## Slide 16
Caballero, Mateo & Bhadeshia

## Slide 17
Peet & Bhadeshia 2011
Giant shear strain of 0.46

## Slide 18
478°C for 43 days – bainite completed in seconds. Bhadeshia (1981)

## Slide 19
Substitutionalsolutes
frozen
Bhadeshia, Waugh, 1981

## Slide 20
(1855)
Flux is proportional to the gradient

## Slide 21
o
o
A
B
A
B
x
Gibbs free energy per mole
Composition
m
A
m
B
m
m
G{x}

## Slide 32
Carbon
Manganese
a
g
a+g
a
g
High supersaturation
NP-LE mode
a
g

## Slide 33
Metall. Mater. Trans. A 43 (2012) 833
diffusion distance 0.03 nm
Metall. Mater. Trans. A 46 (2015) 2347
diffusion distance 0.002-0.04 nm
how do we proceed?

## Slide 35
time
Cr
distance
Yoshiyuki Saito
Carlos Martins

## Slide 36
chemical interfacial energy
larger with steeper gradients
STEEP GRADIENTS RETARD DIFFUSION
Most rapidly growing Fourier components have infinitely small wavelength

## Slide 39
Impossible to avoid partitioning substitutional solutes if local equilibrium is demanded.

## Slide 40
Current Opinion in Solid State and Materials Science,
20 (2016) 396-400
Physica Status Solidi (a)
69 (1982) 745-750
www.phase-trans.msm.cam.ac.uk
Conclusion: NPLE mode does not exist

## Slide 41
Substitutionalsolutes
frozen
Bhadeshia, Waugh, 1981

## Slide 42
Notes: 42

## Slide 49
Temperature / °C
Impact energy / J

## Slide 52
20 µm

## Slide 54
Kevin Sawley: 90 million gross tonnes of traffic on curve

## Slide 56
Prior austenite grain
boundary embrittlement
Displacive atomic mechanism:
more susceptible to impurity embrittlement

## Slide 57
www.phase-trans.msm.cam.ac.uk
Adolf Martens
Bainite forms by the same mechanism as martensite, it is diffusionless, but tempers during the course of transformation.
This is the basis of the modern design of steels.

## Slide 58: Composition following transformation

## Slide 59
Bhadeshia, Met. Sci. (1982)

## Slide 61
It was assumed therefore, that these carbon atoms are trapped at dislocations, since the original paper published in 1981.
Bhadeshia, Edmonds
Metall. Trans. (1979)

## Slide 62
Austenite
Ferrite
Dislocation
Francisca Garcia Caballero
Caballero, Miller, Mateo, Cornide. J. Alloys & Compounds, (2012)
Large carbon concentration in solution in ferrite

## Slide 63
Caballero, Miller, Mateo, Cornide
J. Alloys & Compounds, (2012)
atom probe data for carbon in solid solution in ferrite in contact with austenite

## Slide 64
A diffusionless transformation will necessarily lead to a body-centred tetragonal ferrite.

## Slide 65
Huge increase in solubility; ferrite with tetragonal symmetry
Jang, Suh, Bhadeshia, Scr. Mat. 68 (2012) 195

## Slide 66
C. N. Hulme-Smith, I. Lonardelli,
A. C. Dippel and H. K. D. H. Bhadeshia, Scr. Mat. 69 (2013) 409.