## Slide 3
Martensitic transformation in pure iron
Zerwech & Wayman
Acta Metallurgica 13 (1965) 99

## Slide 4
Displacive transformations (Widmanstaetten ferrite, bainite, martensite) cause deformation.
Reconstructive transformations (pearlite, ferrite) do not.

## Slide 5
Toshihiko Koseki, University of Tokyo

## Slide 6: Unresolved issues:
www.phase-trans.msm.cam.ac.uk
Difficulties in theory of ferrite growth
steep concentration gradients

## Slide 7
(1855)
Flux is proportional to the gradient

## Slide 8
o
o
A
B
A
B
x
Gibbs free energy per mole
Composition
m
A
m
B
m
m
G{x}

## Slide 19
Carbon
Manganese
a
g
a+g
a
g
High supersaturation
NP-LE mode
a
g

## Slide 20
Metall. Mater. Trans. A 43 (2012) 833
diffusion distance 0.03 nm
Metall. Mater. Trans. A 46 (2015) 2347
diffusion distance 0.002-0.04 nm
how do we proceed?

## Slide 22
time
Cr
distance
Yoshiyuki Saito
Carlos Martins

## Slide 23
chemical interfacial energy
larger with steeper gradients
STEEP GRADIENTS RETARD DIFFUSION
Most rapidly growing Fourier components have infinitely small wavelength

## Slide 26
Impossible to avoid partitioning substitutional solutes if local equilibrium is demanded.
a
g

## Slide 27
Current Opinion in Solid State and Materials Science,
20 (2016) 396-400
Physica Status Solidi (a)
69 (1982) 745-750
Conclusion 1: NPLE mode does not exist

## Slide 29
Ae3'
T'
o
x
Carbon in austenite
Temperature

## Slide 30
The NPLE curve on a phase diagram does NOT represent a locus where a reaction stops.
Carbon
Temperature

## Slide 31
Carbon
Manganese
a
g
a+g
a
g
High supersaturation
NP-LE mode
a
g

## Slide 32
Conclusion 2:
NPLE cannot represent incomplete reaction
… because it does not define the
termination of a reaction.

## Slide 33
Carbon
Manganese
Is paraequilibrium possibile for diffusional transformations?

## Slide 34
Chance & Ridley (1981)

## Slide 35
Conclusion 3:
paraequilibrium applies only to
displacive transformations
Comment:
there is no evidence for
paraequilibrium diffusional-transformation

## Slide 36
Diffusional transformations must occur without equilibrium when atomic mobility is limited.
The theory for this exists.
www.phase-trans.msm.cam.ac.uk