## Slide 1: Is graphene stronger than steel?
www.phase-trans.msm.cam.ac.uk
Morinobu Endo, 2004

## Slide 2
Naydenova, Peet, Russo; PNAS 116 (2019) 11718

## Slide 3
July 2020: student recruitment information

## Slide 4
Has graphene delivered a strong material?
Is there a scaling law for strength?

## Slide 5
ideal strength?

## Slide 6
Clatterbuck et al.
Phil. Mag. Lett.
2002

## Slide 7: Maximum strength of iron when pulled along its weakest direction?
14.5 GPa

## Slide 8
Brenner:1956
Single crystals of iron

## Slide 9
Commercial alloy made by Kobe Steel

## Slide 11
Claimed strength of carbon nanotube is 130 GPa
Edwards, Acta Astronautica, 2000
Claimed modulus is 1.2 TPa
Terrones et al., Phil. Trans. Roy. Soc., 2004

## Slide 12: How is the strength of nanotube calculated?
By ignoring the empty space within the nanotube
Therefore strength of steel, which has 32% space unoccupied, is greater by 47% than reported since time zero

## Slide 13
data from Pan et al. 1999, Yu et al. 2000

## Slide 14
An equilibrium number of defects.
Strength of a nanotube rope 2 mm long is less than 2000 MPa

## Slide 15
Lee et al. Science (2008)
reported breaking strength
of 130 GPa for sample
about 2 µm square of
pristine graphene

## Slide 16: Intrinsic strength of Graphene (samples 2 µm2)

## Slide 17
Han et al., Nanoscale, 7 (2015) 15672

## Slide 18
Han et al.
Nanoscale
7 (2015) 15672
Polycrystalline graphene is brittle under homogeneous tensile stress

## Slide 19
Micropillar tests: Dou, Derby, Scripta Mat. 61 (2009) 524

## Slide 21: Graphene in composites
Zhao et al.
Macromolecules
43 (2010) 2357

## Slide 22
500 MPa
2000 MPa
1200 MPa

## Slide 25
strength 130 GPa
modulus 1.2 TPa
 | J g-1 | m s-1
Dynamite | 4650 | 6000
Nanotube | 5420 | 21500

## Slide 26: Conclusions
Graphene is at best ten times stronger than steel but at the micrometre level
No evidence that the strength of graphene is sustained as the size is increased.
Graphene is, a brittle material, can only be stressed elastically.