## Slide 1: Diffusion in steep concentration gradients:
www.phase-trans.msm.cam.ac.uk
Difficulties in theory of ferrite growth
steep concentration gradients
IIT Kharagpur
2002

## Slide 2
(1855)
}
concentration
gradient
diffusion
coefficient
flux

## Slide 3
ice: pure
ocean: salty water
photograph courtesy of Sunita Hansraj from her Antarctica expedition
Why no diffusion of salt from sea-water into ice?

## Slide 4
o
o
A
B
A
B
x
Gibbs free energy per mole
Composition
m
A
m
B
m
m
G{x}

## Slide 9
Kinetics of ferrite growth

## Slide 16
Carbon
Manganese
a
g
a+g
a
g
High supersaturation
NP-LE mode
a
g

## Slide 17
Metall. Mater. Trans. A 43 (2012) 833
diffusion distance 0.03 nm
Metall. Mater. Trans. A 46 (2015) 2347
diffusion distance 0.002-0.04 nm
how do we proceed?

## Slide 19
time
Cr
distance
Yoshiyuki Saito
Carlos Martins

## Slide 20
chemical interfacial energy
larger with steeper gradients
STEEP GRADIENTS RETARD DIFFUSION
Most rapidly growing Fourier components have infinitely small wavelength

## Slide 23
Impossible to avoid partitioning substitutional solutes if local equilibrium is demanded.

## Slide 24
Current Opinion in Solid State and Materials Science,
20 (2016) 396-400
Physica Status Solidi (a)
69 (1982) 745-750
www.phase-trans.msm.cam.ac.uk
Conclusion: NPLE mode does not exist

## Slide 25
Corollary: NP-LE has never been observed experimentally although widely implemented in software
Measurements are crude, do not account for ledge mechanism.
No measurements of concentration profiles for NP-LE, even though we have atom probes.
Pearlite always shows partitioning.
NP-LE should never be used as a limiting composition.
Chance, Ridley
Furuhara et al.

## Slide 26
Corollary: thermodynamics of irreversible processes

## Slide 27
polynomial expansion of flux
as a function of force

## Slide 28
General law of irreversible thermodynamics:
In diffusion, flux becomes proportional to the free energy gradient:

## Slide 29
(1855)
}
concentration
gradient
diffusion
coefficient
flux

## Slide 32
Newton’s cooling law
Phil. Trans. Roy. Soc. 1701

## Slide 33
All of these processes driven by free energy gradients.
www.phase-trans.msm.cam.ac.uk