## Slide 1: Diffusion-controlled growth in multicomponent steels
www.phase-trans.msm.cam.ac.uk
Difficulties in theory of ferrite growth
steep concentration gradients
(Apparao Chintha)

## Slide 2
(1855)
}
concentration
gradient
diffusion
coefficient
flux

## Slide 3
ice: pure
ocean: salty water
photograph courtesy of Sunita Hansraj from her Antarctica expedition
Why no diffusion of salt from sea-water into ice?

## Slide 4
o
o
A
B
A
B
x
Gibbs free energy per mole
Composition
m
A
m
B
m
m
G{x}

## Slide 9
Kinetics of ferrite growth

## Slide 16
Carbon
Manganese
a
g
a+g
a
g
High supersaturation
NP-LE mode
a
g

## Slide 17
Metall. Mater. Trans. A 43 (2012) 833
diffusion distance 0.03 nm
Metall. Mater. Trans. A 46 (2015) 2347
diffusion distance 0.002-0.04 nm
how do we proceed?

## Slide 19
time
Cr
distance
Yoshiyuki Saito
Carlos Martins

## Slide 20
However, diffusion coefficient
is actually a function of the concentration gradient. Large gradients retard diffusion. i.e. free energy is a function of gradient of concentration.
Most rapidly growing Fourier components have infinitely small wavelength

## Slide 23
Impossible to avoid partitioning substitutional solutes if local equilibrium is demanded.

## Slide 24
NP-LE has never been observed experimentally: kinetic data
Babu, Bhadeshia,1981

## Slide 25
NP-LE has never been observed experimentally although widely implemented in software
Pearlite always shows partitioning.
Chance, Ridley

## Slide 26
NP-LE has never been observed experimentally although widely implemented in software
NP-LE should never be used as a limiting composition.
Furuhara et al.

## Slide 27
NP-LE has never been observed experimentally although widely implemented in software
Plenty of warnings in the theory of irreversible thermodynamics that for the concept of local equilibrium to be valid, the situation must not be too far removed from equilibrium.
e.g. J. W. Christian, Theory of Transformations in Metals and Alloys, Pergamon Press, Oxford, 2nd edition, p.98

## Slide 28
Kannan R, Wang Y, Poplawsky J, Babu SS, Li L. Cascading phase transformations in high carbon steel resulting in the formation of inverse bainite: An atomic scale investigation. Scientific reports. 2019 Apr 3;9(1):1-5.

## Slide 29
Kannan R, Wang Y, Poplawsky J, Babu SS, Li L. Cascading phase transformations in high carbon steel resulting in the formation of inverse bainite: An atomic scale investigation. Scientific reports. 2019 Apr 3;9(1):1-5.

## Slide 32
Current Opinion in Solid State and Materials Science,
20 (2016) 396-400
Physica Status Solidi (a)
69 (1982) 745-750
www.phase-trans.msm.cam.ac.uk
NPLE mode cannot exist