## Slide 1
Hydrogen and steel
www.phase-trans.msm.cam.ac.uk

## Slide 2
The first ever paper: William H. Johnson, 1875, Proceedings of the Royal Society, 23 (1875) 168-179
Nascent hydrogen
Diffusible hydrogen
Reversible

## Slide 3
Hobson, 1951

## Slide 4
Hydrogen embrittles iron
both single and polycrystalline forms
L. B. Pfeil, Proceedings of the Royal Society, 1926
normal
pickled
Perspectives in hydrogen embrittlement in metals (1986) 647
Materials Science and Engineering 77 (1986) 75

## Slide 5
R. P. Frohmberg, Wright-Patterson Air Force Base report, 1954

## Slide 6
Increased from 38,400 to 56,100
since 2016 to 2021

## Slide 7
a


Iron

## Slide 8
Fe-H phase diagram
Hydrogen dissolves less in ferrite than in austenite
data from Okamoto:2004

## Slide 9
hydrogen diffuses faster in ferrite, but there are complications

## Slide 10
Metall. Mat. Trans. A 46 (2015) 2323

## Slide 11
Song and Curtin
Nature Materials
12 (2013) 145-151

## Slide 13: Summary
All evidence points to easily diffusible or
weakly trapped hydrogen embrittles
Trapped molecular hydrogen irrelevant.
Strongly trapped hydrogen irrelevant.

## Slide 16
Yamasaki and Bhadeshia, 2006

## Slide 17
Song, Bhadeshia, Suh, 2013

## Slide 20
Fielding et al. (2014)
non-percolating
austenite
percolating austenite

## Slide 21
Mitigating consequences of hydrogen
Provide traps for infused hydrogen
Retard the infusion of hydrogen
Any alloy modifications must not compromise other properties

## Slide 23
Ooi SW, Black oxide coating and its effectiveness on prevention of hydrogen uptake. Materials Science and Technology. 2019, 35:12-25.

## Slide 25
High-pressure, high-temperature hydrogen attack
(13.7 MPa, 600°C)
Reaction of hydrogen with carbides to form methane bubbles.

## Slide 26
Mohamed
Alshafrani
1 µm