## Slide 1
“pearly” structure
Journal of the Iron and Steel Institute 1 (1886) 140

## Slide 2: Strength of undeformed pearlite
www.phase-trans.msm.cam.ac.uk
E. C. Bain

## Slide 3
Three-dimensional, image of lamella of cementite in pearlite. Image generated using serial sectioning.
Courtesy of Yoshitaka Adachi.

## Slide 4
Zhang, Enomoto, ISIJ International, 49 (2009) 921
Kaiming Wu
Wuhan University of Science and Technology

## Slide 5
Cementite 1000 HV
Ferrite 250 HV

## Slide 6: Stress to initiate plasticity sensitive to interlamellar spacing
“Hall-Petch relation …. by no means completely verified”
“equally good”
Page 230

## Slide 7: Other problems
Dollar, Bernstein, Thompson
Acta Metallurgica
36 (1988) 311

## Slide 8: Theories: Hall-Petch

## Slide 9: Cementite: primitive crystal structure

## Slide 10: Theories: Langford
Dislocations pass through and shear cementite

## Slide 11: Dislocation bowing between rigid cementite

## Slide 12: Semiconductors: relaxation of epitaxial layer deposited on a substrate

## Slide 14
Thin film theory
Order of magnitude smaller than expected from theory

## Slide 15: Hall-Petch

## Slide 16: Solid solution effects
Data due to Fu, Furuhara

## Slide 17: Comparison of nanostructure ferrite with pearlite
Data points: Tsuji et al.
Scr Mat 46 (2002) 893

## Slide 18: Bayesian analysis

## Slide 19: Why controversy about Hall-Petch? … friction stress in ferrite negative intercept

## Slide 20: Overfitting of noisy data

## Slide 21: Data can be downloaded from
www.phase-trans.msm.cam.ac.uk/2022/HP.xlsx
Critical assessment: the strength of undeformed pearlite
Materials Science and Technology, 2022
DOI: 10.1080/02670836.2022.2079295