## Slide 1: Choreography of atoms during the bainite transformation
Henry Clifton Sorby Award
Notes: 1050-1150 a.m.

## Slide 2
Réamur, “model of a modern materials scientist”.
Scientists of the time did not know that real materials had crystals.
MDCLXXXIII = 1683
MDCCLVII = 1757

## Slide 3
19th century: Sorby, applied microscope to steel and discovered its crystalline structure (1863).
“pearly” (1886)

## Slide 4
Birmingham Royal Ballet Company: ordered and symmetrical motion that leads to a predictable change in shape

## Slide 5
Siobhan Davies’ Dance Company: disordered equilibrium

## Slide 6
Low atomic mobility:
all atoms
High atomic mobility:
small atoms

## Slide 7: Structure of Fe to terapascal pressures and 40000 K (Stixrude, 2012)
Fe-25Mn-5.2Si wt%

## Slide 8
Sufficient atomic mobility
Reconstructive
transformation

## Slide 9: Any obstacles retard coordinated motion

## Slide 10
Condition for diffusionless growth

## Slide 11
Conditions for diffusionless transformation:
.... slow diffusion
.... large driving force
far from equilibrium
... huge strain energy
... solute trapping
.... crystallographic criteria

## Slide 14
J. H. Pak, D. W. Suh, H. K. D. H. Bhadeshia
Metall. & Mater. Trans A 43 (2012) 4520
Real time
|
|
50 µm

## Slide 15
Swallow E, Bhadeshia HKDH. High resolution observations of displacements caused by bainitic transformation. Materials Science and Technology. 1996;12:121

## Slide 17: Bainite forms at low driving forces .....austenite separates into carbon-rich and carbon-depleted regions ...
.... depleted regions → ferrite

## Slide 18
Aaronson, Domian, Pound, Thermodynamics of the austenite to proeutectoid ferrite transformation I
TMS-AIME 236 (1966) 753-767

## Slide 19
Accelerate electrons around magnetised ring.
Electrons bend around this ring, lose some energy as X-rays.
X-rays funnelled down
beamlines for experiments.

## Slide 20: Time sequence
Diffraction angle 2θ
Intensity
H. J. Stone, M. J. Peet, H. K. D. H. Bhadeshia, P. J. Withers, S. S. Babu, E. D. Specht
Proc. of the Royal Society A, 464 (2008) 1009-1027

## Slide 21: isothermal transformation at 300 °C
111 austenite
002 austenite
011 ferrite
002 Pt
Time
H. J. Stone, M. J. Peet, H. K. D. H. Bhadeshia, P. J. Withers, S. S. Babu, E. D. Specht
Proc. of the Royal Society A, 464 (2008) 1009-1027

## Slide 22: isothermal transformation at 200 °C
111 austenite
002 austenite
002 Pt
H. J. Stone, M. J. Peet, H. K. D. H. Bhadeshia, P. J. Withers, S. S. Babu, E. D. Specht
Proc. of the Royal Society A, 464 (2008) 1009-1027
Time (10 h total)

## Slide 23
Photoemission electron microscopy
3 orders of magnitude faster than carbon diffusion-control
growth rate?

## Slide 24
Acoustic emissions ....
Courtesy of Francisca Garcia Caballero
... from bainite

## Slide 25
Bhadeshia HKDH, Waugh AR. Bainite: An atom-probe study of the incomplete reaction phenomenon. Acta Metallurgica. 1982;30:775-84.

## Slide 26
Bhadeshia HKDH. Theoretical analysis of changes in cementite composition during tempering of bainite. Materials Science and Technology. 1989;5:131-7.

## Slide 28
Growth is diffusionless
but plate decarburised shortly afterwards

## Slide 29
Chart: Limiting carbon / wt%
| 0.557894736842105 | 1.3518796992481199
T_0' 1Si | 477 | 227
T_0 1Si | 475.8688 | 227
1Si | 349.1719 | 299.3982
T0 2Si | 476.2458 | 229.2282
T0' 2Si | 474.9089 | 229.0311
2Si | 400.6241 | 349.8039
T0 3Si | 476.2464 | 225.8273
T0' 3Si | 476.2464 | 225.8273
T0' 3Si | 1
T0' 3Si | 477.1566 | 227.8933
3Si | 397.6293 | 348.2702 | 298.89
T0 4Si | 479.6424 | 228.0886
Ae3'
T0'
T0
Lin S, Borgenstam A, Stark A, Hedström P. Effect of Si on bainitic transformation kinetics in steels explained by carbon partitioning, carbide formation, dislocation densities, and thermodynamic conditions. Materials Characterization. 2022:111774
Notes: Talk about the Swedish W_SB_s concept

## Slide 31
Notes: 31

## Slide 32
Very poor toughness!

## Slide 34
Carbide-free alloys
Fe-0.4C-3Mn-2Si
Fe-0.2C-3Mn-2Si
Fe-0.4C-4Ni-2Si wt%
Notes: 34

## Slide 36
0.5 μm

## Slide 37
0.4C-2Si-4Mn
0.2C-2Si-3Mn
0.4C-2Si-4Ni

## Slide 39
Yates, Jerath, Bhadeshia
Notes: 39

## Slide 40
carbide-free bainitic rail
Carbide-free bainite has no hard particles,
Just bainitic ferrite and retained austenite
Kevin Sawley: 90 million gross tonnes of traffic on curve

## Slide 41
November 2019: 1 billion gross tonnes of traffic achieved, without need for grinding
Pascal Secordel (Francerail), Jay Jaiswal (Arrail)
April 2020
Notes: 41

## Slide 42
“Bainitic low fatigue” (BLF) is mandated for all new French TGV high-speed moveable points.
Daniel Callejas Sevilla
CC BY-SA 3.0 Unported

## Slide 43
2500
2000
1500
1000
20
40
60
80
100
120
140
160
180
Ultimate tensile strength / MPa
Fracture toughness / MPa √m
18 wt% Ni
maraging steel
QT
Ascometal

## Slide 45
Low transformation temperature
Bainitic hardenability
Reasonable transformation time
Elimination of cementite
Austenite grain size control
Avoidance of temper embrittlement

## Slide 47
Real images of nanostructured bainite

## Slide 48
Zhang & Yang, 2019
wind turbines +rolling mill, vibration machinery

## Slide 50
It was assumed therefore, that these carbon atoms are trapped at dislocations, since the original paper published in 1981.
Bhadeshia, Edmonds
Metall. Trans. (1979)

## Slide 51
Austenite
Ferrite
Dislocation
Large carbon concentration in solution in ferrite
Caballero, Miller, Mateo, Cornide, J. Alloys & Compounds, (2012)

## Slide 52
C. N. Hulme-Smith, I. Lonardelli,
A. C. Dippel and H. K. D. H. Bhadeshia, Scr. Mat. 69 (2013) 409.

## Slide 53
Huge increase in solubility; ferrite with
tetragonal symmetry
Jang, Suh, Bhadeshia, Scr. Mat. 68 (2012) 195