## Slide 1: Atomic mechanism of the acicular ferrite transformation
www.phase-trans.msm.cam.ac.uk

## Slide 2
Crystallographic grain size
Gourgues A.-F., Flower HM, Lindley TC. Electron backscattering diffraction study of acicular ferrite, bainite, and martensite steel microstructures. Materials Science and Technology. 2000;16:26-40.
Pickering FB: Proc. Symp. ‘Transformation and hardenability in steels’.
Ann Harbor, MI, February 1967, Climax Molybdenum Co. and The University of Michigan, 109–129.
cleavage facet corresponds to the distance between large-misorientation boundaries that force crack deflection
cleavage facet corresponds to crystallographic grain size

## Slide 3
Crystallographic grain size

## Slide 4
Image courtesy of Graeme Barritte

## Slide 5
Bhadeshia, Bainite in Steels 3rd edition, p. 271

## Slide 6
role of inclusions

## Slide 7: Testing minerals: the method
Gregg JM, Bhadeshia HKDH. Bainite nucleation from mineral surfaces. Acta metallurgica et materialia. 1994 42:3321-30.

## Slide 12
Sketches courtesy of Suresh S. Babu
Competition between grain surface and inclusion nucleation

## Slide 13
Jones, Bhadeshia Metall. Mater. Trans. A
28 (1997) 2005-2103

## Slide 14
Fe-0.06C-0.27Si-1.84Mn-2.48Ni-0.2Mo wt% + 399 ppmw of oxygen
Austenitised at 950°C for 10 min, transformed isothermally at 460°C for 30 min.
Yang JR, Bhadeshia HKDH. Acicular ferrite transformation in alloy-steel weld metals. Journal of materials science. 1991 Feb;26(3):839-45.

## Slide 15
Fe-0.06C-0.27Si-1.84Mn-2.48Ni-0.2Mo wt% + 399 ppmw of oxygen
Austenitised at 1200°C for 10 min, transformed isothermally at 460°C for 30 min.
Yang JR, Bhadeshia HKDH. Acicular ferrite transformation in alloy-steel weld metals. Journal of materials science. 1991 Feb;26(3):839-45.

## Slide 16
Micrograph courtesy of
Martin Strangwood

## Slide 17: Stress affected transformation
Babu SS, Bhadeshia HKDH. Stress and the acicular ferrite transformation. Mat. Sci. and Engineering: A. 1992 156:1-9.

## Slide 19
Growth is diffusionless
but plate decarburised shortly afterwards

## Slide 20
Strangwood M, Bhadeshia HK. The mechanism of acicular ferrite formation in steel weld deposits. ASM INTERNATIONAL,. 1986:209-13.

## Slide 22
Ali, Bhadeshia Materials Science & Techn.
6 (1990) 781-784

## Slide 23
quantitative theory for the transition
from upper to lower bainite

## Slide 24: Lower acicular ferrite
Sugden AA, Bhadeshia HKDH. Lower acicular ferrite. Metallurgical Transactions A. 1989 20:1811-8.

## Slide 26
Acta Metallurgica, Vol. 33, 1985, pp. 1271-1283 H.K.D.H. Bhadeshia, L.-E. Svensson and B. Gretoft