## Slide 1: Steels: martensite Lecture 1
Harry Bhadeshia
Professor of Metallurgy
Queen Mary University of London
Emeritus Tata Steel Professor of Metallurgy
University of Cambridge
Fabio Miani
2022

## Slide 2
Low atomic mobilities

## Slide 3
Low atomic mobilities: diffusionless growth

## Slide 4
Two reasons for diffusionless
transformation:
.... small diffusion coefficient
.... large driving force
but far from equilibrium
... huge strain energy
... solute trapping

## Slide 5: Fe-0.2C-1.5Mn wt%, 300 K
Bhadeshia HKDH, Alternatives to the ferrite-pearlite microstructures
Materials Science Forum 284 (1998) 39-50.

## Slide 6
Diffusion over length
scale of product

## Slide 8
Time-temperature-transformation diagrams

## Slide 10
hard
quenched
plates or laths
displacive
volume change
brittle
body-centred tetragonal
metastable
diffusionless

## Slide 11
Materials, transformation temperatures & strength
F. R. Chien and R. J. Clifton and S. R. Nutt
Journal of the American Ceramics Society
78 (1995) 1537

## Slide 13
Data from: P. G. Winchell and M. Cohen, Effect of carbon on the hardness of martensite and austenite, Trans. Metall. Soc. AIME 224 (1962) 638.

## Slide 14
Data from: J. M. Chilton and P. M. Kelly, Strength of ferrous martensite, Acta Metallurgica 16 (1968) 637

## Slide 15
Courtesy of Professor Koichi Tsuchiya, Toyohashi University of Technology

## Slide 16
can form at incredibly low temperatures
can form very rapidly
no composition change
Diffusionless

## Slide 17
Plate shape

## Slide 18
Needles of molybdenum carbide
Yamasaki S, Bhadeshia HK. Modelling and characterisation of Mo2C precipitation and cementite dissolution during tempering of Fe–C–Mo martensitic steel. Materials Science and Technology. 19 (2003)723-731.

## Slide 20
Irrational: why?

## Slide 21
Shape of martensite ?

## Slide 22
Nishiyama-Wasserman

## Slide 24
Kurdjumov-Sachs

## Slide 25
actual orientation
irrational

## Slide 26
athermal transformation

## Slide 27
Fe-0.05C-24Ni-3Mn-0.2Cu wt%
Kurdjumov GV, Maksimova OP. Kinetics of austenite to martensite transformation at low temperatures. Doklady Akademii Nauk SSSR. 61 (1948) 83-86.

## Slide 31
Glissile interface

## Slide 35
Glissile interface cannot contain >1 set of dislocations.
Martensitic transformation only possible if γ→α’ deformation leaves 1 line undistorted and unrotated, i.e. an invariant-line.
Deformation is an invariant-line strain.

## Slide 40
Wirtschaftsvereinigung Stahl, Düsseldorf
courtesy of Professor Hans Werner Zoch

## Slide 41
M. Benke, V. Mertinger, Institute of Physical Metallurgy, Metalforming and Nanotechnology, University of Miskolc
http://www.matsci.uni-miskolc.hu/new/

## Slide 42
unit length

## Slide 43
J. W. Christian, Accommodation strains in martensite formation, the use of the dilatation parameter, Acta Metallurgica 6 (1958) 377.