## Slide 1: Steels: TRIP steels Lecture 9
Harry Bhadeshia
Professor of Metallurgy
Queen Mary University of London
Emeritus Tata Steel Professor of Metallurgy
University of Cambridge
Fabio Miani
2022

## Slide 2
Tailored blanks

## Slide 3
Inner panels of both doors and side panel use tailored blanks

## Slide 4
aluminium-killed
TRIP-steel
Mizui et al. (1997)

## Slide 5
Fe-0.18C-0.2Si-0.9Mn-2.9Ni-1.5Cr-0.4Mo wt%
Professor Toshihiko Koseki of The University of Tokyo
shape deformation
orthonormal coordinates

## Slide 6
u
v

## Slide 8
Bhadeshia HKDH. An aspect of the nucleation of burst martensite. Journal of Materials Science. 1982;17:383-6.

## Slide 9
s
50 mm
polycrystalline austenite
Bhadeshia HKDH. An aspect of the nucleation of burst martensite. Journal of Materials Science. 1982;17:383-6.

## Slide 12
tensile axis
= 15%
41.7°
Bhadeshia HK. TRIP-assisted steels? ISIJ international. 2002;42:1059.

## Slide 13
Transformation plasticity does not contribute much to elongation, so what gives TRIP-steels their large elongation, typically 25%?
Necking during tension is a plastic instability
..... any localised stress concentration must be balanced by work hardening

## Slide 14
tested at room temperature
14.3% 
7% 
Chatterjee S, Murugananth M, Bhadeshia HKDH. δ TRIP steel. Materials Science and Technology. 2007;23:819-27.

## Slide 15
tested at 100 °C
14.3% 
13% 
Chatterjee S, Murugananth M, Bhadeshia HKDH. δ TRIP steel. Materials Science and Technology. 2007;23:819-27.

## Slide 16
Austenitic stainless steel
(Courtesy Prof. Nobuhiro Tsuji)
25 ∘C
200 ∘C

## Slide 17
TRIP steels that are fully austenitic are expensive
How do we produce cheap austenite?

## Slide 18: TRIP-Assisted Steels
too much carbon is bad
Jae Hoon Jang, In Gee Kim
austenite is expensive
carbon can be cheap
Notes: 18

## Slide 20
Typical composition Fe-0.15C-1.5Si-1.5Mn wt%

## Slide 21
Typical microstructure:
70% allotriomorphic ferrite
16% bainitic ferrite
14% retained austenite
2.1% elongation due to TRIP

## Slide 22
aluminium-killed
TRIP-steel
Mizui et al. (1997)
work hardening!

## Slide 23
Elongation of TRIP-assisted steel
not due to transformation plasticity
work hardening due to hard martensite

## Slide 25
Corten is a weathering steel with 0.25-0.55Cu and 0.5-1.25Cr wt% develops a patina

## Slide 26: TRIP-Assisted Steels
too much silicon is bad
Notes: 26

## Slide 32
Notes: 32

## Slide 33
Notes: 33

## Slide 34
(Prof. Hongliang Yi, Northeastern University, China)
continuous casting
after hot-rolling

## Slide 35
(Prof. Hongliang Yi, Northeastern University, China)
after cold-rolling
after continuous annealing