## Slide 1: Steels: TWIP steels Lecture 10
Harry Bhadeshia
Professor of Metallurgy
Queen Mary University of London
Emeritus Tata Steel Professor of Metallurgy
University of Cambridge
Fabio Miani
2022

## Slide 2
mechanical twinning

## Slide 3
Austenite

## Slide 4
A

## Slide 5
A
B
CA
B
A
B CBC
A
B CBA
A

## Slide 6
Frommeyer, Brux and Neumann

## Slide 7
Frommeyer, Brux and Neumann
dynamic Hall-Petch effect

## Slide 8
TWIP Steels
Fe-25Mn-3Si-3Al wt%
density 7.3 g cm-3
fully austenitic
maintain attractive properties to -150°C
and at high strain rates (103 s-1)
Data from: Frommeyer G, Brüx U, Neumann P. Supra-ductile and high-strength manganese-TRIP/TWIP steels for high energy absorption purposes. ISIJ international. 2003;43:438-46.

## Slide 9
delayed fracture
difficult to produce
high thermal expansion
Courtesy of Bruno de Cooman

## Slide 10: Atomic traps for hydrogen
Fe
Al
Song EJ, Bhadeshia HKDH, Suh DW. Interaction of aluminium with hydrogen in twinning-induced plasticity steel. Scripta Materialia. 2014;87:9-12.

## Slide 11
Sanjeev Sharma and Richard Dashwood of the International Manufacturing Centre, WMG University of Warwick.

## Slide 12
courtesy of
Professor Wolfgang Bleck

## Slide 13
https://www.stahl-innovationspreis.de/news/gewinner-2018-sichere-zuege-dank-stahlforschung-und-entwicklung/
Steel innovation award 2018
photo & graphics: DLR

## Slide 15
TRIP, TWIP:
transformation or twinning deformations under an external stress
enhanced work hardening
greater strength and ductility
Suppose a material develops internal stress:
can TRIP be used to stop that stress from developing?

## Slide 16
Weld: liquid metal solidifies, cools, contracts, stress
liquid
solid
contraction
Compensate for thermal contraction
Notes: 16

## Slide 17
Residual stress
Notes: 17

## Slide 18
Notes: 18

## Slide 19
Notes: 19

## Slide 20
Notes: 20

## Slide 21
Jones & Alberry, 1977
Notes: 21

## Slide 22
Charpy
fatigue
corrosion
tensile
critical stress intensity
Notes: 22

## Slide 23
Notes: 23

## Slide 24
Notes: 24

## Slide 25
Notes: 25

## Slide 26
Notes: 26

## Slide 27
Notes: 27

## Slide 28
Criteria for design of stainless steel welding consumable
Cr concentration > 12 wt%
Carbon concentration minimal
Low MS temperature but not too low
Suppress MS with solutes other than carbon
Capable of becoming fully austenitic
Solidification as -ferrite

## Slide 30
Dramatically reduced distortion
Leif Karlsson
Notes: 30