## Slide 1: Steels: Bulk nanostructured steels Lecture 11
Harry Bhadeshia
Professor of Metallurgy
Queen Mary University of London
Emeritus Tata Steel Professor of Metallurgy
University of Cambridge
Fabio Miani
2022

## Slide 2
torsion-compression
(unlimited strain)
equal-channel
angular extrusion
accumulative
roll-bonding
shape-preserving deformations

## Slide 3
wire drawing
shape-altering deformations

## Slide 4: What is a nanostructure?

## Slide 6
adapted using selected data from
Tsuji et al. Scripta Mat. 47 (2002) 893

## Slide 7
…. bulk nanocrystalline steel which is very strong, tough, cheap ….

## Slide 8
Yokota T, Mateo CG, Bhadeshia HKDH. Formation of nanostructured steels by phase transformation. Scripta Materialia. 2004;51:767-70.

## Slide 9
Fine crystals by transformation
Introduce work-hardening capacity
Need to store the heat
Reduce rate
Transform at low temperature

## Slide 10
Swallow and Bhadeshia, 1996

## Slide 12
1 µm
Cementite suppressed using silicon

## Slide 14
Low transformation temperature
Bainitic hardenability
Reasonable transformation time
Elimination of cementite
Austenite grain size control
Avoidance of temper embrittlement

## Slide 16
Paul Davies, Tata Steel, 2012

## Slide 18
ballistic mass efficiency
consider unit area of armour

## Slide 19
Real images of nanostructured bainite

## Slide 20
Zhang & Yang, 2019
wind turbines +rolling mill, vibration machinery

## Slide 21
g
g
a
Very strong
Huge uniform ductility
No deformation
No rapid cooling
No residual stresses
Cheap
Uniform in very large sections

## Slide 22
Fang, Yang, Liu, Song, Fang, Bhadeshia, Materials and Design, 50 (2013) 38
Cannot easily
be welded

## Slide 23
Steel with impossible combination of properties
>2 GPa
30% ductility at conventional strain rates
ductility at very high strain rate
toughness and Charpy impact at -40°C
weldable
cheap, large in all dimensions
mass production
Mathew Peet

## Slide 26
Saurabh Kundu

## Slide 28
Saurabh Kundu

## Slide 30
Two pass
12 mm
Single pass

## Slide 31: High speed video
V0 = 445 m s-1
Vickram Deshpande, Mathew Peet

## Slide 32: Impact abrasion
courtesy of Kati Valtonen
Tampere University Wear Centre