## Slide 1: Steels: bainite ... the connection between theory and manufacture Lecture 4
Harry Bhadeshia
Professor of Metallurgy
Queen Mary University of London
Emeritus Tata Steel Professor of Metallurgy
University of Cambridge
Fabio Miani
2022

## Slide 3
Fe-0.05C-1.55Mn-0.12Si-0.1Nb wt%
600°C, 30 s
Yan P, Bhadeshia HKDH. Mechanism and kinetics of solid-state transformation in high-temperature processed linepipe steel. Metallurgical and Materials Transactions A. 2013 Dec;44(12):5468-77.

## Slide 4
Chart: Limiting carbon / wt%
| 0.557894736842105 | 1.3518796992481199
T_0' 1Si | 477 | 227
T_0 1Si | 475.8688 | 227
1Si | 349.1719 | 299.3982
T0 2Si | 476.2458 | 229.2282
T0' 2Si | 474.9089 | 229.0311
2Si | 400.6241 | 349.8039
T0 3Si | 476.2464 | 225.8273
T0' 3Si | 476.2464 | 225.8273
T0' 3Si | 1
T0' 3Si | 477.1566 | 227.8933
3Si | 397.6293 | 348.2702 | 298.89
T0 4Si | 479.6424 | 228.0886
Ae3'
T0'
T0
Lin S, Borgenstam A, Stark A, Hedström P. Effect of Si on bainitic transformation kinetics in steels explained by carbon partitioning, carbide formation, dislocation densities, and thermodynamic conditions. Materials Characterization. 2022 Feb 3:111774

## Slide 7
uncontrolled cementite precipitation

## Slide 9
Jang, Kim, Bhadeshia (2009)
Notes: 9

## Slide 10
Simple, carbide-free alloys
Fe-0.4C-3Mn-2Si wt%
suppress
cementite
hardenability

## Slide 11
11

## Slide 12
Fine structure
Retained austenite:
TRIP effect
no ductile-brittle transition
barrier to hydrogen
No cementite
Small concentration of C in ferrite

## Slide 13
Very poor toughness!

## Slide 16
Carbide-free alloys
Fe-0.4C-3Mn-2Si
Fe-0.2C-3Mn-2Si
Fe-0.4C-4Ni-2Si wt%
Notes: 16

## Slide 18
0.5 μm

## Slide 19
0.4C-2Si-4Mn
0.2C-2Si-3Mn
0.4C-2Si-4Ni

## Slide 22
Bain: alloying elements in steels (1939)

## Slide 24
image courtesy of pngimg.com
Creative Commons 4.0 BY-NC
https://creativecommons.org/licenses/by-nc/4.0/
wish to design
rail steels using
the carbide-free
bainitic steel

## Slide 25
Rail steel – requirements:
Rolling-contact fatigue.
Wear resistance.

## Slide 28
Yates, Jerath, Bhadeshia
Notes: 28

## Slide 29
carbide-free bainitic rail
Carbide-free bainite has no hard particles,
Just bainitic ferrite and retained austenite
Kevin Sawley: 90 million gross tonnes of traffic on curve

## Slide 30
Notes: 30

## Slide 31
November 2019: 1 billion gross tonnes of traffic achieved
Notes: 31

## Slide 32
Carbide-free bainitic rail in the tunnel has
completed >1000,000,000 gross tonnes of traffic
without developing fatigue, without need for grinding.
Pascal Secordel (Francerail), Jay Jaiswal (Arrail)
April 2020

## Slide 33: Advances in carbide-free bainitic steels
2500
2000
1500
1000
20
40
60
80
100
120
140
160
180
Ultimate tensile strength / MPa
Fracture toughness / MPa √m
18 wt% Ni
maraging steel
QT

## Slide 34
airbags, wheelchairs, tool holders
Ascometal

## Slide 35
Charpy 120 J at 25°C
Strength > 1100 MPa