## Slide 1: Steels: Widmanstätten ferrite Lecture 5
Harry Bhadeshia
Professor of Metallurgy
Queen Mary University of London
Emeritus Tata Steel Professor of Metallurgy
University of Cambridge
Fabio Miani
2022

## Slide 2
Widmanstätten ferrite
2 m
1808: Alois de Widmanstätten, Hradschina meteorite, Imperial Porcelain Works, Vienna
1900: Floris Osmond, head of steel ingot

## Slide 3
Micrograph courtesy of
Rolando M. Núñez Monrroy of the Pontifical Catholic University of Peru.
Ali and Bhadeshia
Notes: 3

## Slide 4
Crystallographic grain size
Gourgues A.-F., Flower HM, Lindley TC. Electron backscattering diffraction study of acicular ferrite, bainite, and martensite steel microstructures. Materials Science and Technology. 2000;16:26-40.
Pickering FB: Proc. Symp. ‘Transformation and hardenability in steels’.
Ann Harbor, MI, February 1967, Climax Molybdenum Co. and The University of Michigan, 109–129.
cleavage facet corresponds to the distance between large-misorientation boundaries that force crack deflection
cleavage facet corresponds to crystallographic grain size

## Slide 5
Crystallographic grain size
Gourgues A.-F., Flower HM, Lindley TC. Electron backscattering diffraction study of acicular ferrite, bainite, and martensite steel microstructures. Materials Science and Technology. 2000;16:26-40.

## Slide 6
Notes: 6

## Slide 7
Notes: 7

## Slide 8
Notes: 8

## Slide 9
Notes: 9

## Slide 10
Notes: 10

## Slide 11
Notes: 11

## Slide 12
50 µm

## Slide 13
Courtesy of N. Oku, K. Asakura, J. Inoue and T. Koseki,
Tetsu-to-Hagane, Vol. 94 (2008) 363-368.

## Slide 14
Watson and McDougall, 1973
Notes: 14

## Slide 15
- Widmanstätten ferrite can grow at small undercoolings
at temperatures well above T0
carbon diffusion essential during transformation

## Slide 16
Notes: 16

## Slide 17
Notes: 17

## Slide 18
conditions at the transformation interface

## Slide 20
diffusion

## Slide 25
consider a cylinder

## Slide 28
Notes: 28

## Slide 29
Mechanism displacive but carbon must partition during growth.
Pairs of plates grow together to minimise strain.
Summary
The plates can grow in carbon-free alloys of iron, in which case, the lengthening rate would be controlled by the mobility of the glissile transformation interface.
Notes: 29

## Slide 31: Phase field simulation of solidification
Video courtesy of
V. Pavlik and U. Dilthey of the ISF-Welding Institute of Aachen University in Germany

## Slide 33
Fe-7.4Cr-1.8Ni wt%
Ricks RA, Bee JV, Howell PR. The decomposition of austenite in a high purity iron-chromium-nickel alloy. Metallurgical Transactions A. 1981;12:1587-1594.

## Slide 34
Bhadeshia HKDH. A rationalisation of shear transformations in steels. Acta metallurgica. 1981 Jun 1;29(6):1117-30.

## Slide 36
Bhadeshia HKDH. A rationalisation of shear transformations in steels. Acta metallurgica. 1981 Jun 1;29(6):1117-30.