## Slide 1: Steels: Pearlite Lecture 7
Harry Bhadeshia
Professor of Metallurgy
Queen Mary University of London
Emeritus Tata Steel Professor of Metallurgy
University of Cambridge
Fabio Miani
2022

## Slide 3
Notes: 3
3

## Slide 4
Cementite
Fe3C?

## Slide 5
Cementite
Pnma
a=0.51
b=0.68
c=0.45 nm

## Slide 6
Cementite

## Slide 7
Cementite
Courtesy Umemoto, Toyohashi University

## Slide 8
Cementite

## Slide 9: The Pearlite Reaction
(Bain, Alloying elements in steels)

## Slide 10
Pearlite nodule

## Slide 11
Data from:
Behera S, Barik RK, Sk MB, Mitra R, Chakrabarti D. Recipe for improving the impact toughness of high-strength pearlitic steel by controlling the cleavage cracking mechanisms. Materials Science and Engineering: A. 2019;764:138256.

## Slide 13
Image courtesy of Ivan Bataev, Novosibirsk State Technical University

## Slide 15
J. D. Embury, and R. M. Fisher: The structure and properties of drawn pearlite,
Acta Metallurgica, 1966, 14, 147–159

## Slide 16
Images courtesy of:
Pascal Antoine, Baekert
crash absorbing plastic

## Slide 17
largest central span in the world, 2 km of free navigation underneath, Japan. Image courtesy of Nobutaka Yurioka

## Slide 18
Nucleation begins either with ferrite or cementite depending on whether the steel is hypo- or hyper-eutectoid

## Slide 22
2S
2S
2S
S
Energy stored in interfaces

## Slide 23
effective driving force
when all free energy
consumed as interface

## Slide 26
+ flux term due to flux
through interface

## Slide 27
Fe-C
volume
interface
mixed

## Slide 29
Divergent pearlite
To see a real image of divergent pearlite,
Figure 4.17 of “Steels” book.