## Slide 1: Machine learning - steels “artificial intelligence”?
Episodic memory
Planning the future
is everything calculable?
ISIJ International 39 (1999) 966

## Slide 2: The need for empirical learning
600°C steam
40 year service
100 MPa stress
oxidation resistance
consistency
mass production
weldability
sequence of heat treatments
C, Mn, Si, Ni, Cr, Mo, V, W, ....

## Slide 4
Charpy
fatigue
corrosion
critical stress intensity
tensile

## Slide 5
electron theory
molecular dynamics
thermodynamics
kinetics
irreversible thermodynamics
finite elements
structure-properties
uncertainties

## Slide 6
Michael McIntyre
y
x

## Slide 7: Solution
non-linear functions
Many, many variables
uncertainties
large knowledge base
Notes: Dogma - statement of belief

## Slide 8
Empirical Equations

## Slide 12: Hyperbolic Tangents

## Slide 15
non-linear
functions

## Slide 16
51 inputs
17 hidden units
Fujii, Mackay, Bhadeshia. Fatigue crack growth. ISIJ International. 36 (1996) 1373

## Slide 21
y
x
A
B

## Slide 22
ultrasupercritical
>700°C

## Slide 23: Creep

## Slide 24
Suppose we fail to achieve 650°C ferritic creep-resistant steel

## Slide 25: Nickel base alloy FT750dc
wt%

## Slide 27
0
200
400
600
800
1000
0
200
400
600
800
1000
1200
Temperature / °C
Yield stress / MPa
Tancret & Bhadeshia, 2002

## Slide 29
Fatigue

## Slide 31: Generic fatigue model

## Slide 32: Steel

## Slide 33: Nickel Alloys

## Slide 34: Titanium and Aluminium alloys

## Slide 35: Solidification cracking
Babu, David, Park, Vitek

## Slide 36
Cracked = 1
Not cracked = 0
uncertainty?
value of 0.5 is the greatest
uncertainty in the output
Ichikawa, Bhadeshia, MacKay
Model for solidification cracking in low alloy steel weld metals
Science and Technology of Welding and Joining 1 (1996) 43-50.

## Slide 40
increasing
solidification range
decreasing
density change
solidification as
as austenite

## Slide 44: Large number of variables
C, Mn, Si, Ni, Cr, Mo, V, Co, B, N, O…..
Thermomechanical processing of steel
Welding consumable
Welding parameters
Subsequent heat treatment
temperature
duration
number of cycles
deformation
strain
anisotropy
protection
structural changes

## Slide 46
Cool & Bhadeshia, 1996

## Slide 48
welded
600°C
650°C
700°C

## Slide 49
new welding
consumables

## Slide 50
Cole & Bhadeshia, 1999

## Slide 51
20000
30000
40000
0
100
200
300
400
500
600
Life / hours
GTA weld at 823 K (data from Nippon Steel)
Cole & Bhadeshia, 1999

## Slide 52
Cole & Bhadeshia, 1999

## Slide 55
Pous, Lonardeli, Cogswell, Bhadeshia
Mat. Sci. Eng. A 567 (2013) 72

## Slide 57: International Fusion Reactor
Reduced activation steels:
design of experiments

## Slide 58: Modelling irradiation hardening
No strongly predictive model
Data by Yamamoto et al. and European RAFM database
~1800 data up to 90 dpa
  36 input variables
  No heat treatment information included

## Slide 59
Fusion reactor steels
Kemp, Cottrell & Bhadeshia, 2006

## Slide 61: Breast cancer: probability of relapse
tumor size
number of axillary lymph nodes
age
receptors (proteins activated by pro/estrogen)
DNA ploidy
S phase fraction
Ravdin, Clark
Breast Cancer Research & Treatment 22 (1992) 285
Notes: lymph nodes in underarm, responsible for draining lymph from breasts; DNA ploidy – DNA content per nucleus

## Slide 62: Breast cancer: probability of relapse
tumor size
age
estrogen receptor
Ravdin, Clark
Breast Cancer Research & Treatment 22 (1992) 285
Notes: lymph nodes in underarm, responsible for draining lymph from breasts; DNA ploidy – DNA content per nucleus 1.58 million papers