## Slide 1: Commercially viable strong steel with γ-grain size < 0.4 µm
www.phase-trans.msm.cam.ac.uk

## Slide 2
Solano, Bhadeshia
1C 1.5Cr wt%

## Slide 4
Fang, Yang, Liu, Song, Fang, Bhadeshia
Cannot easily be welded
0.76 C wt% +

## Slide 5
adapted from Materkowski, Krauss
Metall. Trans. A 10 (1979) 1643,
Kula, Anctil
Watertown Arsenal report AMRA TR 67-03
Fe-0.4C-0.73Mn-0.27Si-0.75Cr-0.25Mo-1.83Ni wt%
after tempering 200°C, < 3 J at -40°C

## Slide 6
Steel with difficult combination of properties
>2 GPa
30% ductility at conventional strain rates
ductility at very high strain rate
toughness and Charpy impact at -40°C
weldable
cheap, large in all dimensions
mass production
bank of properties

## Slide 7
martensite
Chatterjee & Bhadeshia

## Slide 8
Cracking of high-carbon martensite plates
Fe-1C-1.5Si-2Mn-1.3Cr-0.25Mo wt%
Chatterjee & Bhadeshia
Mat. Sci. Techn. 22 (2006) 645

## Slide 10
avoid impurity
embrittlement
grain size control
hardenability
normally, in quenched condition
Charpy < 10 J at ambient temperature

## Slide 11
Pous et al. (2014)

## Slide 12
Sourabh Kundu
Chintha et al.
Wear 428-429 (2019) 430-437

## Slide 13
Mathew Peet
finish rolling at low temperature

## Slide 14
Chart: Strain
| 1.6771488469601701E-4 | 9.919420171549051E-4 | 1.4876656586457801E-3 | 2.6488067630161399E-3 | 3.3117505550298901E-3 | 3.80747419652078E-3 | 4.4694285201882398E-3 | 5.2995924627248702E-3 | 5.7972950409083297E-3 | 6.2964818216112196E-3
 | 0 | 0.21386 | 0.32448 | 0.51622 | 0.63422 | 0.74484 | 0.87758 | 1.0029 | 1.0841 | 1.1431
 | 0 | 0.18437 | 0.25811 | 0.36136 | 0.48673 | 0.62684 | 0.73009 | 0.90708 | 1.0251 | 1.1283 | 1.2168 | 1.3496 | 1.4454 | 1.5339 | 1.6298 | 1.7035 | 1.7773 | 1.8289 | 1.8805 | 1.9469 | 2.0133 | 2.0649 | 2.1386 | 2.1608 | 2.1829 | 2.1976 | 2.1976 | 2.1755 | 2.146 | 2.1239


pancaked austenite, cooled
undeformed austenite quenched

## Slide 15
quenched, equiaxed austenite
cooled from pancaked austenite

## Slide 16
quenched from
equiaxed austenite
pancaked austenite
(magnification markers 100 µm

## Slide 17
Saurabh Kundu
thousands of orientations
in single austenite grain
only 24 orientations
in single austenite grain

## Slide 18
Tata Steel

## Slide 19
Fang, Yang, Liu, Song, Fang, Bhadeshia, Materials and Design, 50 (2013) 38
Cannot easily be welded
nanostructured bainite
Fe-1C-1.5Si-1.9Mn ... wt%

## Slide 20
12 mm
Single pass

## Slide 21
laser weld 1.2-2.7 kJ cm-1
no cracking

## Slide 22
gas tungsten arc & shielded metal arc welding

## Slide 23
Fracture toughness (KQ / MPa m1/2) of welded samples
Base metal
Coarse grained HAZ
Fine grained HAZ
Tempered HAZ
60
61
67
56

## Slide 24: Weld hardness profile
Mathew Peet

## Slide 25: High speed video
V0 = 445 m s-1
Survival
Vikram Deshpande, Mathew Peet

## Slide 26
Impact tumbler testing
Movie courtesy of K. Valtonen, V.-T. Kuokkala

## Slide 29
3-4 months of service

## Slide 30
1 year in service
6 mm thick

## Slide 31
04-05-2023
Installed May 2019.
Armour grade, sinter-fine return area of blast furnace.
Running successfully for 4 years without visible damage.
Previous, hard-faced steel lasted only 4 months before replacement
wear plate
Dust deposit

## Slide 32
Some microscopic cracks
04-05-2023
(4 years in service)

## Slide 33: 700 m s-1 , 2.5 mm thick, body-armour

## Slide 35
Desire fully martensitic structure following hot-rolling

## Slide 36
Mechanical stabilisation
Chatterjee S, Wang HS, Yang JR, Bhadeshia HKDH
Mechanical stabilisation of austenite
Materials Science and Technology 22 (2006) 641-644

## Slide 38
Mechanical stabilisation
Chatterjee S, Wang HS, Yang JR, Bhadeshia HKDH
Mechanical stabilisation of austenite
Materials Science and Technology 22 (2006) 641-644

## Slide 39
Austenitise, cool to generate bainite in deformed austenite

## Slide 40
Shipway & Bhadeshia
Mechanical stabilisation

## Slide 41: Useful at high-temperatures?
Can 17-7PH steel be treated similarly to improve toughness?
What about rolling load?

## Slide 42
2004