## Slide 1: Bainite
www.phase-trans.msm.cam.ac.uk
unanswered questions,
why they matter.

## Slide 2
Shibata & Maki
transformation twins

## Slide 3: 1972, 40 years after Davenport & Bain Metall. Trans. 3, p.1077
Hehemann: shear transformation,
growth rapid, carbon trapped in αb,
strain energy, carbide secondary .....
Kinsman, Aaronson:
non-lamellar eutectoid (carbide essential),
diffusion controlled,
ledge mechanism
“without participation of shear” .....

## Slide 4: debate on atomic mechanisms
reconstructive
displacive

## Slide 5: KTH Sweden
...... agree that bainite is formed through a displacive mechanism like martensite.
Metallurgical Transactions A 52 (2021) 4546
Controversy resolved?
Was this ever relevant?
... diffusive mechanism is supported ...
Hillert, ISIJ International 35 (1995) 1134

## Slide 6: Tetrataenite
Ferromagnetic
Large magnetic coercivity
Excellent permanent magnet
Ordering temperature 321°C
One atomic jump in 104 years at 300°C
cools 1 K in million years

## Slide 7: T. Ko, S. A. Cottrell (1952) J I S I 172 (1952) 307-313

## Slide 8
Pak, Suh, Bhadeshia
Metall. & Mater. Trans A 43 (2012) 4520
50 µm

## Slide 9: Mistake: acknowledge displacive but not consequences
....strain energy is “extremely small” when fraction of bainite small ....

## Slide 10: Nucleation – small sphere, homogeneous

## Slide 11: Mistake: acknowledge displacive but not consequences
Benrabah, Brechet, Hutchinson, Zurob: Scripta Materialia 250 (2024) 116182
No accounting for strain energy or why plate shape:
Fe-0.4C-1Si-1Mn wt%, 400°C

## Slide 12
Benrabah, Brechet, Hutchinson, Zurob: Scripta Materialia 250 (2024) 116182
As above + Purdy: Scripta Materialia 223 (2023)115076
``Zener-Hillert model can predict carbon supersaturation’’
... but no strain energy!!

## Slide 13: Errors in quoted equation for solid-solution strengthening
Eres-Castellanos et al.
2020
Scripta Mat. 250 (2024) 116182
Scripta Mat. 223 (2023)115076
Acta Mat. 268 (2024) 119791

## Slide 14
Fe-0.7C wt%
Grujicic, Zhou, Mat. Sci. Engng A 190 (1995) 87
Peierls barrier for austenite
Benrabah, Brechet, Hutchinson, Zurob Purdy
Scripta Materialia 223 (2023)115076

## Slide 15
Olson, Cohen
1979

## Slide 16: perturbations in diffusion field leading to
Acta Metallurgica 29 (1981) 1117

## Slide 17: orientation relationships
fundamental condition for displacive transformation

## Slide 18: orientation relationships
real orientation relation is irrational

## Slide 19
Materials Science and Engineering: A
528, Issues 29-30, 8492
near induction weld
base material

## Slide 20: Continuity (of growth) ?
e.g., Hillert, Purdy
Acta Metall. 32 (1984) 823
Hillert: Swedish Institute for Metals Research, 1960
0 strain energy

## Slide 21: Continuity
strain energy should not be neglected
growth rate measured at
appropriate resolution
X/Fe ratio constant at atomic resolution
no possibility of “solute drag”

## Slide 22: universal nucleation function

## Slide 25
MUCG46

## Slide 26: Bainite nucleates predominantly at austenite grain faces
Jimbo & Nambu: Metals 13 (2023) 355

## Slide 27: Solute drag
Controversy resolved?
Benrabah, Brechet, Hutchinson, Zurob
Scripta Materialia 250 (2024) 116182
“drag neglected due to high velocities for bainite”

## Slide 28
Bhadeshia HKDH, Waugh AR. Bainite: An atom-probe study of the incomplete reaction phenomenon. Acta Metallurgica. 1982;30:775-84.

## Slide 31
Growth is diffusionless
but plate decarburised shortly afterwards
Lin, Borgenstam, Stark, Hedström.
Materials Characterization 185 (2022) 111774

## Slide 32
Liu, Miyamoto, Yang, Zhang, Furuhara
Metall. Mat. Trans. A 46 (2015) 1544

## Slide 33
Carbon
Manganese
a
g
a+g
a
g
High supersaturation
NP-LE mode
a
g

## Slide 35
Swallow, Bhadeshia
Materials Science and Technology. 12 (1996) 121

## Slide 37
Photoemission electron microscopy
3 orders of magnitude faster than carbon diffusion-control
growth rate?

## Slide 38
Acoustic emissions ....
Courtesy of Francisca Garcia Caballero
... from bainite

## Slide 39
Shipway & Bhadeshia 1995
only displacive transformations
stabilized by plastic deformation
of austenite
lot of αb
mostly α’

## Slide 40
478°C for 43 days – bainite completed in seconds. Bhadeshia (1981)
reconstructive transformation
6000 times slower

## Slide 41
Bhadeshia, Met. Sci. (1982)

## Slide 42
Bhadeshia, Waugh
Acta Metall. 30 (1982) 775

## Slide 43
dislocation
Time during transformation at 200°C / hours
Caballero, Miller, Mateo, Cornide. J. Alloys & Compounds, (2012)
carbon concentration in solution in ferrite
Fe-1C-1.5Si-1.9Mn-1.3Cr-0.26Mo-0.1V wt%
Acta Mat. 91 (2015) 162

## Slide 44
Jang, Suh, Bhadeshia, Scr. Mat. 68 (2012) 195

## Slide 45
Hulme-Smith, Lonardelli, Dippel and Bhadeshia, Scr. Mat. 69 (2013) 409.
transformed to
bainite at 200°C →25°C
then heated from
25→600°C at 300°C h-1

## Slide 48
TRIP-assisted

## Slide 49: Challenge
Does your theory explain all observations?
Has it been used independently in design?
.... in manufacture?
.... in critical experiments?
prove me wrong!
reconstructive
displacive

## Slide 50
www.phase-trans.msm.cam.ac.uk

## Slide 51: Low entropy conference