## Slide 1: Aspects of pearlite
“I described as pearly. ..... fine straight lines or curved parallel lines alternating thin plates of varying hardness..... iron free from carbon, and the intensely hard substance..”
Sorby (1887)
CC-BY-NC

## Slide 2
1883 condition of carbon in steel, ≅ Fe3C
1883 ⇒ Sorby, first metallography
1888 Howe names cementite, ferrite and austenite
1903 Howe in letter to Sauveur, eutectoid

## Slide 3: Cementite: primitive crystal structure

## Slide 4: Three-dimensional structure of pearlite
E. C. Bain

## Slide 5
Three-dimensional image of θ-lamella, serial sectioning.
Courtesy of Yoshitaka Adachi.

## Slide 6
colony
nodule

## Slide 7: Alexander, Bernstein Metallurgical Transactions A 13 (1982) 1865
Behera et al. Materials Science & Engineering A 764 (2019) 138256
Zhou et al. Mat. Charc. 119 (2016) 110-113

## Slide 8: Intelamellar spacing

## Slide 9: Manabu Takahashi, Ph.D. thesis
Fe-C-1.08Mn
Fe-C-1.98Ni
Fe-C-3.00Ni
Fe-C-1.80Cr
Fe-C-0.90Cr
Fe-C-0.40Cr
Fe-C-9.00Cr wt%

## Slide 10: TE of alloy steels?

## Slide 11: SI independent of carbon concentration?
Fe-C-0.5Mn-0.2Si wt%, Materials Sci. & Techn. 18 (2002) 1317

## Slide 12: Zhang & Enomoto ISIJ Int. 49 (2009) 921
Fe-0.82C-0.71Mn-0.23Si wt%
700°C

## Slide 13: Commercial eutectoid steel, Apparao Chintha

## Slide 14: Banded steel (segregation also in fully pearlitic alloys)
Courtesy of Y. Mutoh
Thompson, Howell, Materials Sci. Techn. 8 (1992) 777

## Slide 18
Zhang, Enomoto, ISIJ International, 49 (2009) 921
Kaiming Wu
Wuhan University of Science and Technology

## Slide 19
Cementite 1000 HV
Ferrite 250 HV

## Slide 20: Stress to initiate plasticity sensitive to interlamellar spacing
“Hall-Petch relation …. by no means completely verified”
“equally good”
Page 230

## Slide 21: Other problems
Dollar, Bernstein, Thompson
Acta Metallurgica
36 (1988) 311

## Slide 22: Nakada et al.
strength & SI spurious correlation
α/θ misfit strains α, in proportion to 1/ SI
pearlite yielding begins in α
therefore, strength varies with 1/ SI
misinterpretation
of line broadening

## Slide 23: Theories: Langford
Dislocations pass through and shear cementite

## Slide 24: Dislocation bowing between rigid cementite

## Slide 25: Theories: Hall-Petch

## Slide 27
Thin film theory
Order of magnitude smaller than expected from theory

## Slide 28: Semiconductors: relaxation of epitaxial layer deposited on a substrate

## Slide 29: Hall-Petch

## Slide 30: Bayesian analysis

## Slide 31: Solid solution effects
Data due to Fu, Furuhara

## Slide 32: Why controversy about Hall-Petch? … friction stress in ferrite negative intercept

## Slide 33: Overfitting of noisy data

## Slide 34: Comparison of nanostructure ferrite with pearlite
Data points: Tsuji et al.
Scr Mat 46 (2002) 893

## Slide 35: Data can be downloaded from
www.phase-trans.msm.cam.ac.uk/2022/HP.xlsx
Critical assessment: the strength of undeformed pearlite
Materials Science and Technology, 2022
DOI: 10.1080/02670836.2022.2079295

## Slide 36
Scripta Materialia 52 (2004) 461
Minoru Umemoto
head-hardened pearlitic rail 420 HV

## Slide 37: Ductility of cementite (θ)
At 300 K, polycrystalline θ: zero ductility in uniaxial compression
Terashima et al. Scr. Mat. 54 (2006) 1925
Minoru Umemoto
Aparna Singh
Cracking immediately
after tensile yielding of ferrite

## Slide 38: Hydrostatic pressure, ductility
Bridgman, Rev. Modern Phys 17 (1945) 3
“1045 steel”
limits cracks, may even seal them,
opposes void formation associate with ΔV ↑

## Slide 39: Wire drawing: also generates hydrostatic stresses
Oh, Trans. Korean Soc. Mech. Engng.
5 (1981) 170

## Slide 40: Wire drawing

## Slide 41: Wire drawing
cross section

## Slide 42: Wire drawing

## Slide 43
Hosford: fibre-textured samples would develop elliptical grains; strain compatibility would force grains to curl around each other

## Slide 44: Electropulsing
Images courtesy
Rongshan Qin