## Slide 1: The metal fragment and the Cuffley Airship
www.phase-trans.msm.cam.ac.uk

## Slide 2
Cuffley is not far from London, nor from the Channel
1916
Population

## Slide 3
Airship raids killed > 500
injured >1000
(https://www.bbc.co.uk/news/uk-england-27517166)
2003 invasion of Iraq
654,965 excess deaths
2.5% of population
(The Lancet, 2006)

## Slide 4
reproduced with permission of Cllr Peter Dace, Northshaw & Cuffley Parish Council
https://northawcuffleypc.org.uk/w-l-robinson-vc/
SL 11 airship under construction.
Approximate data:
174 m in length
20 m diameter
40000 m3 of H2
Payload = 21000 kg

## Slide 5: Fuel + oxygen + spark = fire
simply firing bullets at airship did not set them on fire in spite of the hydrogen within
combination of incendiary and explosive bullets necessary

## Slide 6: Lieutenant William Leefe Robinson 39th squadran, Royal Flying Corps
reproduced with permission of Cllr Peter Dace, Northshaw & Cuffley Parish Council
https://northawcuffleypc.org.uk/w-l-robinson-vc/
first to shoot down an airship on British soil
2/3 September 1916
2 days later, awarded the Victoria Cross

## Slide 7
reproduced with permission of Cllr Peter Dace, Northshaw & Cuffley Parish Council
https://northawcuffleypc.org.uk/w-l-robinson-vc/
Royal Flying Corps personnel examining the debris from the

## Slide 8
reproduced with permission of Cllr Peter Dace, Northshaw & Cuffley Parish Council
https://northawcuffleypc.org.uk/w-l-robinson-vc/
Royal Flying Corps personnel examining the engine from the

## Slide 9
reproduced with permission of Cllr Peter Dace, Northshaw & Cuffley Parish Council
https://northawcuffleypc.org.uk/w-l-robinson-vc/
Wooden frame completely burnt, but reinforcing wire and metal from the gondolas and engine, recovered.

## Slide 10: encounter with Michael Cook
about 3 cm in length
Darwin College

## Slide 11: Unlike myself, Michael is an infrequent visitor for lunch at Darwin College. So he had been carrying the fragment for some time, tucked away in his jacket, until we finally met by chance and introduced ourselves.
The fragment was acquired originally by Michael’s mother’s uncle, apparently the first shooting down of an airship over Cuffley.

## Slide 14: corrugated for engineered rigidity

## Slide 15: Duralumin
an aluminium-(10Cu wt%...+Mg, Mn) alloy invented and patented by Alfred Wilm, a Berlin Chemist, in 1906
First produced in Düren (Prussian territory), hence, Duralumin (pronuounced douralumin)
Heat it to say 500°C, quench, leave. It hardens at room temperature over a period of days

## Slide 16
solution

## Slide 18: Microscopy & microanalysis
Ph.D. student, University of Cambridge
now at Tata Steel Laboratories, Jamshedpur, India

## Slide 19: Microanalysis
Aluminium contains copper, magnesium and silver additions

## Slide 20: Two manufacturers of airships
Duralumin rigid-metal framework
several gas bags within
Wooden rigid-framework
metal components, several gas bags within

## Slide 21: Cuffley airship was SL11, not Zeppelin
“Duralumin .. used exclusively in Zeppelin Airships”, Cllr Peter Dace
“this is a fragment of typical Zeppelin framework, if local, it can only be from L31”, Raymond Rimell, author of The Airship V.C.
“Long conversation with Michael Cook, who is adamant that the piece is from the SL11, based on many family conversations over a long period of time”, Harry Bhdeshia

## Slide 22: Imperial War Museum, Martin Anthony, Assistant Curator (First World War)
SL11. Being of wooden construction, very little was left after it burnt apart from a great deal of wire. Early press reports.... rings and bangles being made from the wire sold to raise money for the Red Cross. .... Cuffley became a popular place to visit. To satisfy visitors and to raise more money, I gather that the wreckage of other airships was also displayed at the Cuffley site when they were shot down in the following weeks or months (possibly including L31 and L32).
.... souvenirs from these other airships were also sold there. If Michael Cook’s mother’s uncle visited the Cuffley site more than three weeks after SL11 crashed, it is very possible that he saw some wreckage from a different airship that was made from duralamin.
For a long time there was some confusion about the identity of the airship shot down by William Leefe Robinson. I think this was probably caused by the displaying of other airship fragments at Cuffley.

## Slide 23: Professor Wolfgang Bleck, Aachen University
searched the German Archives

## Slide 24
basic construction in wood
gondolas in steel

## Slide 25: dissertation, University of Mannheim, 1987, by Dorothea Haaland, p. 253
SL11 construction completed August 1916
Between 24th, 31st August, two trips attempted to England but ended prematurely
On 2nd September 2000 kg of bombs dropped on London, then shot down.

## Slide 26
Bob Waugh

## Slide 27
Bob Waugh

## Slide 28
Bob Waugh
Thank you.