## Slide 2
Дмитрий Константинович Чернов

## Slide 3
Nikolai Timofeevich Beliaev
Lectures at the Royal College of Mines
London, 1922
Damascus steel,
crystallisation,
Widmanstaetten structures,
steel making.
STEREOLOGY

## Slide 4: Disease

## Slide 5: “Hultgren” extrapolation
Beliaev
Journal of the Iron and Steel Institute
105 (1922) 201-227

## Slide 6
Floris Osmond, 1888, chuffage, refroidissment

## Slide 7
Two lectures on steel: first lecture
Proc. Inst. Mech. Engng.
80 (1911) 241-275
Walter Rosenhain
Cementite
6.01-7.38 Cwt%
Muller 1878
Fe3C
Abel et al. 1883
Notes: incorrect idea that β-iron (the non-magnetic form of α-iron above 770∘C) was an amorphous phase
At the boundaries, where grains of different orientation meet, there must be a neutral zone— a kind of “ no man’s land ”—where the crystal¬ line matter cannot assume the orientation of either of the grains.
This thin layer of crystalline matter, which is considered by Rosenhain as in an " amorphous ” state (20) would seem predestined to facilitate the appearance of the nuclei of the secondary depositions.

## Slide 9
He, Daniels, Brown, Brydson, Edmonds
2007

## Slide 11
not sacrosanct

## Slide 12: Temper martensite in Fe-C

## Slide 14
Bhadeshia, Chintha, Lenka
(2019)
Cementite always
most stable phase
Other carbides absent at low carbon conentrations

## Slide 15: Peritectoid reaction
S V Davydov
Steel in Translation
2023

## Slide 16
Bhadeshia, Waugh
Acta Metall. 30 (1982) 775

## Slide 17
dislocation
Time during transformation at 200°C / hours
Caballero, Miller, Mateo, Cornide. J. Alloys & Compounds, (2012)
carbon concentration in solution in ferrite
Fe-1C-1.5Si-1.9Mn-1.3Cr-0.26Mo-0.1V wt%
Acta Mat. 91 (2015) 162
persistent carbon!

## Slide 18
Jang, Suh, Bhadeshia, Scr. Mat. 68 (2012) 195

## Slide 19
Hulme-Smith, Lonardelli, Dippel and Bhadeshia, Scr. Mat. 69 (2013) 409.
transformed to
bainite at 200°C →25°C
then heated from
25→600°C at 300°C h-1

## Slide 21
one interstice per
iron atom
three interstices per
iron atom
x
x
x
x

## Slide 22
Conclusions