## Slide 1: Kinetics of niobium carbide precipitation
www.phase-trans.msm.cam.ac.uk

## Slide 2: Equilibrium
50.12 Nb, 49.88 C at. %

## Slide 3
Journal of Japan Institute of Metals 35 (1971) 1089
CALPHAD 29 (2012) 62
Mn ↑ [Nb][C] in γ

## Slide 4
Smaller particles of mercuric oxide dissolve and their material redeposits on to larger ones, due to surface tension [interfacial energy]
Average size of `solid bodies’ increases

## Slide 5: “Capillarity”
Small particle dissolves, large particle grows.
Total number of particles decreases.

## Slide 6: Concept of local equilibrium

## Slide 7: Concentrations at δ (NbC) / ϒ (austenite) junction
carbide absorbs Nb, C
austenite depletes in Nb, C

## Slide 10
NbC
austenite

## Slide 11: Precipitation
Nucleation
Growth
Impingement

## Slide 12
nucleation
+growth
+impingement = fraction
Fe-0.1C-0.05Nb wt%, 900°C

## Slide 13
Wilhelm Friedrich Ostwald
Geofrey Wilson Greenwood

## Slide 14: AERE UK: nuclear reactor in which fuel is fluid, helps heat extraction
Geoffrey Greenwood: uranium suspended in bismuth+Pb+Sn
blocking, agglomeration etc.
However, observed coarsening of particles isothermally.
Developed first theory based on Ostwald to treat a pattern of diffusion fluxes.
Lifshitz, Wagner, Slyozov
Biographical Memoirs of Fellows of the Royal Society. 2024 Apr 1;76:221-40.

## Slide 15
Small particles dissolve
Large particles grow
Area fraction ≅ constant
Number density decreases

## Slide 16
time = t
time = t+∆t
a

## Slide 17
Coarsening follows
naturally

## Slide 18
time = t
time = t+∆t
a
b

## Slide 20: Interfacial energy per unit area
Jang, Kim
Scripta Mat. 243 (2024) 115967
0.06C-1.54Mn-0.2Si-0.0Al-0.07Nb,-0.04 V wt% 700°C, 5, 8, 11, 13 min ➔
Radis, Kozeschnik
Mod. Sim. Mat. Sci. Engng. 20 (2012) 055010

## Slide 21: Pure Nb/cast-iron interface, annealed 1172°C
Bai, Zhong, Wei, Lv, Xu, Mat. Sci. Techn. 36 (2020) 1749
Notes: It is not just the dislocation density that varies – topology of boundaries, deformation bands etc

## Slide 22: MatCalc, etc.
Radis, Kozeschnik
Mod. Sim. Mat. Sci. Engng. 20 (2012) 055010
Radis, Kozeschnik
Mod. Sim. Mat. Sci. Engng. 20 (2012) 055010

## Slide 23: Use models creatively
Make predictions
Validate those predictions with your own experiments
Validate on all published data

## Slide 24
Best way forward?
2104
Notes: Theoretical minimum

## Slide 26
Paul Hill, Rolls-Royce

## Slide 27
www.phase-trans.msm.cam.ac.uk