A Computer Program for the Calculation of

TTT Diagrams for the Growth and Dissolution of

Oxide, Nitride and Sulfide Inclusions

Version 1.0

March 2000

T. Hong and T. DebRoy

Department of Materials Science and Engineering

The Pennsylvania State University

CONTENTS

#### Introduction 										2

#### Calculation procedure									2

Equilibrium concentrations at the interface					3

TTT diagrams for the growth of inclusions					5

TTT diagrams for the dissolution of inclusions				6

# User guide										7

# Structure of the source code 								11

# Reference										15

##### Appendix A: Default values								16

##### Appendix B: Nomenclature								18

###### Appendix C: Source code								21

Introduction

The time-temperature-transformation (TTT) diagrams provide a road map to understand the growth and dissolution behavior of inclusions in liquid steels. In particular, the diagrams describe the effects of time and temperature on the growth and dissolution behavior of a particular inclusion in an alloy of known composition. Oxides, nitrides and sulfides are the most common inclusions in steels. This document describes a computer program for the calculation of TTT diagrams for fourteen types of oxide, nitride and sulfide inclusions. The calculations take into account the nucleation rates of inclusions and their subsequent growth or dissolution rates that are calculated considering the diffusion of various species toward or away from the inclusion/liquid alloy interface. Further details about the calculations and a set of computed results are available in reference 1.  This document contains a description of the calculation procedure and the computer program used for the calculations.

Calculation Procedure

The following assumptions were made to simplify the calculations:

- The concentration field near each inclusion was assumed to be constant during the growth or dissolution of the inclusions.

- Heterogeneous nucleation of inclusions was considered in the calculations.

- The activities of liquid iron and all solid compounds were assumed to be unity.

- At the interface between the inclusion and the liquid steel, only the concentrations of those elements that make up the inclusion were calculated. The concentrations of other elements were assumed to be the same as that in the bulk metal.

The construction of the TTT diagrams requires calculation of the rates of diffusion of various species near the inclusion/alloy interface. These rates depend on the difference between the concentrations of various species in the bulk alloy and those at the interface.  For a known alloy composition and temperature, the interfacial concentrations can be calculated assuming equilibrium at the interface as described below:

Equilibrium concentrations at the interface

The following reaction is considered at a constant temperature at the interface between an inclusion and liquid steel:

xM+yQ=MxQy          				(1)

where M stands for a metallic element such as Al, Ni, Mn, Si, Fe, or Ti, and Q stands for a nonmetallic element, such as O, N, or S.

The standard free energy for this reaction, G0 is given by:

DG0=-RTlnkeq  					(2)

or, 				keq=e−DG0RT						(3)

where keq is the equilibrium constant defined as:

keq=aMxQyaMxaQy=1[fMcMi]x[fQcQi]y      				(4)

where aMxQy, aM, and aQ are the activities of MxQy (equal to 1), M and Q, respectively, cMi and cQi are the equilibrium concentrations of M and Q expressed in weight percent at the interface between the inclusion and the metal, and fM and fQ are the activity coefficients of M and Q given by:

fi=10j=1neijcji               				(5)

where eij is the first order interaction parameter between element i and j, cji is the concentration of element j at the interface.  From the stoichiometrical formula, the following equation can be derived:

cMi=cMb−xmMymQ(cQb−cQi)                			(6)

where cMb and cQb are the  original concentrations of  M and Q in the bulk metal  and mM and mQ are the atomic weights of M and Q.

For a given temperature, we can solve for the two interfacial concentrations, cMi and cQi using equations (4) and (6) following the steps below:

- The value of keq is calculated from equation (3) for a given temperature. The initial values of cMi and cQi are assumed.

- Substitute values of cMi and cQi in equation (5) to obtain the corresponding values of fM and fQ.

- Using the calculated values of fM and either the assumed or the calculated value ofcMi, the value of aM is calculated from the following relation: aM=fMcMi

- The value of aQ is calculated from equation (4) for known values of aM and keq. A new value of cQi is calculated by cQi=aQfQ.

- A new value of cMi is calculated by substituting the new cQi in equation (6).

- With the new values of cMi and cQi, calculations are repeated starting from step 2 until the new values of cMi and cQi are close enough to their old values.

When a complex inclusion such as MnOAl2O3  is considered, the equations to be solved are somewhat different:

x1M'+x2M''+yQ=Mx1'Qy1Mx2''Qy2			(7)

where M' and M''stand for the two metallic elements, Q stands for a nonmetallic element, and y is equal to y1+y2. The equilibrium constant for equation (7) is given by:

keq=aMx1'Qy1⋅Mx2''Qy2aM'x1aM''x2aQy=1[fM'cM'i]x1[fM''cM''i]x2[fQcQi]y=e−ΔG0RT		(8)

The interfacial concentrations of  M''and Q are related to their corresponding bulk values by the following relations based on stoichiometric considerations:

cM''i=cM''b−x2mM} } }  over  {x rSub { size 8{1} } m rSub { size 8{M'} } } }  \( c rSub { size 8{ { {M}} sup { ' }} }  rSup { size 8{b} }  - c rSub { size 8{ { {M}} sup { ' }} }  rSup { size 8{i} }  \) } {    				(9)

cQi=cQb−ymQx2mM} } } }  \( c rSub { size 8{ { {M}} sup { '' }} }  rSup { size 8{b} }  - c rSub { size 8{ { {M}} sup { '' }} }  rSup { size 8{i} }  \) } {					(10)

where cM'i, cM''i and cQiare the equilibrium concentrations of M', M'' and Q at the interface expressed in weight percent, cM'b, cM''b and cQb are the concentrations of M', M'' and Q in bulk and mM', mM'', and mQ are the atomic weights of M', M'' and Q. We can solve equations (8) to (10) to obtain for three interfacial concentrations, cM'i, cM''i and cQi needed for the calculations of diffusion rates.

TTT diagrams for the growth

Using the calculated cQi, we can calculate2 the growth rate α by:

α=2D0(cQb−cQi)(cQp−cQi)=2D0c			(11)

where Do is the diffusion coefficient of nonmetallic element in the liquid metal, c=(cQb−cQi)(cQp−cQi), cQp is the concentration of nonmetallic element in weight percent in the inclusion particle which can be calculated as: cQp=100(y×mQ)x×mM+y×mQ% for simple compounds or cQp=100(y×mQ)x1×mM'+x2mM} } +y times m rSub { size 8{Q} } } } %} { for complex compounds .

The homogeneous nucleation rate Iv can be calculated3 using the following equation:

Iv=Ae−ΔGhomk0T=Ae−16πσ3Vm23k0TΔG2				(12)

where DGhom is the activation energy for homogeneous nucleation of the inclusion considered, A is a constant, k0 is the Boltzmann constant,  is the interfacial energy, Vm is the molar volume of the inclusion, and G can be calculated by:

ΔG=ΔG0+RTln(aMxNyaMxaQy)=ΔG0+RTln[1(fMcMb)x(fQcQb)y]		(13)

The nucleation rate will be further enhanced if the heterogeneous nucleation mode is operative. The expression for heterogeneous nucleation Ihet is given by:

Ihet=Af(θ)16e−ΔGhetk0T						(14)

where A is a constant, ΔGhet is the activation energy for heterogeneous nucleation, and  is the contact angle between inclusion free surface and substrate nucleation phase. The value of ΔGhet and f() are given by:

ΔGhet=f(θ)ΔGhom						(15)

f(θ)=14(2+cosθ)(1−cosθ)2				(16)

For the overall reaction kinetics, the extent of transformation  as a function of time t is given by2:

ζ=1−e−8Ihetπα3t5215c				(17)

This equation can be rewritten as:

t=−15cln(1−ζ)8Ihetπα325			(18)

Since we have calculated the values of cQi, Ihet and α, we can get the corresponding time t at temperature T for any given value of  .

TTT diagrams for the dissolution

The dissolution rates of small spherical inclusions are assumed to be limited by the transport of nonmetallic elements in the alloy. For the dissolution of the inclusions, the solution of the diffusion equation with stationary interface approximation was considered. By considering the Laplace approximation for short times, a simple approximate solution was obtained4:

r0−r=−k2D0r+DoπtΔt				(19)

where r is the instantaneous radius of the inclusion before every time step, r0 is the radius of the inclusion after the timestep, t is the growth time after nucleation, D0 is the diffusion coefficient of Q in the bulk, r is the change of inclusion radius, t is the time step, and k is defined as k = -2c*.

The time needed to decrease the particle size to a certain value, for example, 1% of the initial radius at different temperature can be calculated from equation (19). This calculation is used to construct the TTT diagrams for dissolution of an inclusion.

User’s Guide

This window-based executable program is very easy to use in PCs. The user just needs to select options presented in the various dialog boxes.

- Start up

To run the executable file, tttdi.exe, under windows environment, the user does not need to have any other compiler or graphics program. To run this program, double click its icon and a ‘Welcome’ window shown below will pop up. Just click the ‘Start’ button to start the calculations.

- Select an inclusion

The user is required to select only one inclusion at a time. A selection of fourteen inclusions are available in this program as shown below. However, the user can provide appropriate data for other inclusions.

3. Change default values

In the frame shown below, user can revise four groups of default values.

1.  Selection of alloy composition:

Steels containing the ten elements shown in the above frame are considered here. Their concentrations may be selected by the user. The default values5 are presented in Table 1 of Appendix A.

2. The standard free energy data:

The standard free energy for the formation is expressed as ΔG0=a+b⋅T.  The values of  a and b for the inclusion selected can be changed if necessary. The default values6 of a and b are presented in Table 2 of Appendix A

3. Kinetic data:

The following constants used in the calculations can be changed: a) diffusion coefficient, D0, of the nonmetallic elements in equations (11) and (19), b) interfacial energy, , in equation (12), c) and d) minimum and maximum temperatures for plotting TTT diagram for inclusion formation, e) the extent of precipitation, , in equations (17) and (18), which equals to 0.01 when the precipitation starts and equals to 0.99 when the precipitation is over, f) the initial inclusion radius for dissolution, r0, g) the assumed final inclusion radius for dissolution calculation, rf and h) the contact angle, , between the free surface of inclusion nuclei and substrate phase. The units of these constants are presented in the dialog box.

4. Output data file names

The output data filenames for both growth and dissolution are selected. The default names are ‘grow.dat’ and ‘diss.dat’. The data files contain computed temperature versus time data and equilibrium concentrations versus temperature data for the inclusion selected.

User can go back to the ‘Inclusion Considered’ frame by clicking on the button ‘Back’ or to the ‘Interaction Parameters’ frame by clicking on the button ‘Revise Interaction Parameters’. If all data modification is done, user can click on the button ‘Calculate’ to start calculation.

4. The first order interaction parameters

The first order interaction parameters eij for all the elements are taken from reference 4.  These values have been assumed to be independent of temperature.  However, these values can be changed if more accurate values become available.  The default value7 are presented in Table 3 of Appendix A.

- Display calculated results

The first graph will be the TTT diagram for the formation of the inclusion selected. A typical diagram is shown below.  The temperature scale can be selected by the user.

Press ‘Enter’ to display the TTT diagram for the dissolution of the inclusion. The initial (R0) and final(Rf) inclusion radi and the equilibrium temperature are displayed in the figure.

Press ‘Enter’ again and a dialog box will come out and ask you if you want to do another calculation. Make your selection.

Structure of the source code

###### Main program

The source code is compiled in Digital Visual Fortran as a QickWin project. It consists of a main program and several subroutines and functions. A flow chart of the FORTRAN code is shown below:

At the beginning, a welcome window is displayed.  This is followed by a frame for the selection of inclusions. Before the calculation of TTT diagrams, a subroutine ‘getstart’ is called to modify the default calculation parameters.

call getstart(	formf,dissf,con,tmin,tmax,sigma,d00,

1zeta,r0,rf,gaa,gbb,eij,theta)

The variables are explained in Appendix B. In the program an inclusion is defined by an index, nincl.  When its value is less than 10, the inclusion is a simple compound whereas a higher value designates a complex inclusion.

if (nincl.le.10) then

.

endif

if(nincl.gt.10) then

.

endif

The chemical formula of the compound and the atomic weights of its constituents are then defined.

x=xx(nincl)

y=yy(nincl)

q=qq(nincl)

m=mm(nincl)

amm=am(m)

amq=am(q)

At any given temperature, a function ‘aiv’ (‘aiv2’ for complex oxide) is called to calculate the heterogeneous and homogeneous nucleation rates.

vhetiv=aiv(temp,theta,con,x,y,eij,nincl,m,q,gaa,gbb,dg,homiv)

Furthermore, a subroutine named ‘equcon’ (‘equcon2’ for complex oxide) is called to calculate the equilibrium concentration of M and Q at the interface, cmi and cqi, respectively at a given temperature:

call equcon(m,q,eij,akeq,x,y,con,cmi,cqi,amm,amq)

At the equilibrium temperature, the concentration of Q at the interface is equal to that in the bulk alloy. The inclusion begins to dissolve above this temperature and calculations are performed for inclusion dissolution. Below this temperature, calculations  are performed for inclusion growth.

if (cni.lt.cnb) then

.

else

.

endif

The program calculates the TTT diagram for formation from equation (18) and dissolution from equation (19) and writes the results in two data files by following commands:

cstar=(cqb-cqi)/(cqp-cqi)

if (cqi.lt.cqb) then

alpha=sqrt(2.*d00*cstar)

t=((-15.*cstar*log(1.-zeta))/(8.*(hetiv+small)*pi*

1			alpha**3))**0.4

if(t.lt.told) goto 30

write(20,1)temp,t,hetiv,homiv,cqi,cmi,cstar,dg/1000.

1			format(f6.1,3(e15.6e3),f11.7,f11.7,e14.6e2,f11.3)

told=t

else

if(ic.eq.0) then

write(21,6)temp,10.,cqi,cmi,0.,0.

equtemp=temp

ic=1

endif

ak=-2.*cstar

rr=r0

do 60 time=dt,10.,dt

rr=rr-ak*d00*dt/(2*rr)-ak*sqrt(d00*dt/pi)/2.

if (rr.lt.rf) goto 70

60			continue

70			write(21,6) temp,time,cqi,cmi,cstar,dg/1000.

6			format(f6.1,e15.6e3,f11.7,f11.7,e13.4e3,f11.2)

endif

The computed results for the formation and the dissolution of the oxides are stored in two output files. Their filenames (grow.dat and diss.dat) are stored in two string variables formf and dissf.

grow.dat:

Al2O3            47.05882  52.94118   0.08400   0.02600

Temp,time,Ivhet,Ivhom,cqi,cmi(wt%),c*,dg(kj/mol)

1600.0  0.187078E-008  0.631768E+033  0.572538E+033  0.0608890  0.0000001  0.491746E-03   -326.046

1601.0  0.187088E-008  0.631685E+033  0.571656E+033  0.0608890  0.0000001  0.491746E-03   -325.495

1602.0  0.187098E-008  0.631603E+033  0.570772E+033  0.0608890  0.0000001  0.491746E-03   -324.944

1603.0  0.187108E-008  0.631520E+033  0.569884E+033  0.0608890  0.0000001  0.491746E-03   -324.392

1604.0  0.187117E-008  0.631437E+033  0.568993E+033  0.0608890  0.0000001  0.491745E-03   -323.841

.	.	.	.	.	.

.	.	.	.	.	.

diss.dat:

Al2O3            47.05882  52.94118   0.08400   0.02600

Temp,time,cqi,cmi(wt%),c*,dg(kj/mol)

2192.0  0.100000E+002  0.0843491  0.0263928  0.0000E+000       0.00

2192.0  0.493313E+001  0.0843491  0.0263928 -0.7432E-005       0.38

2193.0  0.196971E+001  0.0848754  0.0269849 -0.1864E-004       0.93

2194.0  0.121359E+001  0.0854210  0.0275986 -0.3025E-004       1.48

2195.0  0.867632E+000  0.0859872  0.0282356 -0.4231E-004       2.03

2196.0  0.669599E+000  0.0865756  0.0288976 -0.5483E-004       2.58

2197.0  0.540877E+000  0.0871880  0.0295865 -0.6787E-004       3.13

2198.0  0.450677E+000  0.0878264  0.0303047 -0.8146E-004       3.68

2199.0  0.383886E+000  0.0884931  0.0310547 -0.9566E-004       4.24

.	.	.	.	.	.

.	.	.	.	.	.

The first lines in these two files state the type of the inclusion, the concentrations of Q and M in the inclusion particle and concentrations of Q and M in the liquid metal, respectively. In the data file formf, there are eight variables output. They are temperature, time needed to finish the preset extent of precipitation at this temperature, heterogeneous nucleation rate and homogeneous nucleation rate at the temperature, equilibrium concentrations of Q and M at interface, c* in equation (11) and G in equation (13). In the data file dissf, there are six variables output. They are temperature, time needed to finish the preset extent of dissolution at this temperature, equilibrium concentrations of Q and M at interface, c* in equation (11) and G in equation (13).

###### Subroutine getstart

This subroutine displays two dialog boxes and asks the user to modify the values of various parameters interactively.

###### Subroutines equcon and equcon2

These two subroutines calculate the equilibrium concentrations of the constituent elements at the interface. When m = 0, the metallic elements in the inclusion is iron. This situation is dealt with by following commands separately:

if (m.eq.0) then

do 450 ii=1,10

fq=0.

do 460 i=1,me

if (i.eq.q) goto 460

fq=fq+con(i)*eij(q,i)

460			continue

fq=fq+cqi*eij(q,q)

fq=10.**fq

cqi=((1/akeq)**(1./float(y)))/fq

- continue

endif

To achieve rapid convergence, when the concentration of the metallic element in the bulk is higher than that of the nonmetallic element, the value of cqi, is calculated first, and vice verse. This calculation is achieved by following commands:

do 430 ii=1,10

fm=0.

fq=0.

do 420 i=1,me

if (i.eq.q.or.i.eq.m) goto 420

fm=fm+con(i)*eij(m,i)

fq=fq+con(i)*eij(q,i)

420			continue

fm=fm+cqi*eij(m,q)+cmi*eij(m,m)

fq=fq+cqi*eij(q,q)+cmi*eij(q,m)

fm=10.**fm

fq=10.**fq

if(con(m).gt.con(q)) then

actm=fm*cmi

actq=(1./(akeq*(actm**float(x))))**(1./float(y))

cqi=actq/fq

cmi=con(m)-float(x)*amm*(con(q)-cqi)/(float(y)*amq)

endif

if(con(m).lt.con(q)) then

actq=fq*cqi

actm=(1./(akeq*(actq**float(y))))**(1./float(x))

cmi=actm/fm

cqi=con(q)-y*amq*(con(m)-cmi)/(x*amm)

endif

- continue

###### Functions aiv and aiv2

These two functions calculate the nucleation rates at different temperatures in liquid metal for simple compounds and complex oxides. The formation free energy change is calculated from equation (13) by the command:

dg=dgz(temp,gaa,gbb)-1.98*temp*log((abs(actm)**x)*(abs(actq)**y))

The nucleation rates are calculated from equations (14) to (16) by following commands

fm=0.

fq=0.

ftheta=0.25*(2+cos(theta))*(1-cos(theta))**2

do 100 i=1,10

if (m.ne.0) emj=eij(m,i)

if (m.eq.0) emj=0.0

fm=fm+con(i)*emj

fq=fq+con(i)*eij(q,i)

100	continue

actm=10.**fm*con(m)

actq=10.**fq*con(q)

dg=dgz(temp,gaa,gbb)-1.98*temp*log((actm**x)*(actq**y))

dg=dg*4.18

dghom=(16.*pi*sigma**3.*vm(nincl)**2.)/(3.*dg*dg)

dghet=dghom*ftheta

aiv=a*ftheta**(1./6.)*exp(-dghet/(bk*temp))

homiv=a*exp(-dghom/(bk*temp))

###### Subroutine Drawplot

This subroutine reads data for the formation and dissolution of an inclusion from the two output files and draws the plots on the screen. The program can calculate the accurate position of grids and tickmarks automatically. The commands in the program are specific for Digital Visual Fortran and are not discussed here.

### Reference

- T. Hong and T. DebRoy: Time-Temperature-Transformation Diagrams for the Formation and Dissolution of Oxide, Nitride, and Sulfide Inclusions, unpublished document, Department of Materials Science & Engineering, Penn State, March 2000.

- J.W. Christian: The theory of transformations in metals and alloys, p. 535, 2nd edition, 1981, Pergamon Press, Oxford.

- M.L. Tuppin and J.F. Elliot: J. Iron Steel. Inst., 1966, Vol. 204, pp. 217-225.

- M.J. Whelan: Metal Science Journal, 1969, Vol. 3, No. 5, pp. 95-97.

- S.S. Babu, S.A. David, J.M. Vitec, K. Mundra, and T. DebRoy: Materials Science and Technology, Feb. 1995, Vol. 11, No. 2, pp. 186-199.

- E.T. Turkdogan: Physical Chemistry of High Temperature Technology, 1980, Academic Press, New York.

- G.K. Sigworth and J.F. Elliott: Metal Science Journal, 1974, Vol. 8, No. 9, pp. 298-310.

Appendix A

Table 1.  Original composition and diffusion coefficient of the elements in liquid steel

| Element | C | Si | Mn | Ni | Cr | Ti | Al | N | O | S |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| wt% | 0.066 | 0.82 | 1.66 | 0.03 | 0.05 | 0.025 | 0.026 | 0.007 | 0.084 | 0.030 |
| D0 (m2/s) | 810-9 | 3.810-9 | 210-8 | - | 510-9 | 110-9 | 210-9 | 1.210-8 | 110-8 | 2.810-8 |

Table 2.  Standard free energy expressions for various reactions in the form of

DG0=a+bT,Calmole

| Precipitation Reaction | a | B |
| --- | --- | --- |
| 2Al+3O=Al2O3 | -289060 | 93.52 |
| 3Ti+5O=Ti3O5 | -419680 | 136.5 |
| Ti+2O=TiO2 | -161460 | 55.95 |
| Si+2O=SiO2 | -140950 | 54.62 |
| Mn+O=MnO | -68816 | 29.95 |
| Al+N=AlN(s) | -154000 | 44.5 |
| 3Si+4N=Si3N4 | -203000 | 75.3 |
| Ti+N=TiN | -80380 | 24.29 |
| Fe+S=FeS | -111370 | 57.0 |
| Mn+S=MnS | -39500 | 17.00 |
| Mn+2Al+4O=MnO×Al2O3 | -369376 | 125.22 |
| Si+2Al+5O=SiO2×Al2O3 | -319875 | 97.32 |
| Fe+2Al+4O=FeO×Al2O3 | -330180 | 108.4 |
| Mn+Si+4O=MnO×SiO2 | -200466 | 75.0 |

Table 3.  The first order interaction parameters eij, in liquid iron (1873K)

| i↓ j → | C |  | Si |  | Mn | Ni |  | Cr |  | Ti |  | Al |  | N |  | O | S |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| C |  | 0.14 | 0.08 | -0.012 |  |  | 0.012 |  | -0.024 |  | - |  | 0.043 |  | 0.11 | -0.34 | 0.67 |
| Si |  | 0.188 | 0.11 | 0.002 |  |  | 0.005 |  | -0.0003 |  | - |  | 0.058 |  | 0.09 | -0.23 | 0.64 |
| Mn |  | -0.07 | 0 | 0 |  |  | - |  | - |  | - |  | - |  | -0.091 | -0.083 | -0.31 |
| Ni |  | 0.042 | 0.0057 | - |  |  | 0.0009 |  | -0.0003 |  | - |  | - |  | 0.028 | 0.01 | -0.25 |
| Cr |  | -0.12 | -0.0043 | - |  |  | 0.0002 |  | -0.0003 |  | 0.059 |  | - |  | -0.19 | -0.14 | -0.33 |
| Ti |  | - | - | - |  |  | - |  | 0.055 |  | 0.013 |  | - |  | -1.8 | -1.8 | -1.1 |
| Al |  | 0.091 | 0.0056 | - |  |  | - |  | - |  | - |  | 0.045 |  | -0.058 | -6.3 | 0.024 |
| N |  | 0.13 | 0.047 | -0.02 |  |  | 0.01 |  | -0.047 |  | -0.53 |  | -0.028 |  | 0 | 0.05 | - |
| O |  | -0.45 | -0.131 | -0.021 |  |  | 0.006 |  | -0.04 |  | -0.6 |  | -3.9 |  | 0.057 | -0.23 | -3.1 |
| S |  | 0.06 | 0.027 | -0.0014 |  |  | 0 |  | -0.0022 |  | -0.019 |  | 0.013 |  | - | -0.19 | 0 |

Appendix B 	Nomenclature

#### Main Program

a			A in equation (14)

ak			k in equation (19)

akeq			Keq in equation (3)

alpha			a in equation (11)

am(me)		atomic masses of the 10 elements

bk			Boltzman constant, k0, in equations (12) and (14)

con(me)		concentrations of the 10 elements and iron

cmp, cm1p, cm2p, cqp	weight percentage of M, M’, M” and Q in inclusion particle

cmb, cm1b, cm2b, cqb 	weight percentage of M, M’, M” and Q in bulk liquid metal

cmi, cm1i, cm2i, cqi 	weight percentage of M, M’, M” and Q at interface

d00			diffusion coefficient of the selected nonmetallic element (Q)

d0(me)			diffusion coefficients of all nonmetallic elements

dissf			data file name of TTT diagram for inclusion dissolution

dt			small time step in the calculation of the dissolution TTT diagram

eij(me,me)		interaction parameters eij

equtemp		equilibrium temperature

formf			output data file name for inclusion formation

ga(mi), gb(mi)		a and b in the equation of ΔG0=a+bTfor all inclusions

gaa,gbb		user selected values of a and b in the equation of ΔG0=a+bT

homiv, hetiv	homogeneous and heterogeneous nucleation rates in equations (12), (14) and (15)

ic			the index to decide if inclusion growth calculations are over inclusion(mi)		name strings of the 14 inclusions considered

index	index to decide if the calculations for another inclusion are required

mi			number of inclusions, equal to 14 in this program

me			number of elements, equal to 10 in the program

mm(mi), mm2(mi)	index of metallic elements for mi number of inclusions

m, m1, m2		index of constituent elements M, M’, M” for the inclusion selected

pi			 = 3.1416

qq(mi)			index of element Q for every inclusion

q			index of element Q for the selected inclusion

retlog			a logical variable to indicate success of an internal subroutine call

rr			instantaneous radius in every time step

r0, rf			initial and final radii

sigma			interfacial energy, , in equation (12)

t			time t in equation (18)

theta			contact angle, , in equation (16)

vm(mi)		molar volumes of the inclusions

x0, x9, y0, y9		the coordinates (x,y) of the bottom-left and top-right points of the

rectangle in the screen matrix

xx(mi), xx2(mi)	x (or x1) and x2 in equations (1) and (7) for all inclusions

x, x1, x2		x (or x1) and x2 for the inclusion selected in equations (1) and (7)

yy(mi)			y in equation (1) and (7) for all inclusions

y			y in equation (1) and (7) for the selected inclusion

Subroutine Getstart

con(10)		concentrations of the elements in alloy

d00			diffusion coefficient of a nonmetallic element

dissf			output file name for dissolution calculations

eij(10,10)		interaction coefficient, eij

formf			output file name for formation calculations

gaa, gbb		a and b in ΔG0=a+bT for the inclusion selected

r0, rf			the initial and final inclusion radii

sigma			interfacial energy  in equation (12)

theta			contact angle  in equation (16)

tmin, tmax		minimum and maximum temperatures in plotting TTT diagrams

zeta			extent of precipitation  in equations (17) and (18)

Subroutine Drawplot

d00			diffusion coefficient of a nonmetallic element

dissf			output file name for dissolution data

formf			output file name for formation data

inclusion(14)		inclusion name

ix			horizontal coordinate in the screen

iy			vertical coordinate in the screen

dummy		a long string used to read the entire comment line in a data file

maxf, maxd	the maximum length of x-axis for formation and dissolution TTT diagrams

nincl			index of the inclusion selected

r0, rf			initial and final inclusion radii for dissolution calculations

status			index to show the status of calling ‘dialog’ functions

str			output string

t			time in equation (18)

temp			temperature

td			the temperature step of tickmark of  “Temperature” (y) axis

tmax, tmin	maximum and minimum temperatures for plotting TTT diagram

x0, x1, y0, y1		(x,y) of the bottom-left and top-right points in the screen

xd, yd			steps in x and y directions

zeta			extent of precipitation, 

type  curpos, pos, xy	type variables required by the DSFLIB graphic interface

4. Subroutines equcon and equcon2

akeq			equilibrium constant keq in equation (3)

amm, amm1, amm2	atomic mass of M, M’ and M”

amq			atomic mass of Q

actm, actm1, actm2	activities of M, M’ and M”

actq 			activity of Q

cmi, cm1i, cm2i, cqi	equilibrium concentrations of M, M’, M” and Q at interface

con(0:10)		concentrations of elements in alloy

eij(10,10) 		interaction coefficients, eij

fm, fq, fm1, fm2	activity coefficients of M, M’, M” and Q

m, m1, m2, q		indices of M, M’, M” and Q in the selected inclusion

me			number of elements considered

x, x1, x2, y		stoichiometric parameters of M, M’, M” and Q

5. Functions aiv and aiv2

a			constant A in equation (12)

aiv, aiv2		heterogeneous nucleation rates of simple and complex inclusions

actm, actm1, actm2, actq	activities of M, M’, M” and Q

akeq			equilibrium constant keq in equation 3

amm,amm1, amm2	atomic mass of M, M’ and M”

amq			atomic mass of Q

bk			Boltzman constant

cmi, cm1i, cm2i, cni	equilibrium concentrations of M, M’, M” and Q at the interface

con(0:10)		concentrations of elements in alloy

eij(10,10)		interaction coefficients, eij

d0(10)			diffusion coefficients of all elements

dg			free energy of formation

dghet, dghom		activation energy for heterogeneous and homogeneous nucleations

dgz			standard free energy of formation

fm, fm1, fm2, fq	activity coefficients of M, M’, M” and Q

ftheta			f() in equation (16)

gaa, gbb		a and b in standard free energy equation

homiv			homogeneous nucleation rate

m, m1, m2		indices of M, M’ and M” in the selected inclusion

me			number of elements considered

nincl			index of the inclusion selected

pi			 = 3.11416

q			index of element Q in the selected inclusion

sigma			interfacial energy in equation (12)

theta			contact angle  in equations (14) and (16)

vm(14)			molar volume of inclusions

#### x, x1, x2, y		stoichiometric coefficients of M, M’, M” and Q

Source code

c *****************  Index of inclusions ******************************

c 1.Al2O3, 2.Ti3O5, 3.TiO2, 4.SiO2, 5.MnO, 6.AlN, 7.Si3N4, 8.TiN,

c 9.FeS, 10.MnS, 11. MnOAl2O3, 12.SiO2Al2O3, 13. FeOAl2O3, 14.MnOSiO2

c ****************** Index of elements: *******************************

c 0.Fe 1.C, 2.Si, 3.Mn, 4.Ni, 5.Cr, 6.Ti, 7.Al, 8.N, 9.O, 10.S

c *********************************************************************

program main

use DFLOGM

include 'resource.fd'

c -----------  Initialization -----------------------------------------

parameter mi=14,me=10

character*20 formf,dissf,inclusion(mi)

logical retlog,iindex(mi)

real con(0:me),eij(me,me),am(0:me),vm(mi),d0(mi),ga(mi),gb(mi)

real gaa,gbb,rhomxqy(14),r0,rf,theta

integer xx(mi),xx2(mi),yy(mi),mm(mi),mm2(mi),qq(mi)

integer x,x1,x2,y,m,m1,m2,q,retint

type (dialog) dlg

common /c1/pi,sigma,vm,a,bk,d0

data inclusion/'Al2O3','Ti3O5','TiO2','SiO2','MnO','AlN','Si3N4'

1 ,'TiN','FeS','MnS','MnOAl2O3','SiO2Al2O3','FeOAl2O3','MnOSiO2'/

data con/1.,.066,.82,1.66,.03,.05,.025,.026,.007,.084,.03/

data ga/-289060.,-419680.,-161460.,-140950.,-68816.,-154000.,

1-203000.,-80380.,-111370.,-39500.,-369376.,-319875.,-330180.

1,-200466./

data gb/93.52,136.,55.95,54.62,29.95,44.5,75.3,24.29,57.

1,17.00,125.22,97.32,108.4,75./

data xx/2,3,1,1,1,1,3,1,1,1,1,1,1,1/

data xx2/0,0,0,0,0,0,0,0,0,0,2,2,2,1/

data yy/3,5,2,2,1,1,4,1,1,1,4,5,4,3/

data mm/7,6,6,2,3,7,2,6,0,3,3,2,0,3/

data mm2/0,0,0,0,0,0,0,0,0,0,7,7,7,2/

data qq/9,9,9,9,9,8,8,8,10,10,9,9,9,9/

data am/56.,12.,28.,55.,59.,46.,48.,27.,14.,16.,32./

data (eij(2,i),i=1,10)/0.19,0.11,0.002,0.005,-0.0003,0.,

1 0.058,0.09,-0.23,0.056/

data (eij(3,i),i=1,10)/-.07,0.,0.,0.,0.,0.,0.,-.091,-.083,-.048/

data (eij(4,i),i=1,10)/.042,.0057,0.,.0009,-.0003,0.,0.,

1 0.028,0.01,-.0037/

data (eij(6,i),i=1,10)/0.,0.,0.,0.,.055,.013,0.,-1.8,-1.8,-.11/

data (eij(7,i),i=1,10)/.091,.0056,0.,0.,0.,0.,.045,-.058,-6.6,.03/

data (eij(8,i),i=1,10)/0.13,0.047,-0.02,0.01,-0.047,-0.53,

1 -0.028,.0,0.05,0.007/

data (eij(9,i),i=1,10)/-0.45,-0.131,-0.021,.006,-0.04,-0.6,

1 -3.9,.057,-0.23,-.133/

data (eij(10,i),i=1,10)/0.11,0.063,-0.026,0.,-0.011,

1 -0.072,0.035,0.01,-0.27,-0.028/

data dt,x0,x9,y0,y9,small/1.e-4,200.,700.,450.,80.,1.e-28/

c ----------------welcome window----------------------------

retlog=dlginit(dialog1,dlg)

retint=dlgmodal(dlg)

call dlguninit(dlg)

c ---------------- Inclusion selection window --------------

10	nincl=0

retlog=dlginit(dialog2,dlg)

do 14 i=1,14

iindex(i)=.false.

idialog=999+i

retlog=dlgset(dlg,idialog,iindex(i))

14		continue

retint=dlgmodal(dlg)

do 15 i=1,14

idialog=999+i

retlog=dlgget(dlg,idialog,iindex(i))

if (iindex(i)) nincl=i

15		continue

CALL DlgUninit( dlg )

if (nincl.eq.0) goto 10

c ------------------ change default value ------------------

gaa=ga(nincl)

gbb=gb(nincl)

d00=d0(nincl)

call getstart(formf,dissf,con,tmin,tmax,sigma,d00,

1zeta,r0,rf,gaa,gbb,eij,theta)

if (zeta.eq.0) goto 10

open (unit=20,file=formf)

open (unit=21,file=dissf)

td=100.

ic=0.

equtemp=0.

told=0.

c -------------  nincl=1,10  simple compound MxQy  -------------------

if (nincl.le.10) then

x=xx(nincl)

y=yy(nincl)

q=qq(nincl)

m=mm(nincl)

amm=am(m)

amq=am(q)

cmp=100.*x*amm/(x*amm+y*amq)

cmb=con(m)

cqp=100.*y*amq/(x*amm+y*amq)

cqb=con(q)

write(20,2) inclusion(nincl),cqp,cmp,cqb,cmb

write(21,2) inclusion(nincl),cqp,cmp,cqb,cmb

2		format(a15,4f10.5)

write(20,*)'Temp,time,Ivhet,Ivhom,cqi,cmi(wt%),c*,dg(kj/mol)'

write(21,*)'Temp,time,cqi,cmi(wt%),c*,dg(kj/mol)'

do 30 temp=tmin,tmax,1.

hetiv=aiv(temp,theta,con,x,y,eij,nincl,m,q,gaa,gbb,dg,homiv)

akeq=exp(-dgz(temp,gaa,gbb)/(1.98*temp))

cqi=cqb*.5

cmi=cmb*.5

call equcon(m,q,eij,akeq,x,y,con,cmi,cqi,amm,amq)

if ((cqi/cqb).gt.5.0.or.(cmi/cmb).gt.5.0) goto 12

cstar=(cqb-cqi)/(cqp-cqi)

if (cqi.lt.cqb) then

alpha=sqrt(2.*d00*cstar)

t=((-15.*cstar*log(1.-zeta))/(8.*(hetiv+small)*pi*

1		alpha**3))**0.4

if(t.lt.told) goto 30

write(20,1)temp,t,hetiv,homiv,cqi,cmi,cstar,dg/1000.

1			format(f6.1,3(e15.6e3),f11.7,f11.7,e14.6e2,f11.3)

told=t

else

if(ic.eq.0) then

write(21,6)temp,10.,cqi,cmi,0.,0.

equtemp=temp

ic=1

endif

ak=-2.*cstar

rr=r0

do 60 time=dt,10.,dt

rr=rr-ak*d00*dt/(2*rr)-ak*sqrt(d00*dt/pi)/2.

if (rr.lt.rf) goto 70

60			continue

70			write(21,6) temp,time,cqi,cmi,cstar,dg/1000.

6			format(f6.1,e15.6e3,f11.7,f11.7,e13.4e3,f11.2)

endif

30		continue

endif

c -------------  nincl=10,14  complex oxide M1x1M2x2Qy ------------------

if (nincl.gt.10) then

x1=xx(nincl)

x2=xx2(nincl)

y=yy(nincl)

q=qq(nincl)

m1=mm(nincl)

m2=mm2(nincl)

amm1=am(m1)

amm2=am(m2)

amq=am(q)

cm1p=100.*x1*amm1/(x1*amm1+x2*amm2+y*amq)

cm1b=con(m1)

cm2p=100.*x2*amm2/(x1*amm1+x2*amm2+y*amq)

cm2b=con(m2)

cqp=100.*y*amq/(x1*amm1+x2*amm2+y*amq)

cqb=con(q)

write(20,3) inclusion(nincl),cqp,cm1p,cm2p,cqb,cm1b,cm2b

write(21,3) inclusion(nincl),cqp,cm1p,cm2p,cqb,cm1b,cm2b

3		format(a15,6f10.5)

write(20,*)'Temp,time,Ivhet,Ivhom,cqi,cmi,cmi(wt%),c*,dg(kj)'

write(21,*)'Temp,time,cqi,cmi,cmi(wt%),c*,dg(kj/mol)'

do 85 temp=tmin,tmax,1.

hetiv=aiv2(temp,theta,con,x1,x2,y,eij,nincl,m1,m2,q,

1	gaa,gbb,dg,homiv)+small

akeq=exp(-dgz(temp,gaa,gbb)/(1.98*temp))

cqi=cqb/2.

cm1i=cm1b/2.

cm2i=cm2b/2

call equcon2(m1,m2,q,eij,akeq,x1,x2,y,con,cm1i,cm2i,cqi,

1	amm1,amm2,amq)

if (cqi/cqb.gt.5.0.or.cm2i/cm2b.gt.5.0) goto 12

cstar=(cqb-cqi)/(cqp-cqi)

if (cqi.lt.cqb) then

c ---	formation TTT diagram

alpha=sqrt(2.*d00*cstar)

t=((-15.*cstar*log(1.-zeta))/(8.*hetiv*pi*alpha**3))**0.4

write(20,4)temp,t,hetiv,homiv,cqi,cm1i,cm2i,cstar,dg/1000.

4			format(f6.1,3(e15.6e3),4(f11.7),f11.2)

else

c --- dissolution TTT diagram

if(ic.eq.0) then

write(21,4)temp,10.,cqi,cm1i,cm2i,cstar,0

equtemp=temp

ic=1

endif

ak=-2.*cstar

rr=r0

do 86 time=dt,10.,dt

rr=rr-ak*d00*dt/(2.*rr)-ak*.5*sqrt(d00*dt/pi)

if (rr.lt.rf) goto 75

86			continue

75			write(21,4) temp,time,cqi,cm1i,cm2i,cstar,dg/1000.

endif

85		continue

endif

12	close (unit=20)

close (unit=21)

call drawplot(formf,dissf,tmax,tmin,x0,x9,y0,y9,nincl,zeta

1,r0,rf,inclusion,td,equtemp)

c --------------- Another calculation? --------------------

retlog=dlginit(dialog5, dlg)

retint=dlgmodal(dlg)

call dlguninit(dlg)

if (retint.eq.1110) goto 10

end

!!!!!!!!!!!!!!!!!!!!!  Main program ends here !!!!!!!!!!!!!!!!!!!!!!!!

block data

real sigma,pi,a,bk,vm(14),d0(10)

common /c1/pi,sigma,vm,a,bk,d0

data sigma,pi,a,bk/.5,3.1416,1.e33,1.38e-23/

data vm/25.e-6,23.e-6,22.e-6,19.e-6,27.e-6,24.e-6,25.e-6,

1 24.2e-6,29.3e-6,34.2e-6,23.6e-6,29.3e-6,30.1e-6,30.e-6/

data d0/8.e-9,3.8e-9,2.e-8,5.e-9,5.e-9,1.e-9,2.e-9,1.2e-8,

1 1.e-8,2.8e-8/

end

function aiv(temp,theta,con,x,y,eij,nincl,m,q,gaa,gbb,dg,homiv)

real con(0:10),eij(10,10),vm(14),d0(10)

real theta,aiv,dg,dgz,gaa,gbb,vvih,ftheta

integer x,y,m,q

integer nincl

common /c1/pi,sigma,vm,a,bk,d0

fm=0.

fq=0.

ftheta=0.25*(2+cos(theta))*(1-cos(theta))**2

do 100 i=1,10

if (m.ne.0) emj=eij(m,i)

if (m.eq.0) emj=0.0

fm=fm+con(i)*emj

fq=fq+con(i)*eij(q,i)

100	continue

actm=10.**fm*con(m)

actq=10.**fq*con(q)

dg=dgz(temp,gaa,gbb)-1.98*temp*log((actm**x)*(actq**y))

dg=dg*4.18

dghom=(16.*pi*sigma**3.*vm(nincl)**2.)/(3.*dg*dg)

dghet=dghom*ftheta

aiv=a*ftheta**(1./6.)*exp(-dghet/(bk*temp))

homiv=a*exp(-dghom/(bk*temp))

return

end

function aiv2(temp,theta,con,x1,x2,y,eij,nincl,m1,m2,q,

1gaa,gbb,dg,homiv)

real con(0:10),eij(10,10),vm(14),d0(10),aiv

real theta,dg,dgz,gaa,gbb

integer nincl,x1,x2,y,m1,m2,q

common /c1/pi,sigma,vm,a,bk,d0

fm1=0.

fm2=0.

fq=0.

ftheta=0.25*(2+cos(theta))*(1-cos(theta))**2

do 110 i=1,10

if (m1.eq.0) em1j=0.0

if (m1.ne.0) em1j=eij(m1,i)

fm1=fm1+con(i)*em1j

fm2=fm2+con(i)*eij(m2,i)

fq=fq+con(i)*eij(q,i)

110	continue

actm1=10.**fm1*con(m1)

actm2=10.**fm2*con(m2)

actq=10.**fq*con(q)

dg=dgz(temp,gaa,gbb)-

1 1.98*temp*log((actm1**x1)*(actm2**x2)*(actq**y))

dghom=(16.*pi*sigma**3.*vm(nincl)**2.)/(3.*dg*dg)

dghet=dghom*ftheta

aiv2=a*ftheta**(1./6.)*exp(-dghet/(bk*temp))

homiv=a*exp(-dghom/(bk*temp))

return

end

function dgz(temp,gaa,gbb)

real dgz,temp,gaa,gbb

dgz=gaa+gbb*temp

return

end

subroutine getstart(formf,dissf,con,tmin,tmax,sigma,d0,

1zeta,r0,rf,gaa,gbb,eij,theta)

use DFLOGM

include 'resource.fd'

integer retint,i,j,idialog

logical retlog

real con(0:10),tmin,tmax,sigma,zeta,d0,r0,dr,gaa,gbb,eij(10,10)

character*20 formf,dissf,ccon(10),const(8),eijc

character*10 gac,gbc,tminstr,tmaxstr

type (dialog) dlg

250	retlog=dlginit(dialog3,dlg)

retlog=dlgset(dlg,edit_growf,"grow.dat")

retlog=dlgSet(dlg,edit_dissf,"diss.dat")

do 200 i=1,10

write(ccon(i),'(f5.3)') con(i)

retlog =dlgset(dlg,1015+i,ccon(i) )

200		continue

retlog=dlgset(dlg,edit_tmin, '1600.')

retlog=dlgset(dlg,edit_tmax, '2500.')

retlog=dlgset(dlg,edit_sigma, '0.5')

retlog=dlgset(dlg,edit_d0, '1.e-8')

retlog=dlgset(dlg,edit_zeta, '0.01')

retlog=dlgset(dlg,edit_r0, '1.0')

retlog=dlgset(dlg,edit_dr, '0.01')

retlog=dlgset(dlg,edit_theta, '50')

write(gac,'(f9.1)') gaa

retlog=dlgset(dlg,edit_ga,gac)

write(gbc,'(f7.2)') gbb

retlog=dlgset(dlg,edit_gb,gbc)

retint=dlgmodal(dlg)

retlog=dlggetchar(dlg,edit_growf,formf)

retlog=dlggetchar(dlg,edit_dissf,dissf)

do 205 i=1,10

retlog=dlgget(dlg,1015+i,ccon(i))

read(ccon(i),*) con(i)

205		continue

retlog=dlgget(dlg,edit_tmin,const(1))

retlog=dlgget(dlg,edit_tmax,const(2))

retlog=dlgget(dlg,edit_sigma,const(3))

retlog=dlgget(dlg,edit_d0,const(4))

retlog=dlgget(dlg,edit_zeta,const(5))

retlog=dlgget(dlg,edit_r0,const(6))

retlog=dlgget(dlg,edit_dr,const(7))

retlog=dlgget(dlg,edit_theta,const(8))

read(const(1),*) tmin

read(const(2),*) tmax

read(const(3),*) sigma

read(const(4),*) d0

read(const(5),*) zeta

read(const(6),*) r0

r0=r0*1.e-6

read(const(7),*) rf

rf=rf*1.e-6

read(const(8),*) theta

theta=theta*3.14159/180.

retlog=dlgget(dlg,edit_ga,gac)

read(gac,'(f9.1)') gaa

retlog=dlgget(dlg,edit_gb,gbc)

read(gbc,'(f7.2)') gbb

call dlguninit(dlg)

if (retint.eq.1028) zeta=0.

if (retint.eq.1030.or.retint.eq.1028) goto 245

retlog=dlginit(dialog4,dlg)

do 220 i=2,10

if (i.eq.4.or.i.eq.5) goto 220

do 225 j=1,10

idialog=1037+j+(i-2)*10

if (i.gt.5) idialog=1037+j+(i-4)*10

write(eijc,'(f7.4)') eij(i,j)

225			retlog=dlgset(dlg,idialog,eijc)

220		continue

retint=dlgmodal(dlg)

do 230 i=2,10

if (i.eq.4.or.i.eq.5) goto 230

do 235 j=1,10

idialog=1037+j+(i-2)*10

if (i.gt.5) idialog=1037+j+(i-4)*10

retlog=dlgget(dlg,idialog,eijc)

235			read (eijc, *) eij(i,j)

230		continue

call dlguninit(dlg)

if (retint.eq.1108) goto 250

245	return

end subroutine getstart

subroutine equcon(m,q,eij,akeq,x,y,con,cmi,cqi,amm,amq)

integer m,q,x,y

real eij(10,10),con(0:10),cmi,cqi,akeq,amm,amq

me=10

if (m.eq.0) then

do 450 ii=1,10

fq=0.

do 460 i=1,me

if (i.eq.q) goto 460

fq=fq+con(i)*eij(q,i)

460			continue

fq=fq+cqi*eij(q,q)

fq=10.**fq

cqi=((1./akeq)**(1./float(y)))/fq

450		continue

cmi=con(m)

else

do 430 ii=1,10

fm=0.

fq=0.

do 420 i=1,me

if (i.eq.q.or.i.eq.m) goto 420

fm=fm+con(i)*eij(m,i)

fq=fq+con(i)*eij(q,i)

420			continue

fm=fm+cqi*eij(m,q)+cmi*eij(m,m)

fq=fq+cqi*eij(q,q)+cmi*eij(q,m)

fm=10.**fm

fq=10.**fq

if(con(m).gt.con(q)) then

actm=fm*cmi

actq=(1./(akeq*(actm**float(x))))**(1./float(y))

cqi=actq/fq

cmi=con(m)-float(x)*amm*(con(q)-cqi)/(float(y)*amq)

endif

if(con(m).lt.con(q)) then

actq=fq*cqi

actm=(1./(akeq*(actq**float(y))))**(1./float(x))

cmi=actm/fm

cqi=con(q)-y*amq*(con(m)-cmi)/(x*amm)

endif

430		continue

endif

return

end subroutine equcon

subroutine equcon2(m1,m2,q,eij,akeq,x1,x2,y,con,cm1i,cm2i,cqi,

1amm1,amm2,amq)

integer m1,m2,q,x1,x2,y

real eij(10,10),con(0:10),cm1i,cm2i,cqi,akeq

me=10

if (m1.eq.0) then

do 550 ii=1,10

fq=0.

fm2=0.

do 560 i=1,me

if (i.eq.q.or.i.eq.m2) goto 560

fq=fq+con(i)*eij(q,i)

fm2=fm2+con(i)*eij(m2,i)

560			continue

fq=fq+cqi*eij(q,q)+cm2i*eij(m2,q)

fm2=fm2+cqi*eij(q,m2)+cm2i*eij(m2,m2)

fq=10.**fq

fm2=10.**fm2

actq=fq*cqi

actm2=(1./(akeq*(actq**float(y))))**(1./float(x2))

cm2i=actm2/fm2

cqi=con(q)-float(y)*amq*(con(m2)-cm2i)/(float(x2)*amm2)

550		continue

cm1i=con(m1)

else

do 530 ii=1,10

fm1=0.

fm2=0.

fq=0.

do 520 i=1,me

if (i.eq.q.or.i.eq.m1.or.i.eq.m2) goto 520

fm1=fm1+con(i)*eij(m1,i)

fm2=fm2+con(i)*eij(m2,i)

fq=fq+con(i)*eij(q,i)

520			continue

fm1=fm1+cqi*eij(m1,q)+cm1i*eij(m1,m1)+cm2i*eij(m1,m2)

fm2=fm2+cqi*eij(m2,q)+cm1i*eij(m2,m1)+cm2i*eij(m2,m2)

fq=fq+cqi*eij(q,q)+cm1i*eij(q,m1)+cm2i*eij(q,m2)

fm1=10.**fm1

fm2=10.**fm2

fq=10.**fq

if (con(q).gt.con(m2)) then

actm1=fm1*cm1i

actq=fq*cqi

actm2=(1./(akeq*(actq**y)*(actm1**x1)))**(1./float(x2))

cm2i=actm2/fm2

cm1i=con(m1)-x1*amm1*(con(m2)-cm2i)/(x2*amm2)

cqi=con(q)-y*amq*(con(m2)-cm2i)/(x2*amm2)

endif

if (con(q).lt.con(m2))then

actm1=fm1*cm1i

actm2=fm2*cm2i

actq=(1./(akeq*(actm1**x1)*(actm2**x2)))**(1./float(y))

cqi=actq/fq

cm1i=con(m1)-x1*amm1*(con(q)-cqi)/(y*amq)

cm2i=con(m2)-x2*amm2*(con(q)-cqi)/(y*amq)

endif

530		continue

endif

return

end subroutine equcon2

subroutine drawplot(formf,dissf,tmax,tmin,x0,x1,y0,y1,nincl,zeta

1,r0,rf,inclusion,td,equtemp)

USE MSFLIB

USE DFLIB

integer status,nincl,maxf,maxd,i

real tmax,tmin,x0,x1,y0,y1,zeta,r0,rf,td,temp,t

character*20 formf,dissf,inclusion(14)

character*80 dummy,str

type (rccoord) curpos

type (xycoord) pos

type (wxycoord) xy

data maxf,maxd/18,10/

c -----------------  draw axie for formation TTT diagram-------------

status=setbkcolorrgb(#ffffff)

call clearscreen($GCLEARSCREEN)

status=setcolorrgb(#ffffff)

status=lineto(x0,y0)

status=setcolorrgb(#000000)

status=rectangle($GBORDER,x0,y0,x1,y1)

yd=td*(y1-y0)/(tmax-tmin)

xd=(x1-x0)/maxf

status=initializefonts()

call setgtextrotation(0)

status=setfont('t''Arial''h12w8')

do 310 i=0,maxf

x=x0+xd*i

write(str,'(i3)') i-10

call moveto(int(x-12),int(y0+10),pos)

call outgtext(str)

status=rectangle($GBORDER,x,y0,x,y0-5)

310	continue

do 320 y=y0,y1,yd

temp=tmin+(y-y0)*td/yd

call moveto(int(x0-60),int(y-5),pos)

write(str,'(i5)')int(temp+0.05)

call outgtext(str)

status=rectangle($GBORDER,x0,y,x0+5,y)

320	continue

call moveto(int(x1-250),int(y0-50),pos)

write(str,302)inclusion(nincl),float(int(zeta*1000.+.5))/1000.

302	format(a11,'zeta =',f5.2)

call outgtext(str)

status=setfont('t''Arial''h16w12')

call moveto(int(x0+150),int(y0+50),pos)

call outgtext('Log (time(sec))')

call moveto(int(x0-90),int(y0-75),pos)

call setgtextrotation(900)

call outgtext('Temperature (K)')

c ---------------------draw formation TTT diagram ----------

status=setcolorrgb(#ffffff)

status=lineto(x0,y0)

status=setcolorrgb(#000000)

open (unit=20,file=formf)

read (20,304) dummy

read (20,304) dummy

304	format(a60)

330	read (20,303,end=340) temp,t

303	format(f6.1,e15.6e3)

iy=y0+(y1-y0)*(temp-tmin)/(tmax-tmin)

ix=x0+(log10(t)+10.)*(x1-x0)/maxf

if(ix.gt.int(x1)) ix=int(x1)

if(iy.lt.int(y1)) iy=int(y1)

status=lineto(ix,iy)

goto 330

340	close(unit=20)

status=settextcolorrgb(#ffffff)

pause

c-------------------- draw axis for dissolution TTT diagram -----

status=setbkcolorrgb(#ffffff)

call clearscreen($GCLEARSCREEN)

tmin=int(equtemp/10.)*10.

tmax=tmin+50.

td=10.

status=setcolorrgb(#ffffff)

status=lineto(x0,y0)

status=setcolorrgb(#000000)

status=settextcolorrgb(#000000)

status=rectangle($GBORDER,x0,y0,x1,y1)

yd=td*(y1-y0)/(tmax-tmin)

xd=(x1-x0)/maxd

status=initializefonts()

call setgtextrotation(0)

status=setfont('t''Arial''h14w10')

do 350 i=0,maxd

x=x0+xd*i

call moveto(int(x-10),int(y0+10),pos)

write(str,'(i2)') i

call outgtext(str)

status=rectangle($GBORDER,x,y0,x,y0-5)

350	continue

do 360 y=y0,y1,yd

temp=tmin+(y-y0)*td/yd

call moveto(int(x0-60),int(y-5),pos)

write(str,'(i5)')int(temp)

call outgtext(str)

status=rectangle($GBORDER,x0,y,x0+5,y)

360	continue

call setgtextrotation(0)

call moveto(int(x1-400),int(y1+50),pos)

write(str,306)inclusion(nincl),r0*1.e6,rf*1.e6

306	format(a11,'R0= ', f4.1,' µm  Rf= ',f4.2,' µm')

call outgtext(str)

call moveto(int(x1-400),int(y1+75),pos)

write(str,307) equtemp

307	format('Equilibrium Temp = ', f6.1, ' K')

call outgtext(str)

status=setfont('t''Arial''h16w12')

call moveto(int(x0+150),int(y0+50),pos)

call outgtext('Time (sec)')

call moveto(int(x0-90),int(y0-75),pos)

call setgtextrotation(900)

call outgtext('Temperature (K)')

c ---------------------draw dissolution TTT diagram ----------

open (unit=21,file=dissf)

read (21,308) dummy

read (21,308) dummy

308	format(a60)

i=0

370	read (21,309,end=380) temp,t

309	format(f6.1,e15.6e3)

i=i+1

status=setcolorrgb(#000000)

if (i.eq.1) status=setcolorrgb(#ffffff)

iy=y0+(y1-y0)*(temp-tmin)/(tmax-tmin)

ix=x0+t*(x1-x0)/10.

if(ix.gt.int(x1)) ix=int(x1)

if(iy.lt.int(y1)) iy=int(y1)

status=lineto(ix,iy)

goto 370

380	close(unit=21)

status=settextcolorrgb(#ffffff)

pause

end subroutine drawplot