Chapter 5   Background Material

5.1  HAZ Hardness Module

This module anticipates the heat-affected zone (HAZ) hardness of welds

given the input parameters: current, voltage, welding speed and process efficiency;

together with the base metal chemical composition. The module is based on

relatively independent algorithms generated for this purpose from the

investigations of: Arata [1], Yurioka [2,3], Suzuki [4,5], Terasaki [6,7], Dueren

[8], Beckert [9] and Cottrell [10]. Weld cooling time (800 - 500oC) required in all

models is predicted by the Adams [11] heat transfer relationships. Regression

limits are listed as follows:

Arata : 	C     0.07 - 0.53  wt%

Mn    0.00 - 1.50

Si    0.00 - 0.60

Ni    0.00 - 3.50

Cr    0.00 - 1.50

Mo    0.00 - 0.60

V     0.00 - 0.15

B     0.00 - 0.01

Yurioka I :	low alloy steels with carbon content between 0.01 and 0.30 wt%.

Yurioka II :		C   <=  0.80 wt%

Si  <=  1.20

Mn  <=  2.00

Cu  <=  0.90

Ni  <= 10.00

Cr  <= 10.00

Mo  <=  2.00

Suzuki :	low alloy steels with carbon content between 0.017 - 0.33 wt%.

Terasaki :	low alloy steels with carbon content less than 0.60 wt%.

Dueren :	pipeline steels with carbon content less than 0.3 wt%.

Beckert :	low alloy steels with carbon content less than 0.3 wt%.

Cottrell :	C      0.06  - 0.23 wt%

Si     0.00  - 0.55

Mn     1.01  - 2.00

Ni     0.00  - 0.89

Mo     0.00  - 0.54

V      0.00  - 0.15

Nb     0.00  - 0.05

Cu     0.00  - 0.03

S      0.002 - 0.043

N      0.003 - 0.010

References :

(1)	Y.Arata, K.Nishiguchi, T.Ohji, N.Kohsai, Transaction of Journal of

Japanese Welding Research Institute, 1979, Vol. 8, No. 1, pp 43.

(2)	N.Yurioka, S. Ohshita, H.Tamehiro, AWRA Symposium "Pipeline

Welding in the 80"s", Melbourne, March 18 1981, also JWS WM-784-80, pp

1-11.

(3)	N.Yurioka, M. Okumura, T.Kasuya, Metal Construction, April, 1987,

Vol. 19, No. 4, pp 217R-223R.

(4)	H.Suzuki, IIW DOC IX-1351-85, 1985, pp 1-15.

(5)	H.Suzuki, Trans. of Jap. Weld. Soc., 1984, Vol. 15, No. 1, pp 25-33.

(6)	K.Satoh, T.Terasaki, Jap. Weld., Soc. General Meeting, 1979, Vol.25, pp

98.

(7)	T.Terasaki, Jour. ISIJ, 1981, Vol. 16, pp 145-152.

(8)	C. Dueren, IIW DOC IX-1358-85, 1985, "3R International", 24 Jahrgang,

Heft.

(9)	M.Beckert, R. Hoz, Schw. Tech., 1973, Vol. 23, No. 8, pp 344.

(10)	C.L.M.Cottrell, Metal Construction, Dec.1984, Vol. 16, pp 740-744.

(11)	C.M.Adams, Welding Journal AWS, 1958, Vol. 37, No. 5, pp 210.

5.2  Reheat Hardness Module

Post weld heat treatment (PWHT) is applied to a weldment to reduce

residual stress levels which among other things decreases the sensitivity of a joint

to corrosion. It may also lower the HAZ hardness and thereby increase the

toughness of this region.

The PWHT materials model is based on a regression model proposed by

Yurioka et al [12]. The input data consists of the welding conditions (voltage,

current, welding speed, process efficiency and ambient temperature), the base

metal chemical composition and the reheat parameters (reheat time and reheat

temperature). The as-welded HAZ hardness is calculated in the first instance. The

hardness after PWHT is then determined by subtracting the change in hardness

due to the reheat treatment from the as-welded HAZ hardness. The Adams [11]

heat transfer relationships are employed to calculate the 800 to 500oC weld

cooling time. The regression limits are listed as follows:

Yurioka Reheat Model : 	C   <=  0.263 wt%

Si  <=  0.410

Mn  <=  1.450

Cu  <=  0.119

Ni  <=  3.328

Cr  <=  0.504

Mo  <=  0.562

V   <=  0.100

Nb  <=  0.100

P   <=  0.017

S   <=  0.007

B   <=  2ppm

550oC < Reheat Temperature < 650oC

1hr <    Reheat Time     < 10hr

Reference

(12)	M.Okumura, N.Yurioka, T.Kasuya, H.J.V.Cotton, "Prediction of HAZ

Hardness after PWHT", IIW International Conference on Residual Stress and

Stress Relieving, Sofia, Bulgaria, July 6-7, 1987, pp 61-68.

5.3  Preheat Treatment Module

Underbead cold cracking is one of the principal concerns in the welding

industry. Without preventive measures, cracks can form in the heat-affected zone

(HAZ) immediately adjacent to the fusion line as the weld cools. The probability

of underbead crack formation is greatly enhanced by the presence of hydrogen.

Hydrogen is trapped in a supersaturated state in the HAZ and fusion zone when a

weld cools rapidly. However, if a weld cools relatively slowly, the hydrogen that

appears in the HAZ can escape before tension stresses and hardened

microstructure develop. Slow cooling is, therefore, a way of minimizing the risk

of crack formation.

In practice preheat is used to slow the weld cooling process. A preheat

temperature high enough to permit enough time at temperature for the hydrogen

level to drop below a critical level is specified by welding engineers. So important

is the hydrogen factor that the Yurioka model [13,14,15] is based entirely on this

principal. According to this model, a weld must reside above 100oC for a time

longer than the critical time necessary for the hydrogen level drop to a safe level.

The critical time depends on the chemical composition of the workpiece, the stress

level (influenced by joint configuration and work piece size primarily), and the

hydrogen level generated by the heat source.

Both uniform and local preheat conditions are provided in this software.

Furthermore, for the convenience of the users, typical heat intensity values for

electric strip heaters and torches are also included in the software. They are 2.5

J/mm.s per plate thickness (mm) with about 250 mm heating width and 4.5

J/mm.s per plate thickness with about 100 mm heating width respectively [13]

with local heating effect.

The actual residence time above 100oC is a function of the preheat level

and workpiece dimensions. The heat transfer model of Satoh and Matsui [16] is

used to calculate the residence time above 100oC. If this time is greater than the

critical time, the formation of underbead cracks is said to be prevented. The unit

of "length" and "width" used in the preheat parameters is in mm. The unit of "heat

intensity" used in the locally preheat model is in J/(mm2s). This is the heat input

rate (J/s) per unit of cross sectional area (mm2) along the weld joint. Some

commonly used figures are listed below:

Typical HIIW values for common welding techniques.

Rutile Coated     :     25

Flux-cored CO2    :     22

Submerged-arc     :     15

Basic Coated      :     13

Gas shielded      :      7

Typical restraint coefficients (rf) for benchmark weld tests.

Tekken Test       :    690

Stout Test        :    490

H-slit Test       :    680

RRC Test          :    E/l

Ordinary Joints   :  <=390

Typical stress concentration factors (Kt) for common weld preparations.

y Groove          :      4

Double-V          :    3.5

Y Groove          :    4-5

Single-Bevel      :    6-8

V or Toe          :    1.5

Alloy content limitations for the Yurioka Preheat Model.

C       0.02 - 0.26 wt%

Si      0.04 - 0.45

Mn      0.87 - 2.01

Cu      0.00 - 0.23

Ni      0.00 - 0.81

Cr      0.00 - 0.85

Mo      0.00 - 0.47

V       0.00 - 0.07

Nb      0.00 - 0.05

References

(13)	N.Yurioka, H.Suzuki, S.Ohshita, S.Saito, welding Journal, Vol. 62, No. 6,

pp 147s, 1983.

(14)	N.Yurioka, M.Okumurs, S.Ohshita, S.Saito, IIW DOC XII-E-10-81, April

1981.

(15)	H.Suzuki, N.Yurioka, IIW DOC IX-1458-87, 1987.

(16)	K.Satoh, S.Matsui, Journal of JWES, Vol. 40, No. 11, pp 1117, 1971.

(17)	N.Yurioka, Materials and Sesign, Vol. VI, No. 4, 1985.

(18)	V.Mehrotra, M.Bibby, J.Goldak, J.Moore, "A Microcomputer Method for

Predicting Preheating Temperature", published in "Welding for Challenging

Environments", edited by the Welding Institute of Canada, Pergamon Press, New

York, 1986, pp 233-244.

Remark :	A more detailed description of these models is contained in Chan's

Master's thesis [19].

(19)	B.K.H.Chan, "Software for Welding Engineers", Master Thesis, 1990,

Department of Mechanical and Aerospace Engineering, Carleton University.