Supplemental User's Guide

The 'Weld Shape' module consists of four sub-modules: 'GMAW', 'SAW', 'SAW Y 1e'

and 'SAW Y 2e'. The 'GMAW' module is for predicting gas metal arc weld size and shape, please

refer to Chapter 3 & 4 in the user's guide for details. The other three modules are for predicting

submerged arc weld size and shape for different welding situations.

1)  'SAW' Module

The 'SAW' module is for predicting the size and shape of bead-on-plate submerged arc

welds. The weld features definitions are illustrated in Figure 1. The system is based on algorithms

originated by McGlone et al (McG.) [1]. However, McGlone model has not included the effects

of electrode polarity and electrode extension. The Chandel model (Cha.) [2,3,4,5] extended the

McGlone model to cover the effect of different electrode polarity and electrode extension. The

Yang models (two) are based on curvilinear (Y.Cu.) and linear (Y.Li.) regression technologies

[5,6,7]. Both models are useful in practice and Yang suggests that while the curvilinear approach

is more comprehensive, there does not seem to be a great deal of difference in accuracy.

Regression limits are listed in Table 1.

Table 1  The 'SAW' Module Regression Limits.

|  | McGlone Model | Chandel/Yang Models |
| --- | --- | --- |
| Electrode extension | 25 mm | 25.4 - 76.2 mm |
| Electrode orientation | 90o | N/A |
| Joint gap | 0 mm | 0 mm |
| Plate thickness | 19.0 mm | 19.0 mm |
| Material type | C-Mn steel | ASTM A36 |
| Electrode / Flux type | S3 / A50 | L60 / Linde124,OP121TT |
| Welding Current | 400 - 900 Amp | 300 - 1000 Amp |
| Arc Voltage | 25 - 35 Volt | 32 - 38 Volt |
| Welding Speed | 6.67 - 13.33 mm/s | 3.22 - 12.66 mm/s |
| Electrode diameter | 3.2 - 5.0 mm | 2.4 - 4.0 mm |
| Joint included angle | 0 - 90o | 0o |

2)  'SAW Y 1e' Module

Joint preparation (Y-groove) is also include in McGlone model [1]. Independent work has

also been done by Chandel and Yang [5]. The weld features definitions are shown in Figure 2. All

these models for predicting weld size and shape of SAW with Y-groove plate preparation and

single electrode are wplemented in the 'SAW Y 1e' module. we regression limits of these four

models are listed in Table 2.

Table 2  The 'SAW Y 1e' Module Regression Limits.

(All limits are the same as Table 1 except the following.

M1 is McGlone model and M2,M3&M4 are Yang models.)

| Model | Electrode Polarity | Electrode Diameter | Electrode Extension | Root Gap |
| --- | --- | --- | --- | --- |
| M1 | +ve | 3.2 - 5.0 mm | 25.0 mm | 0 mm |
| M2 | -ve | 2.4 mm | 32.0 mm | 1.58 mm |
| M3 | +ve | 2.4 mm | 76.0 mm | 1.58 mm |
| M4 | -ve | 4.0 mm | 32.0 mm | 1.58 mm |

3)  'SAW Y 2e' Module

Chandel and Yang [5] have extended the SAW Y-groove single electrode to include twin

electrodes. Four relationships have been proposed to cover different welding situations. The weld

features definitions are shown in Figure 2. All these models are automated in the 'SAW Y 2e'

module and the regression limits are listed in Table 3.

Table 3  The 'SAW Y 2e' Module Regression Limits.

(All limits are the same as Table 1 except the following.)

| Model | Electrode Polarity | Electrode Diameter | Electrode Extension | Skew Angle |
| --- | --- | --- | --- | --- |
| M1 | -ve/+ve | 2.4 mm | 32.0 mm | 0o |
| M2 | -ve/+ve | 2.0 mm | 32.0 mm | 0o |
| M3 | +ve | 2.4 mm | 32.0 mm | 10o |
| M4 | +ve | 4.0 mm | 32.0 mm | 10o |

4)  References

1)	J.C. McGlone, D.B. Chadwick, The Submerged Arc Butt Welding of Mild Steel Part 2:

The Prediction of Weld Bead Geometry from the Procedure Parameters, The Welding

Institute Report No. 80/1978/PR, Dec. 1978, 26 pgs.

2)	R.S. Chandel, S.R. Bala, Relationship between Submerged Arc Welding Parameters and

Weld Bead Size, Welding and Cutting Journal, Vol. 2, p.p. E28-30, 1988.

3)	R.S. Chandel, Mathematical of Melting Rates for Submerged Arc Welding, Welding

Journal, p.p. 135s-140s, May 1987.

4)	R.S. Chandel, Melting Efficiency of SAW and its Prediction, Australian Welding Journal,

p.p. 23-25, First Quarter 1989.

5)	L.J. Yang, personal communication, School of Mechanical & Production Engineering,

Nanyang Technological Institute, Singapore, January, 1991.

6)	L.J. Yang, M.J. Bibby, R.S. Chandel, Modelling the Submerged-Arc Welding Process

Using Linear Regression Equations, 3rd Conference on Trends in Welding Research,

Gatlinburg, Tennessee, USA, June 1-5 1992 (to be presented).

7)	L.J. Yang, A Study on the Submerged-Arc Welding Process Variables, Internal Report,

School of Mechanical & Production Engineering, Nanyang Technological Institute,

Singapore, April 30, 1991.