Chapter 3    Quick Tutorial

If a hard disk system is used, the logged directory should be the sub-

directory holding all the WeldSoft package files.

3.1   Loading WeldSoft

At the DOS prompt:

-	type :- WELDSOFT

The main interface appears with a pop-up menu displaying the following choices:

'HAZ HARDNESS', 'REHEAT HARDNESS', 'PREHEAT TREATMENT',

'DOCUMENTATION', 'SET UP' and 'EXIT', as shown in Figure 3.1. If a mouse

is present, a pointing arrow cursor also appears.

3.2   Changing Default Set Up

-	select by pressing <↓> to highlight 'SET UP' and <enter> or move the

mouse cursor to the 'SET UP' box and click.

A second pop-up menu appears with the choices of: 'REGRESS.LIMITS',

'PRINTER', 'COLOR' and 'EXIT', as shown in Figure 3.2.

-	to select 'REGRESS.LIMITS', press <↓>/<↓> and <enter> or click the

mouse button at the 'REGRESS.LIMITS'  box. This confines all

calculations to the chemical composition and welding parameters limits

imposed by the models.

A third pop-up menu appears showing the choices of regression limits

status - 'active' (default setting) or 'inactive'.

-	to change the current regression limits status to 'inactive', press <↑>/<↓>

and <enter> or click the mouse button at 'inactive' box.

The default printer type is 'dot matrix'. If you are using a HP II Laser Jet,

change the printer type to 'HPII Laser' by following the instructions below:

-	on the 'SET UP' menu, to select 'PRINTER', press <↑>/<↓> and enter or

click the mouse button at the 'PRINTER' box.

-	to select 'HP II Laser', press <↑>/<↓> and <enter> or click the mouse

button at the 'HP II Laser' box.

-	to select 'EXIT', press <↑>/<↓> and <enter> or click the mouse button at

the 'EXIT' box and the system will return to main interface.

3.3   Calculating HAZ Hardness

-	select 'HAZ Hardness' at main interface. The HAZ Hardness module

comes up on the screen as shown in Figure 3.3. Please note the menu bar

at the top of the screen.

- For example :

type :-	300	<enter>	{welding current}

25	<↓>		{welding voltage}

{<↓> accepts value as <enter> does}

5	<↑>		{amb. temperature}

{<↑> accepts value and moves the cell upward}

<enter>

<enter>

50	<enter>	{plate thickness}

{in most cases only 2 decimal digits are printed}

5	<enter>	{welding speed}

90	<enter>	{efficiency}

0.12	<enter>	{C}

1.29	<enter>	{Mn}

0.26	<enter>	{Si}

0.15	<enter>	{Ni}

0.15	<enter>	{Cr}

0.05	<enter>	{Mo}

0.1	<enter>	{V}

0.0	<enter>	{B}

0.01	<enter>	{Cu}

0.01	<enter>	{Nb}

0.01	<enter>	{N}

0.01	<enter>	{S}

All necessary welding parameters (both welding conditions and steel

chemical composition) have now been entered and it is ready to activate the

calculation.

-	press <F1> or click the mouse button at 'F1 CALC' box.

The calculated HAZ hardness appear in the output window at the lower

left-hand corner of the screen, as shown in Figure 3.4.

Note :	Please remember to select 'F1 CALC' if you want to re-compute the

results.

3.4   Data File Features

You may want to save the current data to a file for future use.

-	press <F7> or click the mouse button on 'F7 FILE'.

A pull-down menu appears, as shown In Figure 3.5, which allows you to

select either process or steel compositions files to work with.

-	select 'PROCESS'.

A new pull-down menu appear as shown in Figure 3.6, which allows you

to retrieve, add, edit or delete a data file.

-	select 'ADD' by pressing <↓> and <enter> or by using the mouse.

You are asked to enter the file name as shown in Figure 3.7.

-	type :- DATA1 <enter>

The current data are echoed as shown in Figure 3.8. You can change any

data here as in the input data editor.

-	press <ESC> to save the data listed in the pop-up window to the file,

DATA1.HAZ.

-	select 'F7 FILE' again by pressing <F7> or by using the mouse.

-	select 'PROCESS' and then 'EDIT' from the pull-down menus to edit a

data file.

-	select 'DATA1' from the pull-down menu.

-	press <enter> to confirm that you do not want to change the file name.

-	press <↓> until 'INIT TEMP' is highlighted.

-	type '25' <ENTER>.

-	press <ESC> to confirm the change and re-save the file, DATA1.HAZ.

-	press <F7> or select 'F7 FILE' by using the mouse again.

-	select 'PROCESS' and then 'DELETE' from the pull-down menus to delete

a data file.

-	select 'DATA1' from the pull-down menu.

A pop-up message appears and you are asked to confirm the deletion.

-	type :-  y    {to confirm the deletion}

The file to be deleted is saved as DATA1.BAK for backup reasons. After

the extension has been changed to .BAK, the data file becomes invisible to the

system. You can re-activate the data file by changing the .BAK extension to .HAZ

with the DOS command (copy DATA1.BAK DATA1.HAZ). On the other hand,

if you want to delete the data file permanently, type:- del DATA1.BAK at the

DOS prompt.

Instead of entering the values with the input data editor, frequently used

data can be retrieved directly from the data file.

-	press <F7> or select 'F7 FILE' with the mouse.

-	select 'PROCESS' and then 'RETRIEVE' from the pull-down menus.

-	select 'WELD' from the pull-down menu.

The input data window is automatically updated.

At this point in the tutorial, you will be able to use the 'Data File Features'

fluently.

3.5   Plotting a Graph (Parametric Study) -

e.g. plot [Suzuki calculated HAZ hardness vs voltage]

-	press <F6> or click the mouse button at 'F6 PLOT'.

A pull-down menu is activated as shown in Figure 3.9 which allows you

to select an x-axis title.

-	select 'VOLTAGE' by pressing <↓> and <enter> or using the mouse.

Another pull-down menu appears automatically which allows you to select

a y-axis title.

-	select 'Suzuki' by using <↓> and <enter> or by using the mouse.

A pop-up window appears and asks you to enter the lowest welding

voltage as the minimum plotting range.

-	type :- 30 <enter>

A pop-up window appears and asks you to enter the highest welding

voltage as the maximum plotting range.

-	type :- 50 <enter>

You have now asked the system to plot the Suzuki calculated HAZ

hardness vs welding voltage in the range of 30 volts to 50 volts. An automatically

scaled and titled graph (see Figure 3.10) is generated in a few seconds.

3.6   Output to a Printer

-	press <F8> or select 'F8 PRIN' from the menu bar by using the mouse.

A pop-up window appears and the system tells you both the printer type

you selected and the printer status, see Figure 3.11. Check to see if the correct

printer type is selected. If the printer is connected properly, the system will ask

you to confirm the print command;

type :- y {if you are positive}

n {if you are not positive}.

3.7   Changing Default Settings inside the Module

-	press <Alt P> to switch the printer type.

{a message will appear on the screen to confirm the newly selected

printer type.}

-	press <Alt R> to switch the regression limits status.

{a message will display the latest regression limits status.}

3.8   On-Line Help

On-line help is provided for each individual module.

-	press <F9> or select 'F9 HELP' from the menu bar by using the mouse.

A pop-up help window appears as shown in Figure 3.12. You can remove

it by pressing any key, e.g. <enter>.

3.9   Exiting HAZ Hardness Module

-	type <ESC> or click the mouse button at the '<ESC>' box to end this

section and return to the main interface.

3.10   Next Move

Are you ready to explore the other special features provided by this

system? Select the desired module and press <enter> or move the mouse cursor to

the appropriate box and click the mouse button. If you still feel uncomfortable or

hesitate, please follow the next few chapters. They will guide you through the

entire system.

Selecting 'EXIT' will terminate the program and put you back to the DOS

prompt.

Congratulations!! You have finished practising all the basic WeldSoft features.

You should be able to work through the other modules. The documentation

section in the main interface provides you some quick hints and background

material. Please spend some time to read it.